Supplementary file

Efficient Synthesis of Isoamyl Acetate Using a Thermostable Geobacillus kaustophilus Lipase Immobilized in TPP-Crosslinked ZIF-8

Murat Türk*

Cukurova University, Ceyhan Vocational School, 01330, Adana, Turkey

*Corresponding author: e-mail: murturk@cu.edu.tr

Table S1. Summarization of purification process of GkL.

| Purification step | Volume (mL) | Total protein (mg) | Total activity (U) | Specific activity (U/mg protein) | Purification (fold) | Activity yield (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Cell free | 10.0 | 26.8 | 1786.3 | 66.7 | 1.0 | 100 |
| Ni2+-NTA | 6 | 4.6 | 813.2 | 176.8 | 2.7 | 45.5 |
| Concentrated protein | 2.5 | 2.3 | 437.6 | 190.3 | 2.9 | 24.5 |

Fig. S1. The retention times of isoamyl alcohol (6.34 min) and isoamyl acetate (8.13 min).

Fig. S2. SDS PAGE profile of the concentrated GkL. Lane 1 shows the GkL sample after ultrafiltration, exhibiting a distinct band at approximately 45 kDa. Lane M corresponds to the molecular weight marker (BioRad All Blue Protein Standards, catalog no. 161-0373).