Precise and convergence pattern was obtained in the detection of mammary gland carcinoma using molybdenum enhanced poly taurine nano-biofilms compared to pathological examination

Hassan Nasrollahpoura, Balal Khalilzadehb*, Reza Rahbarghazib,c, Nevin Erkd, Mohammad-Reza Rashidie, Abdolhossein Naseria*

a Department of Analytical Chemistry, Faculty of Chemistry, University of Tabriz, Tabriz, Iran.

b Stem Cell Research Center, Tabriz University of Medical Sciences, Tabriz, Iran.

c Department of Applied Cell Sciences, Faculty of Advanced Medical Sciences, Tabriz University of Medical Sciences, Tabriz, Iran.

d Department of Analytical Chemistry, Faculty of Pharmacy, Ankara University, Ankara 06560, Turkey.

e Research Center for Pharmaceutical Nanotechnology (RCPN), Tabriz University of Medical Sciences, Tabriz, Iran.

Corresponding authors:

Balal Khalilzadeh, PhD, Stem Cell Research Center (SCRC), Tabriz University of Medical Sciences, 51664-14766 Tabriz- Iran, Tel: +98(41)-33363311; Fax: +98(41)33363231

Email: khalilzadehb@tbzmed.ac.ir, balalkhalilzadeh@gmail.com

Abdolhossein Naseri, PhD, Department of Analytical Chemistry, Faculty of Chemistry, University of Tabriz, PO Box 51644‐14766, Tabriz, Iran. Email: a_naseri@tabrizu.ac.ir

Figure captions:

Figure S1: Investigation of the effect of each modifier on the electrochemical behavior of the proposed framework. All the data were obtained in K4[Fe (CN)6] (5 mM).

Figure S2: The EDX and dot mapping quantitative elemental analysis of the different modified electrodes. A and B: MoO3 modified electrode. C and D: p-Tau modified electrode. E and F: MoO3/p-Tau modified electrode.

Figure S3: Effect of the deposition cycle numbers on the electrochemical signals. A) DPV voltammograms and B) Correlated histograms. All the signals were obtained in K4[Fe(CN)6] (5 mM).

Figure S4: Incubation time study of anti-HER-2 on the as-prepared MoO3/p-Tau/GCE at different time points (10, 30, 45, 60, 90 and 120 minutes).

Figure S5: Evaluation of the selectivity of the design immunosensor in the presence of 10 pg/mL of CEA, BSA and CA-15-3, different concentrations of HER-2 (1pg/mL and 1 fg/mL) and also in the presence of mixture of them.

Figure S6: The reproducibility screening of the suggested framework at different three electrodes with the same procedure.

Figure S7: The signal stability of the immunosensor for 10 consecutive signals.

Figure S1

A

B

C

D

F

E

Figure S2

Figure S3

Figure S4

Figure S5

Figure S6

Figure S7