Supporting Information

Bioinspired nano-ordered liquid membrane for precise molecular separation

Haozhen Dou,1 Mi Xu,1,2 Baoyu Wang,4 Feifei Peng,1,2 Zhen Zhang,1 Guobin Wen,1 Dan Luo,1 Aiping Yu,1 Zhengyu Bai,3 Zhongyi Jiang2*& Zhongwei Chen1*

DOI:

Table of Contents

Experimental  ·················································································································································································3

Materials ···························································································································································································3

Synthesis of PES support ·································································································································································3

Synthesis of PSs ···············································································································································································3

Results and Discussion ··································································································································································4

Supplementary Figures ····································································································································································4

Supplementary Tables ····································································································································································18

References ······················································································································································································20

Author Contributions ··································································································································································21

Experimental

Materials

Ethylene, ethane and nitrogen (99.99 mol%) gases were purchased from Linde Gas. Ethanolamine, diethanolamine, triethanolamine, 1-methylimidazole and caprolactam were supplied by Alfa Aesar and was further purified by Vacuum reduced pressure distillation prior to use. Nitric acid (65-68 wt%), N-methyl-2-pyrrolidone (NMP), 1, 4-dioxane (DX), glycerol (G), ethylene glycol (EG), triethylene glycol (TEG) and silver nitrate were all supplied from Sigma-Aldrich and were used without purification. Poly (L-lactic acid) (4032D, Mw = 196kDa, Mw/Mn = 2, 1.6% D-lactide) was purchased from Nature Works LLC (USA). Polyethersulfone (PES Ultrason E6020P, MW = 58 kDa) was supplied by BASF (Germany) and was dried at 110 °C for 12 h prior to use. Deep eutectic solvent (Decanoic acid (DecA): tetrabutylammonium chloride (N4444-Cl)= 2:1) was kindly supplied by Tianjin University.

Synthesis of PES support

The home-made PES flat support was fabricated via immersion precipitation method according to the our previously reported procedure with some modifications.1, 2 In a typical process, 10 wt% PES and 5 wt% Poly(L-lactic acid) were dissolved in the mixed solvents of NMP and DX (2:1) with the deep eutectic solvent (DecA:N4444-Cl (2:1)) concentration of 6 wt%. The mixture was stirred vigorously at 65 °C for 10 h to obtain a uniform and homogeneous casting solution, and then the solution was degassed in a vacuum drier overnight. Afterwards, the solution was spread by a casting knife with the clearance of 80 μm onto a clean glass plate. After 30 s exposure to air, the glass plate was immediately immersed in a distilled water coagulation bath at ambient temperature and kept for 24 h to remove the residual solvent. Finally, the prepared membranes were dried for 24 h at room temperature for further use.

Synthesis of PSs

The PSs such as ethanolammonium nitrate, diethanolammonium nitrate, triethanolammonium nitrate, 1-methylimidazolium nitrate, caprolactam nitrate, were prepared at University of Waterloo and the synthesis was made using a similar procedure as described in our previous report.3, 4 The PSs were formed by dropwise addition of acid to the equimolar quantities of the respective amines at 0 oC or below and the methanol was used as solvent. Then the mixture was then stirred vigorously at room temperature for several hours. The pure PSs were obtained after crystallization, washing and drying.

Results and Discussion

Supplementary Figures

Figure S1. (a) The chemical structure of PSs and polyols involved in this study.

Figure S2. 1HNMR spectra of PSs.

Figure S3. FTIR spectra of PSs.

Figure S4. A synthetic route to prepare membrane liquid.

Figure S5. TG Curves of binary eutectics of DEAN- G and EAN-G to indicate the good thermal stability of corresponding bioinspired nano-ordered liquid membrane.

Figure S6. Demonstrations of hydrogen bonding and electrostatic attractions in binary eutectics based on PS (EAN) and polyol (TEG or EG) by 1HNMR.

Figure S7. Demonstrations of hydrogen bonding and electrostatic attractions in binary eutectics based on PS (EAN) and polyol (TEG or EG) by ATR-FTIR spectra.

Figure S8. Radial distribution functions of carrier-cation, carrier-anion and carrier-G molecule.

Figure S9. Snapshot bulk structure of bioinspired nano-ordered liquid membrane (EAN: glycerol = 1:2), where the carbon, hydrogen, oxygen, nitrogen and silver atoms are shown in grey, in white, in red, in blue and in Tiffany blue, respectively, (a) all atoms, (b) G molecules. (c) EAN cations, (d) NO3- anions of EAN and silver salt

Figure S10. Diagram of experimental setup.1-gas bottles, 2-buffer tanks, 3-mass flow controllers, 4-two-way valves, 5-static mixer, 6-three-way valves, 7-permeation cell, 8- air blowing thermostatic oven, 9-mass flow meter, 10-presure transducers, 11-micrometric values, 12-gas chromatograph. Mixed-gas permeation experiments were performed as reported by our group previously and the set-up was shown in Figure S10. The membrane cell was composed of three parts, the upper chamber, a rubber ring and the lower chamber, which were made of stainless steel (AISI 316L). Two buffer tanks were installed after the gas cylinders to stabilize the gas flow. The flow rate of each gas was adjusted by a mass flow controller (CS200A, Bei Jing Sevenstar Electronics Co., Ltd, China) to obtain the equal molar ratio of ethylene to ethane. The ethylene and ethane were thoroughly mixed by the static mixer, and the composition of the gas mixture was further analyzed by an online gas chromatograph. The mixed gas flowed through the upper chamber of the membrane cell, whose pressure was regulated by a micrometer value according to the experimental requirements. The nitrogen, as a sweep gas, flowed through the lower chamber of the cell, and the pressure of nitrogen was kept at the atmosphere pressure throughout the experiment. The outlet gas flow rate from the lower chamber, containing nitrogen, ethylene and ethane, was measured using a mass flowmeter (CS200, Bei Jing Sevenstar Electronics Co., Ltd). The composition of the permeated gas was analyzed by the online gas chromatograph equipped with a flame ionization detector and a packed column (GC-7820, Lunan Analytical Instrument Co., Ltd, China).

Figure S11. Effect of PSs on separation performance in terms of ethylene permeability and ethane permeability.

Figure S12. Effect of polyols on separation performance in terms of ethylene permeability and ethane permeability.

Figure S13. Effect of silver salt concentration on separation performance in terms of gas permeability and ethylene/ethane permeability.

Figure S14. The effects of transmembrane pressure, operating temperature, the feed ratio of ethylene/ethane and the flow rate of sweep gas on gas separation performances.

Figure S15. Comparison of bioinspired nano-ordered liquid membranes with other previously reported ethylene/ethane separation membranes based on the ethylene/ethane selectivity-ethylene permeance.

Supplementary Tables

Table. S1 Densities and melting points of protic ionic liquids (PSs)

| PSs | Abbreviations | Tm (oC) | ρ (g/cm3) |
| --- | --- | --- | --- |
| 1-methylimidazolium nitrate | [MIMN] | 70 | 1.125 |
| Caprolactam nitrate | [CAPN] | 52 | 1.085 |
| ethanolammonium nitrate | [EAN] | 51.0 | 1.265 |
| diethanolammonium nitrate | [DEAN] | 72 | 1.204 |
| triethanolammonium nitrate | [TEAN] | 80 | 1.178 |

Table. S2 The compositions, melting points, densities, ion conductivities and the viscosities of the studied PS-DESs

| HBA | HBD | nHBA : nHBD | Tm /K | ρ /g·cm-3 | η /cp | σ /ms·cm-1 |
| --- | --- | --- | --- | --- | --- | --- |
| [MIMN] | [G] | 1:1 | -91.50 | 1.212 | 23.91 | 3.163 |
| [MIMN] | [G] | 1:2 | -88.20 | 1.177 | 33.75 | 1.784 |
| [MIMN] | [G] | 1:3 | -86.40 | 1.179 | 73.275 | 1.256 |
| [MIMN] | [EG] | 1:1 | -87.50 | 1.188 | 11.955 | 6.263 |
| [MIMN] | [TEG] | 1:1 | -70.50 | 1.123 | 19.62 | 2.530 |
| [CPAN] | [G] | 1:2 | -75.40 | 1.109 | 117.65 | 0.785 |
| [EAN] | [G] | 1:1 | -90.96 | 1.251 | 68.52 | 3.070 |
| [EAN] | [G] | 1:2 | -88.06 | 1.270 | 102.35 | 1.867 |
| [EAN] | [G] | 1:3 | -87.06 | 1.176 | 178.35 | 1.136 |
| [EAN] | [EG] | 1:1 | -88.43 | 1.191 | 12.77 | 11.940 |
| [EAN] | [TEG] | 1:1 | -68.23 | 1.121 | 53.16 | 2.490 |
| [DEAN] | [G] | 1:1 | -87.43 | 1.252 | 103.62 | 1.602 |
| [DEAN] | [G] | 1:2 | -82.72 | 1.185 | 115.875 | 1.034 |
| [DEAN] | [G] | 1:3 | -78.43 | 1.198 | 158.57 | 0.707 |
| [DEAN] | [EG] | 1:1 | -85.65 | 1.183 | 15.645 | 4.380 |
| [DEAN] | [TEG] | 1:1 | -65.32 | 1.117 | 39.54 | 1.602 |
| [TEAN] | [G] | 1:2 | -80.35 | 1.180 | 134.175 | 0.987 |

Table. S3 The coordination number obtained by molecular dynamics simulation.

| Molecule A | Molecule B | Rmax/A | Ncoord |
| --- | --- | --- | --- |
| Anion | Glycerol | 4.35 | 1.43 |
| Glycerol | Glycerol | 4.75 | 2.57 |
| Anion | Anion | 4.95 | 2.22 |
| Cation | Cation | 5.05 | 1.75 |
| Glycerol | Cation | 4.65 | 1.69 |

References

1.Jiang B, Zhang N, Zhang L, Sun Y, Huang Z, Wang B, et al. Enhanced separation performance of PES ultrafiltration membranes by imidazole-based deep eutectic solvents as novel functional additives. J Membr Sci 2018, 564: 247-258.

2.Jiang B, Wang B, Zhang L, Sun Y, Xiao X, Yang N, et al. Preparation of poly (L-lactic acid) membrane from solvent mixture via immersion precipitation. Separation Science and Technology 2016, 51(18): 2940-2947.

3.Dou H, Jiang B, Xiao X, Xu M, Wang B, Hao L, et al. Ultra-stable and cost-efficient protic ionic liquid based facilitated transport membranes for highly selective olefin/paraffin separation. J Membr Sci 2018, 557: 76-86.

4.Dou H, Jiang B, Xiao X, Xu M, Tantai X, Wang B, et al. Novel Protic Ionic Liquid Composite Membranes with Fast and Selective Gas Transport Nanochannels for Ethylene/Ethane Separation. ACS Appl Mater Inter 2018, 10(16): 13963-13974.

Author Contributions

H. Dou, M. Xu and Z. Jiang, Z. Chen devised the idea. H. Dou, M. Xu and F. Peng conducted the experiments. H. Dou, B. Wang and Z. Zhang cowrote the manuscript.  G. Wen and D. Luo conducted MD simulation. and made efforts on writing the manuscript. A. Yu, Z. Bai, Z. Jiang, Z. Chen gave valuable advices along the work. All authors discussed the results.