Supplementary Material

Construction of triazine-based COF/Zr-based MOF S-scheme heterojunctions for efficient photocatalytic H2O2 production under simulated sunlight irradiation

Lisong Chen a,b,   Yunchao Zhang c,   Yan Yan c,   Jinhui Jiang a,c,   Rongfeng Guan a,b,*,   Pengyu Dong a,c,*

a Key Laboratory for Advanced Technology in Environmental Protection of Jiangsu Province, Yancheng Institute of Technology, Jiangsu, China.

b School of Chemistry and Chemical Engineering, Yancheng Institute of Technology, Jiangsu, China.

c School of Materials Science and Engineering, Yancheng Institute of Technology, Jiangsu, China.

* Corresponding authors.

E-mail addresses: rongfengg@163.com (R. Guan), dongpy11@ycit.edu.cn (P. Dong).

1. Additional experimental section

1.1. Detection of H2O2

After sampling every 15 min, solid-liquid separation procedure was carried out with a filter of 0.22 μm. To this solution, 1 mL of 0.1 mol·L1 aqueous potassium hydrogen phthalate (C8H5KO4) solution and 1 mL of 0.4 mol·L1 aqueous potassium iodide (KI) solution was added, and the mixture was allowed to sit for 30 minutes. Under acidic conditions (H2O2 + 3I + 2H+ → I3 + 2H2O), H2O2 molecules reacted with iodide anions (I) to produce triiodide anions (I3) with strong absorption around 350 nm. The quantity of I3 was determined via UV-vis spectroscopy based on the absorbance at 350 nm, which allowed the estimation of the amount of H2O2 produced during each reaction.

1.2. Measurement and calculation of apparent quantum efficiency

The measurement of AQE (Apparent Quantum efficiency) for H2O2 evolution was conducted under monochromatic light irradiation (300 W xenon lamp, λ = 420, 450, 500, and 550  nm). The concentration of catalyst is 0.3 mg/mL, and the radiation area is 6.9 cm2.The calculation formula for AQE was estimated as following equation:

AQE=number of H2O2 production×2number of incidaent photons×100%

The number of incident photons is:

Nincident=Pthv=ptλhc=IStλhc

Where I is the light power intensity (W m2), S is the irradiation area (m2), t is the reaction time (s), λ is the wavelength length (m) of the monochromatic light, h is Planck’s constant (6.63×1034 m2 kg s1), and c is the speed of light in free space (3.0 ×108 m s1).

2. Supplementary Figures

Fig. S1 The H2O2 concentration-absorbance standard curve.

The absorbance and standard fitting curves of H2O2 aqueous solutions with different known concentrations reacted with potassium iodide are shown in Fig. S1.

Fig. S2. Optical photograph of (a) NH2-UiO-66, (b) TFPT-Pa(CH3)2, (c) TNU-1, (d) TNU-2 and (e) TNU-3.

Fig. S3. XRD patterns of as-prepared products after photocatalytic cycles.

Fig. S4. (a) XPS survey, (b) C1s, (c) N 1s, (d) O 1s of TNU-2 before and after photocatalytic cycles.

3. Supplementary Table

Table S1. BET-specific surface area and pore volume of TFPT-Pa(CH3)2，NH2-UiO-66 and TNU-2 samples.

| Samples | BET-specific surface area (m2 g1) | Pore volume (cm3 g1) |
| --- | --- | --- |
| TFPT-Pa(CH3)2 | 467 | 0.529 |
| NH2-UiO-66 | 795 | 0.622 |
| TNU-2 | 689 | 0.577 |