Supplementary Information

Step-by-step mechanism insights into TiO2/Ce2S3 S-scheme photocatalyst for enhanced aniline production with water as proton source

Xu et al.

Supplementary Figures

Supplementary Figure 1. The calculation of work function. The electrostatic potentials of a anatase TiO2 (101), b rutile TiO2 (110) and c Ce2S3 (001) facets. The cyan, red, green and violet spheres stand for Ti, O, Ce and S atoms, respectively. Blue and red dashed lines indicate the Fermi and vacuum energy levels, respectively.

Supplementary Figure 2. X-ray diffraction (XRD) patterns of TiO2, TC1, TC5, TC7 and Ce2S3. TCx represents the TiO2/Ce2S3 hybrids, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; x is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 3. Morphology of TiO2 nanofibers. a TEM image, b HRTEM image.

Supplementary Figure 4. X-ray photoelectron spectroscopy (XPS) spectra of resultant samples. High resolution XPS spectra a O 1s of TiO2 and TC5, b S 2p of Ce2S3 and TC5. In-situ XPS spectra were recorded under UV-vis light irradiation. TC5 represents the TiO2/Ce2S3 hybrid, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; 5 is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 5. Band structures of TiO2 and Ce2S3. a Valence band (VB) XPS spectra, b Mott-Schottky plots and c Kubelka–Munk energy curve plots of TiO2 and Ce2S3. d Band structures of the composite photocatalyst.

Supplementary Figure 6. The transient absorption spectrum of TiO2 nanofibers recorded following the addition of an electron scavenger (AgNO3) and measured with 350 nm excitation.

Supplementary Figure 7. Electron spin resonance (ESR) spectra of TiO2 and TC5. TC5 represents the TiO2/Ce2S3 hybrids, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; 5 is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 8. The transient absorption kinetic traces of TiO2 and TC5 at 645 nm with prolonging the delay time.

Supplementary Figure 9. Electrochemical characterizations. a Transient photocurrent response for TiO2 and TC5 under UV-visible light irradiation in 0.5 M Na2SO4 aqueous solution. b Nyquist plots of TiO2, TC5 and Ce2S3 in 0.5 M Na2SO4 aqueous solution. c Polarization curves of TiO2, TC5 and Ce2S3 at a scan rate of 5 mV s−1 in 0.5 M Na2SO4 under UV-visible light irradiation. TC5 represents the TiO2/Ce2S3 hybrids, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; 5 is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 10. The recyclability of TC5 for the photocatalytic transfer hydrogenation. TC5 represents the TiO2/Ce2S3 hybrid, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; 5 is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 11. XRD patterns of TC5 before and after photocatalytic reaction. TC5 represents the TiO2/Ce2S3 hybrid, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; 5 is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 12. FESEM and TEM images of TC5 after photocatalytic reaction. TC5 represents the TiO2/Ce2S3 hybrid, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; 5 is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 13. High resolution XPS spectra of a Ce 3d and b S 2p of TC5 after photocatalytic reaction. TC5 represents the TiO2/Ce2S3 hybrid, where T and C represent TiO2 nanofiber and Ce2S3 nanoparticle, respectively; 5 is the mole percentages of Ce2S3 with respect to TiO2.

Supplementary Figure 14. The adsorption of reactants. Optimized structures of H2O and nitrobenzene molecules adsorbed on anatase TiO2 (101), rutile TiO2 (110), and Ce2S3 (001) facets. The cyan, red, green, violet, light pink, brown and blue spheres stand for Ti, O, Ce, S, H, C and N atoms, respectively.

Supplementary Figure 15. The desorption of products. Optimized structures of aniline molecule adsorbed on anatase TiO2 (101), rutile TiO2 (110), and Ce2S3 (001) facets. The cyan, red, green, violet, light pink, brown and blue spheres stand for Ti, O, Ce, S, H, C and N atoms, respectively.

Supplementary Figure 16. The photocatalytic hydrogenation process over TiO2/Ce2S3 hybrid. The green, red, violet, light pink, brown and blue spheres stand for Ce, S, O, H, C and N atoms, respectively.

Supplementary Figure 17. Free energy diagrams of photocatalytic nitrobenzene hydrogenation to aniline for: a anatase TiO2 and b rutile TiO2 single-unit-cell layers. The cyan, red, light pink, brown and blue spheres stand for Ti, O, H, C and N atoms, respectively.

Supplementary Table

Supplementary Table 1. The calculated surface energy of the typical low-index surfaces of Ce2S3.

| Facets | Surface energy (J m−2) |
| --- | --- |
| (001) | 0.34 |
| (011) | 0.59 |
| (111) | 0.80 |
| (113) | 0.73 |
| (121) | 0.91 |