Tables

Table 1: Independent variables and their coding levels used to optimise the extraction of lignin from Pterocarpus tinctorius via the response surface method

| Variables | Factors | Coded levels |  |  |
| --- | --- | --- | --- | --- |
|  |  | -1 | 0 | +1 |
| NaOH solution concentration (% w/v) | X1 | 0,05 | 0,07 | 0,09 |
| Agitation speed (rpm) | X2 | 150 | 200 | 250 |
| solid/liquid ratio | X3 | 0,05 | 0,075 | 0,1 |
| Extraction Temperature (°C) | X4 | 60 | 80 | 100 |
| Extraction time (H) | X5 | 2 | 4 | 6 |

Table 2: Total phenolic content (TPC) of lignin extracts obtained under different alkaline hydrolysis conditions

| Run | NaOH solution concentration (% w/v) | Agitation speed (rpm) | Solid/liquid ratio (% w/v) | Temperature (°C) | Time (hours) | TPC (mg GAE/g extracts) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0,05 | 150 | 0,05 | 60 | 2 | 175,51±0.02 |
| 2 | 0,05 | 150 | 0,05 | 60 | 4 | 174,8±0.2 |
| 3 | 0,05 | 150 | 0,05 | 60 | 6 | 175,02±0.42 |
| 4 | 0,05 | 150 | 0,05 | 80 | 2 | 174,91±0.015 |
| 5 | 0,05 | 150 | 0,05 | 80 | 4 | 170,8±0.01 |
| 6 | 0,05 | 150 | 0,05 | 80 | 6 | 168,55±0.12 |
| 7 | 0,05 | 150 | 0,05 | 100 | 2 | 178,01±0.21 |
| 8 | 0,05 | 150 | 0,05 | 100 | 4 | 176,84±0.06 |
| 9 | 0,05 | 150 | 0,05 | 100 | 6 | 168,89±0.045 |
| 10 | 0,05 | 150 | 0,075 | 60 | 2 | 168,02±0.1 |
| 11 | 0,05 | 150 | 0,075 | 60 | 4 | 170,89±0.05 |
| 12 | 0,05 | 150 | 0,075 | 60 | 6 | 168,02±0.00 |
| 13 | 0,05 | 150 | 0,075 | 80 | 2 | 158,78±0.09 |
| 14 | 0,05 | 150 | 0,075 | 80 | 4 | 178,58±0.07 |
| 15 | 0,05 | 150 | 0,075 | 80 | 6 | 178,41±0.20 |
| 16 | 0,05 | 150 | 0,075 | 100 | 2 | 175,44±0.72 |
| 17 | 0,05 | 150 | 0,075 | 100 | 4 | 169,78±0.09 |
| 18 | 0,05 | 150 | 0,075 | 100 | 6 | 179,81±0.061 |
| 19 | 0,05 | 150 | 0,1 | 60 | 2 | 168,52±0.08 |
| 20 | 0,05 | 150 | 0,1 | 60 | 4 | 168,02±0.011 |
| 21 | 0,05 | 150 | 0,1 | 60 | 6 | 157,57±0.09 |
| 22 | 0,05 | 150 | 0,1 | 80 | 2 | 149,09±0.28 |
| 23 | 0,05 | 150 | 0,1 | 80 | 4 | 154,6±0.013 |
| 24 | 0,05 | 150 | 0,1 | 80 | 6 | 160,4±0.4 |
| 25 | 0,05 | 150 | 0,1 | 100 | 2 | 161,1±0.073 |
| 26 | 0,05 | 150 | 0,1 | 100 | 4 | 170,56±0.014 |
| 27 | 0,05 | 150 | 0,1 | 100 | 6 | 172,96±0.05 |
| 28 | 0,05 | 200 | 0,05 | 60 | 2 | 171,5±0.033 |
| 29 | 0,05 | 200 | 0,05 | 60 | 4 | 174,02±0.00 |
| 30 | 0,05 | 200 | 0,05 | 60 | 6 | 171,52±0.42 |
| 31 | 0,05 | 200 | 0,05 | 80 | 2 | 170,25±0.59 |
| 32 | 0,05 | 200 | 0,05 | 80 | 4 | 172,51±0.085 |
| 33 | 0,05 | 200 | 0,05 | 80 | 6 | 174,12±0.32 |
| . | . | . | . | . | . | . |
| . | . | . | . | . | . | . |
| . | . | . | . | . | . | . |
| 245 | 0,09 | 250 | 0,1 | 60 | 2 | 155,55±0.02 |
| 246 | 0,09 | 250 | 0,1 | 60 | 2 | 155,55±0.02 |
| 247 | 0,09 | 250 | 0,075 | 100 | 2 | 164,02±0.02 |

Table 3: validation coefficients and their qualifications

| Metric | Significations | Valid values | Source |
| --- | --- | --- | --- |
| R2 (Fit) | Measures the proportion of the total variance in the dependent variable (Y) that is explained by the model (Goodness-of-Fit). | R2 ≤ 1 (nearly 1) | [1] |
| RMSE (Mean Squared Error) | Represents the average difference between observed values (yi) and predicted values (yi). It is expressed in the unit of variable Y (Magnitude and Penalty). | RMSE≈0 (nearly 0) | [1], [2] |
| MAE (Mean Absolute Error) | Gives a better idea of the typical error | MAE ≈ 0 (nearly 0) | [1], [2] |
| MPE (Mean Percentage Error) | signed mean error as a percentage | MPE ≈ 0 (nearly 0) | [1] |
| MAPE (Mean Absolute % Error) | Mean Absolute Percentage Error | MAPE ≈ 0 (nearly 0) | [1] |
| σn2 (Noise or Nugget) | Estimates the variance of irreducible noise or very short-range variability (source variance). | σn2 ≈ 0 (nearly 0) | [3] |

Table 4: Results of analysis of variance (ANOVA) for the quadratic model of the TPC of lignin extracts

| Source | Valeur F | Valeur de p |
| --- | --- | --- |
| Model | 11,58 | <10-4 |
| Linear | 22,1 | <10-4 |
| X1 | 9,15 | 0,014 |
| X2 | 1,14 | 0,313 |
| X3 | 34,55 | <10-3 |
| X4 | 0,83 | 0,385 |
| X5 | 1,16 | 0,309 |
| Square | 5,46 | 0,014 |
| X12 | 0,07 | 0,793 |
| X22 | 1 | 0,345 |
| X32 | 0,71 | 0,421 |
| X42 | 0,21 | 0,658 |
| X52 | 0,04 | 0,840 |
| Interaction with 2 factors | 4,71 | 0,014 |
| X1*X2 | 0,4 | 0,542 |
| X1*X3 | 13,24 | 0,005 |
| X1*X4 | 0,95 | 0,356 |
| X1*X5 | 0,82 | 0,391 |
| X2*X3 | 0,38 | 0,553 |
| X2*X4 | 0,23 | 0,64 |
| X2*X5 | 0,11 | 0,752 |
| X3*X4 | 3,52 | 0,093 |
| X3*X5 | 0,02 | 0,879 |
| X4*X5 | 0,26 | 0,622 |
| Lack of fit | 2.15 | 0.115 |
| R2 | 96.26% |  |

Table 5: Comparative study of the two models based on validation coefficients

| Metric | BO (Processus Gaussien) | MSR (Modèle Polynomial) | Interprétation |
| --- | --- | --- | --- |
| R2 (Fit) | 0.9996 (99.96 %) | 0.9701 (97.01 %) | The GP explains an additional 3% variance compared to the MSR model. Almost perfect fit for BO. |
| RMSE (Mean Squared Error) | 0.2234 | 1.93 | The average prediction error of the MSR is ≈ 8.6 times higher than that of the BO model. |
| MAE (Mean Absolute Error) | 0.051 | 1.48 | The typical error of the MSR is ≈29 times higher than that of the BO model. |
| MPE (Mean Percentage Error) | +0.029 % | -0.015 % | MSR shows almost zero directional bias, while BO shows a slight overestimation. MSR is more directionally neutral.. |
| MAPE (Mean Absolute % Error) | 3.1 % | 0.92 % | MSR shows a lower average relative error, which is counterintuitive but possible. |

Table 6: Predicted and experimental values of the total phenolic content (TPC) of lignin extracts obtained under optimal extraction conditions (5% NaOH, agitation speed of 178 rpm, 0.074 solid/liquid ratio, 82°C temperature at 4.59 h (≈275 min))

| Response | Predicted value | Experimental value | Relative error (%) |
| --- | --- | --- | --- |
| TPC (mg GAE/g extract) | 182.06 | 178.51±0.14 | 1.95 |