Supplementary Information

Electric field control of field-free spin-orbit torque switching via laterally modulated Rashba effect in Pt/Co/AlOx structures

Min-Gu Kang1†, Jong-Guk Choi1†, Jimin Jeong1, Jae Yeol Park1, Hyeon-Jong Park2, Jong Min Yuk1, Kyung-Jin Lee3, and Byong-Guk Park1★

1Department of Materials Science and Engineering, KAIST, Daejeon 34141, Korea

2KU-KIST Graduate School of Converging Science and Technology, Korea University, Seoul 02841, Korea

3Department of Physics, KAIST, Daejeon 34141, Korea

† These two authors equally contributed to this work.

★ Correspondence to: bgpark@kaist.ac.kr (B.-G.P.)

Supplementary Note 1. Electron energy loss spectroscopy analysis of Pt/Co/AlOx/TiO2 structure.

To investigate the effect of the gate voltage on oxygen concentration in Pt (5nm)/Co (1.4nm)/AlOx (2 nm)/TiO2 (40 nm) samples, we perform scanning transmission electron microscopy (STEM) and electron energy loss spectroscopy (EELS) measurements, which provides a hint for the lateral asymmetry caused by the gate voltage. Before preparing a cross-sectional sample using focused ion beam (FIB) technique, we applied an asymmetric gate voltage (VG,L = 0V, VG,R = +8V), VG < 0. Figure S1a shows the STEM image and elemental maps of the oxygen obtained from EELS, in which the position A (B) represents the region of the gate oxide located just below the edge of the gate electrode VG,L (VG,R). This demonstrates that the oxygen concentration is increased at the position B where a VG,R of +8V was applied as compared to the position A. This indicates that the VG induces the oxygen ion redistribution depending on its polarity, resulting in the oxygen concentration gradient (Fig. S1b). Moreover, Figure S1c shows the EELS spectra of the Ti L edges measured at the positions A and B, indicating that a positive VG causes a valence change of the Ti ion into a higher oxidation state, and thus Ti L3,2 peaks move toward higher energy [1]. From the oxygen EELS intensity, the stoichiometries are qualitatively estimated as TiO1.84 on the left and TiO2.16 on the right.

Figure S1. Electron energy loss spectroscopy analysis. a, STEM image and EELS mapping of oxygen in the TiO2 layer of a Pt(5nm)/Co(1.4nm)/AlOx(2 nm)/TiO2(40 nm) structure. b, EELS intensity of oxygen in TiO2 as a function of the position indicated in Fig. S1a. c, EELS spectra of the of Ti L3,2 edges at the positions A and B.

Supplementary Note 2. In-plane harmonic Hall voltage analysis of the spin-orbit torque

Landau-Lifshitz-Gilbert equation including out-of-plane spin-orbit torque (SOT) terms is given as [2-4]

∂m∂t=-γm×Beff+BDLTym×y+BFLTyy+BDLTzm×z+BFLTzz+αm×∂m∂t (S1),

where Beff includes the anisotropy (Bani), demagnetization (Bdem), exchange, and external fields; α is the damping constant; γ is the gyromagnetic ratio; BDLTy (BFLTy) and BDLTz (BFLTz) are the damping-like (field-like) SOT effective field from y-SOT and z-SOT, respectively. Here, we define the unit vector x as the current direction and z as the direction perpendicular to the film plane. We assume that inversion symmetry is broken in both the z- and y-directions, generating y-SOT and z-SOT, respectively. Figure S2a shows the effective fields due to y-SOT and z-SOT acting on the magnetization.

The current-induced effective field (∆B) due to the inversion asymmetry along the z- and y-directions is given by [5]

∆B=∆Bx,∆By,∆Bz=(-BDLTycosθ0+BDLTzsinθ0sinφ0, BFLTy+BOe-BDLTzsinθ0cosφ0,BDLTysinθ0cosφ0+BFLTz) (S2),

where BOe is the Oersted field, θ and φ are the polar and azimuthal angles of the magnetization direction, respectively. The subscript “0” denotes the equilibrium state of magnetization.

When applying a sinusoidal oscillating current (I=∆Isinωt) with frequency ω, the Hall voltage Vxy is expressed as,

Vxy=RxyI=Rxy,0+dRxydI∆Isinωt∆Isinωt (S3),

where Rxy is the Hall resistance. In normal-metal/ferromagnet/oxide structure, the Rxy is

Rxy=RAHEcosθ+RPHEsin2θsin2φ (S4),

where RAHE (RPHE) is the anomalous Hall resistance (planar Hall resistance). The spin torque from ∆Isinωt induces the perturbation of magnetization in polar angle (∆θsinωt) and azimuthal angle (∆φsinωt). Therefore, the Rxy can be expanded as,

Rxy=Rxy,0+dRxydI∆Isinωt≈RAHEcosθ0-∆θsinωtsinθ0+RPHE(sin2θ0sin2φ0+∆θsinωtsin2θ0sin2φ0+2∆φsinωtsin2θ0cos2φ0) (S5).

When in-plane component of an external magnetic field (Bext) with polar angle θB and azimuthal angle φB is sufficiently larger than the demagnetization field Bdem (Bdem≪BextsinθB and φ0≈φB), the perturbation angles become [5]

∆θ=cosθ0∆BxcosφB+∆BysinφB-sinθ0∆BzBani-Bdemsin2φBcos2θ0+Bextcos(θB-θ0) (S6)

∆φ=-∆BxsinφB+∆BycosφB-Bdemsinθ0cos2φB+BextsinθB (S7).

By substituting the Eq.(S2) and Eqs. (S5-S7) into Eq.(S3), the Hall voltage and each harmonic Hall resistance (Rxy0ω, Rxy1ω, and Rxy2ω) can be rewritten as

Vxy=(12Rxy0ω+Rxy1ωsinωt-12Rxy2ωcos2ωt) ∆I (S8).

Rxy0ω=A+B (S9).

Rxy1ω=Rxy,0 (S10).

Rxy2ω=A+B  (S11).

A=-RAHEsinθ0+2RPHEsin2θ0sin2φH×-BFLTzsinθ0-BDLTycosφH+(BFLTy+BOe)cosθ0sinφBBani-Bdemsin2φBcos2θ0+Bextcos(θB-θ0)

B=2RPHEsin2θ0cos2φHBDLTycosθ0sinφB+(BFLTy+BOe)cosφB-BDLTzsinθ0-Bdemsinθ0cos2φB+BextsinθB

In particular, when applying an in-plane magnetic field (θB=π2) sufficient to make the magnetization direction aligned in the plane (θ0≈π2), BFLTy and BDLTz (BDLTy and BFLTz) only changes the azimuthal (polar) angle of magnetization, as shown in Fig. S2b. In such condition, the second harmonic Hall resistance Rxy2ω becomes

Rxy2ωφB=RAHEBDLTyBeff+R∇T2ωcosφB+2RPHEBFLTy+BOeBext2cos3φB-cosφB-2RPHEBDLTzBextcos2φB+RAHEBFLTzBeff (S12),

Where thermal contribution (R∇T2ω) to Rxy2ω is included. Equation (S12) is the same as Eq. (1) in the main text.

Figure S2. Effective fields due to y-SOT and z-SOT. a-b, The effective field directions acting on the arbitrary magnetization direction (a) and θ=π2 (b).

Supplementary Note 3. Hysteresis loops shift of anomalous Hall resistance

We measure the anomalous Hall resistance Rxy with a d.c. current Jd.c as a function of the out-of-plane magnetic field Bz. The Rxy vs. Bz hysteresis loop will shift when z-SOT is present [3,6]. Figures S3a shows the hysteresis loop in Pt/Co/AlOx/TiO2 structures (TiO2 sample) depending on the VG. When VG > 0 (VG,L = +8V, VG,R = -8V), the hysteresis loop shifts to the positive Bz direction for a positive Jd.c, while it is opposite for VG < 0. Figure S3b shows that the BS gradually increases with Jd.c without a threshold current. Here, BS is the amount of the hysteresis loop shift, defined BSId.c.= BC+Id.c.-BC-Id.c./2, where BC are positive and negative coercive fields. Figures S3c,d show the results of the ZrO2 sample, demonstrating the hysteresis shift direction of the ZrO2 sample is opposite to that of the TiO2 sample. This is consistent with the SOT switching and harmonic measurement results in the main text.

Figure S3. Hysteresis loop shift of Rxy in Pt/Co/AlOx/gate oxide structure a, Rxy versus Bz curves in the TiO2 sample for VG > 0 (VG,L = +8 V, VG,R = -8 V) (black line) and VG < 0 (VG,L = -8 V, VG,R = +8 V) (red dash line). b, BS versus Id.c. curves in the TiO2 sample for VG > 0 (black square) and VG < 0 (red circle). c, Rxy versus Bz curves in the ZrO2 sample for VG > 0 (VG,L = +10 V, VG,R = -10 V) (black line) and VG < 0 (VG,L = -10 V, VG,R = +10 V) (red dash line). d, BS versus Id.c. curves in the ZrO2 sample for VG > 0 (black square) and VG < 0 (red circle). The error bars indicate single-standard-deviation uncertainties.

Supplementary Note 4. Spin-orbit torque measurements in Pt/Co/AlOx/ZrO2 sample

We perform the in-plane harmonic Hall measurements [7] for a Pt/Co/AlOx/ZrO2 structure (ZrO2 sample). Figures S4a-c show the cosφ, 2cos3φ-cosφ, and cos2φ components of the Rxy2ω as a function of the Beff or Bext, which correspond to BDLTy, BFLTy and BDLTz, respectively. For the ZrO2 sample, the cos2φ component or BDLTz only appears when an asymmetric VG is applied, similar to the TiO2 sample (Fig. 3 of the main text). However, the sign of BDLTz in the ZrO2 sample is opposite to that of the TiO2 sample, which is consistent with field-free switching results shown in Fig. 3 of the main text. The estimated SOT-induced effective SOT fields according to the gate voltage conditions are summarized in Table S1.

Figure S4. Harmonic spin-orbit torque measurements in Pt/Co/AlOx/ZrO2. a, cosφ component of Rxy2ω versus 1/Beff. b, (2cos3φ-cosφ) component of Rxy2ω versus 1/Bext. c, cos2φ component of Rxy2ω versus 1/Bext.

Table S1. SOT effective fields depending on gate voltage conditions.

Supplementary Note 5. Voltage-controlled magnetic anisotropy (VCMA) effect

We investigate voltage-controlled magnetic anisotropy (VCMA) effect of the Pt (5 nm)/Co (1.4 nm)/AlOx (2 nm) structures with different gate oxides of TiO2 (40 nm) or ZrO2 (40 nm), in which FM Co is fully covered by a single gate. We measure the anomalous Hall resistance (Rxy) as a function of an in-plane magnetic field (Bx), allowing us to evaluate the perpendicular magnetic anisotropy field (HK) and its variation with gate voltage (VG) [8-10]. Figures S5a,b show that the HK decreases when applying a positive gate voltage (VG) for both samples regardless of the gate oxide. We further investigate the VCMA effect of the same samples that are used for the SOT switching measurements in the main text with four different gate conditions of VG(+,+), VG(-,-), VG(+,-), and VG(-,+). Figures S5c-5f show the changes in the coercivity HC and HK with VG, demonstrating that the HC and HK increase (decrease) when applying negative (positive) voltages to both left and right gate electrodes simultaneously: VG(-,-) (VG(+,+)). On the other hand, for the asymmetric voltages VG(+,-) and VG(-,+), the HC and HK exhibit intermediate values. Moreover, the VCMA effect exhibits the same sign for both samples regardless of the gate oxides.

Figure S5. Voltage-controlled magnetic anisotropy measurements. a-b, Normalized anomalous Hall resistance (Rxy) as a function of in-plane magnetic field (Bx) under VG = +8 V for the TiO2 sample (a) and VG = +10 V for ZrO2 samples (b) with a single gate. c-d, Normalized Rxy as a function of an out-of-plane magnetic field (Bz) under different gate voltages of VG(+,+), VG(-,-), VG(+,-), and VG(-,+) for the TiO2 sample (c) and ZrO2 sample (d). e-f, Normalized Rxy as a function of Bx under different gate voltages of VG(+,+), VG(-,-), VG(+,-), and VG(-,+) for the TiO2 sample (e) and ZrO2 sample (f).

Supplementary Note 6. Variation of damping-like spin-orbit torque with gate voltage

Figure S6 shows the cosφ component of Rxy2ω as a function of 1/Beff depending on VG in Pt (0.5 nm)/Co (2 nm)/AlOx (2 nm)/gate oxide (40 nm) samples, which corresponds to the change in BDLTy with VG. Unlike the BFLTy (Figs. 4c-d in the main text), the BDLTy and its gate voltage dependence is negligible for the samples regardless of the gate oxide material.

Figure S6. Gate voltage dependence of damping-like SOT. a-b, Damping-like SOT component of Rxy2ω depending on pre-biased gate voltage VG of 2.5 MV/cm for Pt(0.5 nm)/Co (2 nm)/AlOx (2 nm)/TiO2 (40 nm) (a) and Pt (0.5 nm)/Co (2 nm)/AlOx (2 nm)/ZrO2 (40 nm) (b) samples.

Supplementary Note 7. Reconfigurable logic operation using a single device

Figures 1 and 3 in the main text show the electrical control of spin-orbit torque switching polarity in a reversible and non-volatile manner. This allows us to demonstrate reconfigurable logic operations using a single device, where a gate voltage (VG,L or VG,R) and input current (IIN) are used as two input parameters (Fig. S7a). Figure S7b shows the device performance; the magnetization switching occurs at a current of 10 mA, and the switching polarity is reversed by changing the sign of VG. Based on the device, we construct a truth table, as shown in Figs. S7c,d, demonstrating that two logic operations are possible depending on the input parameters; first, the device operates the XOR function with input parameters of IIN and VG,L (Fig. S7c). Here, we define the positive values of the inputs (IIN = +15 mA, VG,L = +10 V) as digital input ‘1’, and their negative values (IIN = -15 mA, VG,L  = -10 V) as digital input ‘0’. They determine the digital output of the device, the magnetization direction; UP [DOWN] magnetization (Rxy > 0) [(Rxy < 0)] corresponds to digital output ‘1’ [‘0’]. Second, it operates the AND function with input parameters of IIN and VG,R when the device is initialized as the ‘0’ state (Fig. S7d). For a AND gate, we define the inputs of IIN = +15 mA, VG,L = +10 V as digital input ‘1’, and those of IIN = +5 mA, VG,L  = -10 V as digital input ‘0’. The different logic operations can be achieved by changing one input parameter, demonstrating a programmable logic operation in the SOT device with two side gates.

Figure S7. Reconfigurable logic operations of a single SOT device. a, Schematic of the device, in which gate voltage (VG,L or VG,R) and input current IIN are used as two input parameters. b, Current-induced switching of the device according to VG under +10 V of VG,L (VG > 0, red) or VG,R (VG < 0, green). c-d, Logic truth tables constructed using the results in Fig. S7b. XOR function (c) and AND function (d).

References

- Tan, H., Verbeeck, J., Abakumov, A. & Van Tendeloo, G. Oxidation state and chemical shift investigation in transition metal oxides by EELS. Ultramicroscopy 116, 24–33 (2012).

- Garello, K. et al. Symmetry and magnitude of spin-orbit torques in ferromagnetic heterostructures. Nat. Nanotechnol. 8, 587–593 (2013).

- Yu, G. et al. Switching of perpendicular magnetization by spin-orbit torques in the absence of external magnetic fields. Nat. Nanotechnol. 9, 548 (2014).

- Lee, D.-K. & Lee, K.-J. Spin-orbit torque switching of perpendicular magnetization in ferromagnetic trilayers. Sci. Rep. 10, 1772 (2020)

- Hayashi, M., Kim, J., Yamanouchi, M. & Ohno, H. Quantitative characterization of the spin-orbit torque using harmonic Hall voltage measurements. Phys. Rev. B 89, 144425 (2014).

- Baek, S. C. et al.Spin currents and spin-orbit torques in ferromagnetic trilayers. Nat. Mater. 17, 509–513 (2018).

- Avci, C. O. et al. Interplay of spin-orbit torque and thermoelectric effects in ferromagnet/normal-metal bilayers. Phys. Rev. B 90, 224427 (2014).

- Maruyama, T. et al. Large voltage-induced magnetic anisotropy change in a few atomic layers of iron. Nat. Nanotechnol. 4, 158–161 (2009).

- Bauer, U. et al. Magneto-ionic control of interfacial magnetism. Nat. Mater. 14, 174–181 (2015).

- Park, K. W. et al. Electric field control of magnetic anisotropy in the easy cone state of Ta/Pt/CoFeB/MgO structures. Appl. Phys. Lett. 109, 012405 (2016).