Table 1. Pore formation methods in/on nanofibers [1].

| Method explanation | Porosity formation method |
| --- | --- |
| jet partially fast freezing by fast evaporating of very volatile solvent or collecting nanofibers in the liquid bath | Phase separation between polymer and solvent |
| Vapor phase separation (usually, with electrospinning in high humidity, the water molecules in the air works as nonsolvent) and liquid phase separation | Phase separation between polymer and nonsolvent |
| Jet with triple-phase separation due to difference between volatility of solvent and nonsolvent (by changing ratios of this system) and pores form by changing relative rates of solvent/nonsolvent, controlling phase separation dynamic | Phase separation of the liquid section in polymer, nonsolvent, and solvent system |
| Phase separation between polymer and nonsolvent due to residual solvent in nanofiber by receiving nanofibers to nonsolvent bath and pore formation due to miscibility between solvent and nonsolvent | Collecting the nanofibers in a nonsolvent bath |
| Washing small molecules (like salt), block copolymers, polymers from nanofibers, or calcinating (the best way because pores formation by solvent evaporating is time-consuming and sometimes is impossible to remove one phase) | Selective removal of one phase of nanofiber |
| Controlling porosity by adjusting the ratio of two phases in nanofibers | Thermal degradation of one phase |

Table 2 shows the average diameters of the nano webs.

| Sample code | FESEM image | Higher resolution |
| --- | --- | --- |
| PA/PVA |  |  |
| PA/noPVA |  |  |
| PA and PA/no PVA |  |  |

Table 3. Porosity and pore size of the nano webs.

| Sample code | Porosity from BET (m2/g) | Average pore size from BET (nm) | Diameter (nm) |
| --- | --- | --- | --- |
| PA6/PVA | 2.358 | 17.22 | 317.4±103.4 |
| PA6/no PVA | 0.933 | 17.29 | 346.5±103 |

Table 4. Showing adsorption, and deadsorption curves.

| Sample code | Adsorption and deadsorption curve |
| --- | --- |
| PA/PVA |  |
| PA/no PVA |  |

Table5. Surface roughness and pore volume measurements.

| sample | Surface roughness curve | Pore volume distribution |
| --- | --- | --- |
| PA/PVA |  |  |
| PA/noPVA |  |  |

Table 6. Orientation measurements.

| sample | Radon curve | Orientation (degree) |
| --- | --- | --- |
| PA/PVA |  | 88 |
| PA/no PVA |  | 89 |