Supplementary Materials

Anticonvulsant Activity, Molecular Modeling and Synthesis of Spirooxindole-4H-Pyran Derivatives using a Novel Reusable Organocatalyst

Leila Emami1, Leila Moezi2, Leila Amiri-Zirtol1, Fatemeh Pirsalami2, Masoumeh Divar1, Aida Solhjoo3, Soghra Khabnadideh1

1Pharmaceutical Sciences, Research Center, Shiraz University of Medical Sciences, Shiraz, Iran.

2Department of Pharmacology, School of Medicine, Shiraz University of Medical Sciences, Shiraz, Iran.

3Faculty of Pharmacy, Shiraz University of Medical Sciences, Shiraz, I.R.Iran.

Instrumentation

Melting points were measured by a Buchi melting point B-540 B.V.CHI apparatus and are uncorrected. Fourier transform infrared (FT-IR) spectra were run on a Bruker Equinox by KBr pills in the 400-4000 cm-1 region. Raman spectroscopy was recorded from 500 to 3500 cm−1 on an Almega Thermo Nicolet Dispersive Raman Spectrometer using a Nd:YLF laser source operating at wavelength of 532 nm. X-ray diffraction (XRD) patterns were recorded on a Philips X-pert diffractometer equipped with a Cu-Ka radiation (λ = 1.54 A°) in the 2θ range from 5 to 80. Field emission scanning electron microscopy (FE-SEM) image was recorded using FE-SEM MIRA 3-XMU with a high-energy beam of electrons. The magnetic measurement was carried out using a vibrating sample magnetometer model VSM-4 inh. Energy-dispersive X-ray spectroscopy (EDS) analysis was performed using Zeiss SIGMA VP-500.

FESEM images of GO (a) and GO-A.P (b) with different magnifications.

EDS mapping analysis distribution of O (a), N (b), C (c) and GO-A.P. (d).

Thermal gravimetric analysis curves of GO (a) and GO-A.P. (b).

Corresponding author: Tel.: +98-71-32424127-8; Fax: +98-71-32424126; E-mail: khabns@sums.ac.ir