Table 4 Images of fibers under OM

| Flax and hemp fibers, 100x, sample 3D | Blue cotton fiber, 100x, sample 3D | Blue silk fiber, 100x, sample 10D | Herzberg Stain Test, flax and hemp fiber, 100x, sample 3D |
| --- | --- | --- | --- |

Table 5 SEM-EDS images and spectra of historical papers

| Sample mark | SEM | EDS | Found items (trace elements) |
| --- | --- | --- | --- |
| 1D |  |  | C, O, Ca, (Si, Al, Ni) |
| 2D |  |  | O, C, Ca, (Cu, Al, Si, Ni) |
| 3D |  |  | O, C, (Cu, Si, Al, Ni) |
| 4D |  |  | O, C, (Si, Cu, Al, Ni, Au, S, Ag) |
| 5D |  |  | O, C, Ca, (Al, Si, Cu, Ni) |
| 6D |  |  | O, C, Ca, (Cu, Si, Ni) |
| 7D |  |  | O, C, Ca, (Ni, Cu Mg, Si, K) |
| 8D |  |  | O, C, Ca, (Cu, Si, Ni, Mg, Al, Si) |
| 9D |  |  | O, C, (Si, Mg, Al, Cu, Ni) Ag? |
| 10D |  |  | O, C, Ca, (Si, Mg, Al, Cu, Ni) |

Table 6 XRF spectra of historical papers

| Sample mark | XRF | Found items (trace elements) |
| --- | --- | --- |
| 1D |  | Ca (Si, Mn, Fe, S) |
| 2D |  | Ca, Fe (K, Si, S) |
| 3D |  | Ca, Fe, (K, Al, Si, S, Mn) |
| 4D |  | Ca, (Fe, K, S, Al, Si, Mn, Cu?) |
| 5D |  | Ca (K, Si, Mn, Fe) |
| 6D |  | Ca (K, Si, Mn, Fe, S) |
| 7D |  | Ca (K, Si, Mn, Fe, S) |
| 8D |  | Ca (Fe, Cu, Si, S, K) |
| 9D |  | Ca, Fe (Si, S, K, Mn, Ti) |
| 10D |  | Ca, Fe (K, S, Mn, Si) |