Table S1 The solubility of melanin

| Solvent | Dissolved volume /g | Color | Solubility |
| --- | --- | --- | --- |
| Distilled water | 0.1204 | Colorless transparent | insoluble |
| HCl | 0.0012 | Colorless transparent | insoluble |
| Dilute sulfuric acid | 0.0015 | Colorless transparent | insoluble |
| NaOH | 21.3486 | Dark brown | Soluble |
| Ammonia | 16.7217 | Dark brown | insoluble |
| Ethanol | 0.0047 | Colorless transparent | insoluble |
| Methanol | 0.2521 | Light Brown | slightly soluble |
| Ethyl acetate | 0.0037 | Colorless transparent | insoluble |
| Dichloromethane | 0.0318 | Colorless transparent | insoluble |
| DMSO | 0.3156 | Light Brown | slightly soluble |
| Acetone | 0.0612 | Colorless transparent | insoluble |
| Petroleum ether | 0.0014 | Colorless transparent | insoluble |

Table S2 Effects of PH value on the stability of the melanin

| pH | Absorbance value | Color | Sedimentation |
| --- | --- | --- | --- |
| 3 | 0.078±0.035 | Light brown | ** |
| 5 | 0.098±0.049 | Light brown | * |
| 7 | 0.325±0.024 | brownish red | - |
| 9.16 | 0.913±0.074 | dark brown | - |
| 10.83 | 0.908±0.067 | dark brown | - |

Note: "*" indicates the degree of precipitation of the pigment solution; "-" indicates that no precipitation is produced in the pigment solution.

Table S3 The effect of light on the stability of melanin

| Natural Light （d） |  |  |  |  |  |  |  | Ultraviolet light （min） |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 | 1 | 2 | 3 | 4 | 0 | 30 |  | 60 |
| A | 0.851± | 0.858± | 0.873± | 0.882± | 0.885± | 0.849± | 0.863± |  | 0.870± |
|  | 0.006* | 0.013* | 0.009** | 0.027 | 0.015 | 0.031 | 0.009* |  | 0.028** |

Note: * Differences are significant (P < 0.05); ** Differences are highly significant (P < 0.01).

Table S4 The effect of microwave on the stability of melanin

| Microwave（min） | 0 | 5 | 10 | 15 | 20 | 25 | 30 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A | 0.957±0.013* | 0.974±0.017 | 0.956±0.024 | 0.942±0.027 | 0.947±0.021 | 0.951±0.018* | 0.953±0.025* |

Note: * Differences were significant (P < 0.05).

Table S5 The effect of H2O2 on the stability of melanin

| H2O2（mL） | 0 | 2 | 4 | 6 | 8 | 10 |
| --- | --- | --- | --- | --- | --- | --- |
| 1 h | 0.872±0.006** | 0.897±0.023* | 0.876±0.056 | 0.885±0.019** | 0.878±0.008* | 0.892±0.027* |
| 2 h | 0.872±0.006** | 0.836±0.043 | 0.841±0.032* | 0.843±0.041* | 0.836±0.027* | 0.825±0.006** |

Note: * Differences are significant (P < 0.05); ** Differences are highly significant (P < 0.01).

Table S6 The effect of Na2SO3 on the stability of melanin

| Na2SO3（mL） | 0 | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- | --- |
| 1 h | 0.835±0.024* | 0.712±0.015* | 0.503±0.101* | 0.472±0.027** | 0.458±0.004** |
| 2 h | 0.835±0.024 | 0.432±0.038* | 0.311±0.047* | 0.152±0.039* | 0.081±0.028** |

Note: * Differences are significant (P < 0.05); ** Differences are highly significant (P < 0.01).

Table S7 The effect of Vc on the stability of melanin

| Vc（mL） | 0 | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- | --- |
| 1h | 0.887±0.013* | 0.845±0.034* | 0.836±0.043 | 0.845±0.023* | 0.835±0.013** |
| 2h | 0.885±0.035* | 0.856±0.042 | 0.872±0.027* | 0.816±0.037 | 0.826±0.015** |
| 4h | 0.882±0.015** | 0.828±0.034* | 0.838±0.035** | 0.824±0.019** | 0.834±0.027* |

Note: * Differences are significant (P < 0.05); ** Differences are highly significant (P < 0.01).

Table S8 The effect of sodium benzoate on the stability of melanin

| Sodium benzoate（mol/L） | 0 | 0.001 | 0.002 | 0.003 | 0.004 |
| --- | --- | --- | --- | --- | --- |
| 1h | 0.889±0.013** | 0.793±0.034* | 0.816±0.023 | 0.806±0.023* | 0.828±0.041* |
| 2h | 0.887±0.016** | 0.824±0.016** | 0.858±0.017* | 0.848±0.026* | 0.814±0.024* |
| 4h | 0.882±0.023* | 0.856±0.018* | 0.727±0.014** | 0.818±0.031* | 0.836±0.017* |

Note: * Differences are significant (P < 0.05); ** Differences are highly significant (P < 0.01).

Table S9 Tentative identification of the melanin compositions from L-25-2

| Serial number | [M-H]- (m/z) | Possible attribution | Quasi-ionic peak time(min) |
| --- | --- | --- | --- |
| 5 | 311.1961 | C14H23N4O4（Ke，2006） | 22.400 |
| 6 | 325.2134 | C20H25N2O2 （Ke，2006） | 22.842 |
| 7 | 339.2302 | C17H27N2O5 （Ke，2006） | 23.215 |
| 1 | 677.5656 | C17H27N2O5, C8H9NO2, C9H5NO4（Xu，2006） | 13.188 |
| 2 | 790.6635 | 677.5656+113.0973 | 14.151 |
| 3 | 903.7575 | 790.6635+113.0940 | 14.897 |
| 4 | 1016.8587 | 903.7575+113.1012 | 15.511 |