Supplementary information

Time-Resolved Detection of Multilevel Switching of the Magnetization and Exchange Bias Driven by Spin-Orbit Torques

Yuyan Wang1,2*, Takuya Taniguchi2, Po-Hung Lin3, Daniel Zicchino2, Andreas Nickl2, Jan Sahliger2, Chih-Huang Lai3, Cheng Song4, Huaqiang Wu1,5, Qionghai Dai1, Christian Back2*

1Beijing National Research Center for Information Science and Technology, Tsinghua University, Beijing, China. 2Department of Physics, Technical University of Munich, Garching b. Munich, Germany. 3Department of Materials Science and Engineering, National Tsing Hua University, Hsinchu, Taiwan. 4School of Materials Science and Engineering, Tsinghua University, Beijing, China. 5School of Integrated Circuits, Tsinghua University, Beijing, China.

Email: wangyuyan@tsinghua.edu.cn; christian.back@tum.de

Supplementary Note 1: Magnetic properties of the thin film samples

Fig. S1. Normalized M-H loops along the (a) out-of-plane direction, (b) in-plane direction obtained using vibrating sample magnetometer (VSM). The in-plane M-H loops are measured with the externally applied magnetic field along the in-plane direction of the annealing field (black squares), and opposite to the annealing field (red circles), respectively.

Supplementary Note 2: Time-resolved SOT switching

Fig. S2 Reversal of the magnetization mz for opposite directions of the in-plane magnetic field Bx = +100 mT and –100 mT as a function of delay time. The magnetization of Co switches between upward and downward orientation when the direction of the external magnetic field Bx is reversed.

Fig. S3 Time-resolved magnetization switching for negative current pulses and different in-plane magnetic fields Bx larger than 100 mT. Full switching of the magnetization is achieved at Bx = 100 mT, as discussed in Fig. 2a in the main text. When Bx exceeds the critical field of 100 mT, the polar Kerr signal decreases dramatically due to the tilt of the magnetization towards the in-plane magnetic field Bx, together with a notable increase of the switching speed.

Fig. S4 Time-resolved magnetization switching at Bx = 50 mT and current pulse length 𝛕P ranging from 0.4 ns to 1.3 ns.

Supplementary Note 3: Quasistatic SOT switching

Fig. S5 Summarized Kerr intensity (normalized) for quasistatic current induced magnetization reversal for different external magnetic fields Bx.

Supplementary Note 4: Micromagnetic simulations

Fig. S6 Schematic illustration of the system used in the simulation. The blue and red arrows indicate the magnetization of each layer. The detailed parameters are described in the part of Methods of the main text.

Fig. S7 Micromagnetic simulations of the time-resolved SOT switching process on a timescale of 15 ns. Magnetization switching for different current densities (a) when the external field is absent, and (b) with in-plane field Bx of 100 mT. The switching of the magnetization stabilizes after 6 ns and is non-volatile, being is faster for larger Bx.

Fig. S8 Micromagnetic simulations of the out-of-plane M-H loops before and after SOT switching at Bx = 0 mT and Bx = –20 mT, which indicates the reversal of exchange bias. Larger in-plane field of –20 mT results in a more shift of exchange bias field (26 mT) than that of zero in-plane field (17 mT).