|  |  | Table 1. Composition of the tested calcium silicate cements. Data from manufacturer technical information and product inserts. |  |
| --- | --- | --- | --- |

| Material | Major Components | Radiopacifier / Additives | Key Characteristics |
| --- | --- | --- | --- |
| NeoMTA®2 | Tricalcium silicate, dicalcium silicate | Tantalum oxide | Powder mixed with proprietary gel; designed to avoid discoloration and support bioactivity |
| ProRoot® MTA | Tricalcium silicate, dicalcium silicate, calcium aluminate | Bismuth oxide | Classic MTA formulation; hydrophilic powder that sets in presence of moisture |
| TotalFill® BC RRM™ Putty | Tricalcium silicate, dicalcium silicate, calcium phosphate, calcium hydroxide | Zirconium oxide, tantalum oxide | Premixed bioceramic putty; moisture-activated setting |

Table 1A. Estimated difference in median MTT values (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| ProRoot MTA vs CONTROL |  |  |  |
| 24 hours | 0.03 | (-0.20, 0.26) | >0.999 |
| 48 hours | -0.04 | (-0.27, 0.19) | >0.999 |
| 72 hours | 0.02 | (-0.21, 0.25) | >0.999 |
| TotalFill vs CONTROL |  |  |  |
| 24 hours | 0.05 | (-0.18, 0.29) | >0.999 |
| 48 hours | -0.02 | (-0.25, 0.22) | >0.999 |
| 72 hours | 0.28 | (0.05, 0.51) | 0.009 |
| Neo MTA vs CONTROL |  |  |  |
| 24 hours | 0.00 | (-0.23, 0.23) | >0.999 |
| 48 hours | -0.16 | (-0.40, 0.07) | 0.413 |
| 72 hours | 0.07 | (-0.16, 0.31) | >0.999 |
| TotalFill vs ProRoot MTA |  |  |  |
| 24 hours | 0.02 | (-0.21, 0.26) | >0.999 |
| 48 hours | 0.02 | (-0.21, 0.26) | >0.999 |
| 72 hours | 0.26 | (0.03, 0.50) | 0.017 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 24 hours | -0.03 | (-0.26, 0.20) | >0.999 |
| 48 hours | -0.12 | (-0.36, 0.11) | >0.999 |
| 72 hours | 0.06 | (-0.18, 0.29) | >0.999 |
| Neo MTA vs TotalFill |  |  |  |
| 24 hours | -0.06 | (-0.29, 0.18) | >0.999 |
| 48 hours | -0.15 | (-0.38, 0.08) | 0.635 |
| 72 hours | -0.21 | (-0.44, 0.03) | 0.119 |

* Bonferroni corrected

Table 1B. Estimated difference in median MTT (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 48 hours vs 24 hours |  |  |  |
| CONTROL | 0.29 | (0.06, 0.52) | 0.006 |
| ProRoot MTA | 0.22 | (-0.01, 0.45) | 0.069 |
| TotalFill | 0.22 | (-0.01, 0.45) | 0.072 |
| Neo MTA | 0.13 | (-0.10, 0.35) | 0.975 |
| 72 hours vs 24 hours |  |  |  |
| CONTROL | 0.64 | (0.41, 0.87) | <0.001 |
| ProRoot MTA | 0.63 | (0.40, 0.86) | <0.001 |
| TotalFill | 0.87 | (0.64, 1.09) | <0.001 |
| Neo MTA | 0.72 | (0.49, 0.94) | <0.001 |
| 72 hours vs 48 hours |  |  |  |
| CONTROL | 0.35 | (0.12, 0.58) | 0.001 |
| ProRoot MTA | 0.41 | (0.18, 0.64) | <0.001 |
| TotalFill | 0.65 | (0.42, 0.88) | <0.001 |
| Neo MTA | 0.59 | (0.36, 0.82) | <0.001 |

* Bonferroni corrected

Table 2A. Estimated difference in median ALP (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| TotalFill vs ProRoot MTA |  |  |  |
| 3 days | 0.28 | (-0.38, 0.94) | >0.999 |
| 5 days | 0.61 | (-0.05, 1.26) | 0.090 |
| 7 days | 0.02 | (-0.64, 0.68) | >0.999 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 3 days | 0.90 | (0.24, 1.56) | 0.003 |
| 5 days | -0.12 | (-0.78, 0.54) | >0.999 |
| 7 days | 0.91 | (0.25, 1.56) | 0.002 |
| Neo MTA vs TotalFill |  |  |  |
| 3 days | 0.62 | (-0.04, 1.28) | 0.078 |
| 5 days | -0.72 | (-1.38, -0.07) | 0.023 |
| 7 days | 0.88 | (0.23, 1.54) | 0.003 |

* Bonferroni corrected

Table 2B. Estimated difference in median ALP (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 5 days vs 3 days |  |  |  |
| ProRoot MTA | 0.51 | (-0.15, 1.17) | 0.230 |
| TotalFill | 0.84 | (0.18, 1.50) | 0.005 |
| Neo MTA | -0.50 | (-1.16, 0.16) | 0.252 |
| 7 days vs 3 days |  |  |  |
| ProRoot MTA | -0.24 | (-0.90, 0.42) | >0.999 |
| TotalFill | -0.49 | (-1.15, 0.17) | 0.276 |
| Neo MTA | -0.23 | (-0.89, 0.43) | >0.999 |
| 7 days vs 5 days |  |  |  |
| ProRoot MTA | -0.75 | (-1.41, -0.09) | 0.017 |
| TotalFill | -1.33 | (-1.99, -0.67) | <0.001 |
| Neo MTA | 0.28 | (-0.38, 0.93) | >0.999 |

* Bonferroni corrected

Table 3A. Estimated difference in median OCN (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| TotalFill vs ProRoot MTA |  |  |  |
| 3 days | -0.01 | (-0.78, 0.77) | >0.999 |
| 5 days | -0.01 | (-0.79, 0.77) | >0.999 |
| 7 days | -0.21 | (-0.99, 0.57) | >0.999 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 3 days | -0.38 | (-1.16, 0.39) | >0.999 |
| 5 days | 0.23 | (-0.55, 1.01) | >0.999 |
| 7 days | 1.22 | (0.44, 1.99) | <0.001 |
| Neo MTA vs TotalFill |  |  |  |
| 3 days | -0.38 | (-1.16, 0.40) | >0.999 |
| 5 days | 0.23 | (-0.55, 1.01) | >0.999 |
| 7 days | 1.43 | (0.65, 2.21) | <0.001 |

* Bonferroni corrected

Table 3B. Estimated difference in median OCN (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 5 days vs 3 days |  |  |  |
| ProRoot MTA | 0.11 | (-0.67, 0.89) | >0.999 |
| TotalFill | 0.11 | (-0.67, 0.89) | >0.999 |
| Neo MTA | 0.72 | (-0.05, 1.50) | 0.083 |
| 7 days vs 3 days |  |  |  |
| ProRoot MTA | -1.20 | (-1.98, -0.42) | 0.001 |
| TotalFill | -1.40 | (-2.18, -0.62) | <0.001 |
| Neo MTA | 0.40 | (-0.38, 1.18) | 0.992 |
| 7 days vs 5 days |  |  |  |
| ProRoot MTA | -1.31 | (-2.09, -0.53) | <0.001 |
| TotalFill | -1.51 | (-2.29, -0.74) | <0.001 |
| Neo MTA | -0.32 | (-1.10, 0.46) | >0.999 |

* Bonferroni corrected

Table 4A. Estimated difference in median COL1A1 (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| TotalFill vs ProRoot MTA |  |  |  |
| 3 days | -0.19 | (-1.46, 1.07) | >0.999 |
| 5 days | -0.60 | (-1.86, 0.66) | >0.999 |
| 7 days | 0.07 | (-1.19, 1.33) | >0.999 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 3 days | 0.16 | (-1.10, 1.42) | >0.999 |
| 5 days | -1.16 | (-2.42, 0.10) | 0.090 |
| 7 days | 0.21 | (-1.05, 1.47) | >0.999 |
| Neo MTA vs TotalFill |  |  |  |
| 3 days | 0.36 | (-0.90, 1.62) | >0.999 |
| 5 days | -0.56 | (-1.82, 0.70) | >0.999 |
| 7 days | 0.14 | (-1.12, 1.40) | >0.999 |

* Bonferroni corrected

Table 4B. Estimated difference in median COL1A1 (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 5 days vs 3 days |  |  |  |
| ProRoot MTA | 0.29 | (-0.97, 1.55) | >0.999 |
| TotalFill | -0.11 | (-1.37, 1.15) | >0.999 |
| Neo MTA | -1.03 | (-2.29, 0.23) | 0.179 |
| 7 days vs 3 days |  |  |  |
| ProRoot MTA | -1.85 | (-3.11, -0.58) | 0.001 |
| TotalFill | -1.58 | (-2.84, -0.32) | 0.007 |
| Neo MTA | -1.80 | (-3.06, -0.54) | 0.001 |
| 7 days vs 5 days |  |  |  |
| ProRoot MTA | -2.14 | (-3.40, -0.88) | <0.001 |
| TotalFill | -1.47 | (-2.73, -0.21) | 0.014 |
| Neo MTA | -0.77 | (-2.03, 0.49) | 0.612 |

* Bonferroni corrected

Table 5A. Estimated difference in median DMP1 (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| TotalFill vs ProRoot MTA |  |  |  |
| 3 days | 0.57 | (-0.13, 1.28) | 0.183 |
| 5 days | 0.00 | (-0.69, 0.68) | >0.999 |
| 7 days | 0.07 | (-0.62, 0.75) | >0.999 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 3 days | 0.48 | (-0.20, 1.16) | 0.362 |
| 5 days | 0.21 | (-0.47, 0.89) | >0.999 |
| 7 days | 0.43 | (-0.25, 1.11) | 0.548 |
| Neo MTA vs TotalFill |  |  |  |
| 3 days | -0.09 | (-0.80, 0.61) | >0.999 |
| 5 days | 0.22 | (-0.47, 0.90) | >0.999 |
| 7 days | 0.36 | (-0.32, 1.05) | 0.913 |

* Bonferroni corrected

Table 5B. Estimated difference in median DMP1 (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 5 days vs 3 days |  |  |  |
| ProRoot MTA | 0.27 | (-0.41, 0.96) | >0.999 |
| TotalFill | -0.30 | (-1.01, 0.40) | >0.999 |
| Neo MTA | 0.01 | (-0.68, 0.69) | >0.999 |
| 7 days vs 3 days |  |  |  |
| ProRoot MTA | -0.60 | (-1.28, 0.09) | 0.123 |
| TotalFill | -1.10 | (-1.80, -0.40) | <0.001 |
| Neo MTA | -0.65 | (-1.33, 0.04) | 0.074 |
| 7 days vs 5 days |  |  |  |
| ProRoot MTA | -0.87 | (-1.55, -0.19) | 0.005 |
| TotalFill | -0.80 | (-1.48, -0.12) | 0.013 |
| Neo MTA | -0.65 | (-1.33, 0.03) | 0.070 |

* Bonferroni corrected

Table 6A. Estimated difference in median NESTIN (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| TotalFill vs ProRoot MTA |  |  |  |
| 3 days | -0.11 | (-1.21, 0.99) | >0.999 |
| 5 days | -0.14 | (-1.24, 0.96) | >0.999 |
| 7 days | 0.16 | (-0.94, 1.26) | >0.999 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 3 days | 0.12 | (-0.98, 1.22) | >0.999 |
| 5 days | 0.34 | (-0.77, 1.44) | >0.999 |
| 7 days | 0.57 | (-0.53, 1.68) | 0.973 |
| Neo MTA vs TotalFill |  |  |  |
| 3 days | 0.23 | (-0.87, 1.33) | >0.999 |
| 5 days | 0.47 | (-0.63, 1.58) | >0.999 |
| 7 days | 0.41 | (-0.69, 1.52) | >0.999 |

* Bonferroni corrected

Table 6B. Estimated difference in median NESTIN (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 5 days vs 3 days |  |  |  |
| ProRoot MTA | -0.05 | (-1.15, 1.06) | >0.999 |
| TotalFill | -0.07 | (-1.18, 1.03) | >0.999 |
| Neo MTA | 0.17 | (-0.93, 1.27) | >0.999 |
| 7 days vs 3 days |  |  |  |
| ProRoot MTA | -0.63 | (-1.74, 0.47) | 0.740 |
| TotalFill | -0.36 | (-1.47, 0.74) | >0.999 |
| Neo MTA | -0.18 | (-1.28, 0.92) | >0.999 |
| 7 days vs 5 days |  |  |  |
| ProRoot MTA | -0.59 | (-1.69, 0.52) | 0.915 |
| TotalFill | -0.29 | (-1.39, 0.81) | >0.999 |
| Neo MTA | -0.35 | (-1.45, 0.75) | >0.999 |

* Bonferroni corrected

Table 7A. Estimated difference in median DSPP (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| TotalFill vs ProRoot MTA |  |  |  |
| 3 days | -0.39 | (-1.51, 0.74) | >0.999 |
| 5 days | -0.07 | (-1.23, 1.09) | >0.999 |
| 7 days | 0.27 | (-0.86, 1.39) | >0.999 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 3 days | -0.16 | (-1.25, 0.93) | >0.999 |
| 5 days | 0.60 | (-0.56, 1.76) | 0.995 |
| 7 days | 0.34 | (-0.75, 1.43) | >0.999 |
| Neo MTA vs TotalFill |  |  |  |
| 3 days | 0.23 | (-0.90, 1.35) | >0.999 |
| 5 days | 0.67 | (-0.49, 1.83) | 0.728 |
| 7 days | 0.07 | (-1.05, 1.20) | >0.999 |

* Bonferroni corrected

Table 7B. Estimated difference in median DSPP (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 5 days vs 3 days |  |  |  |
| ProRoot MTA | 0.15 | (-0.97, 1.28) | >0.999 |
| TotalFill | 0.47 | (-0.69, 1.63) | >0.999 |
| Neo MTA | 0.91 | (-0.21, 2.04) | 0.185 |
| 7 days vs 3 days |  |  |  |
| ProRoot MTA | -1.43 | (-2.52, -0.33) | 0.004 |
| TotalFill | -0.77 | (-1.93, 0.39) | 0.450 |
| Neo MTA | -0.93 | (-2.02, 0.17) | 0.146 |
| 7 days vs 5 days |  |  |  |
| ProRoot MTA | -1.58 | (-2.71, -0.45) | 0.002 |
| TotalFill | -1.24 | (-2.40, -0.08) | 0.029 |
| Neo MTA | -1.84 | (-2.97, -0.71) | <0.001 |

* Bonferroni corrected

Table 8A. Estimated difference in median RUNX2 (95% Confidence Interval) by material at each time of measurement.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| TotalFill vs ProRoot MTA |  |  |  |
| 3 days | 0.11 | (-0.74, 0.95) | >0.999 |
| 5 days | -0.10 | (-0.94, 0.75) | >0.999 |
| 7 days | -0.20 | (-1.05, 0.64) | >0.999 |
| Neo MTA vs ProRoot MTA |  |  |  |
| 3 days | 0.18 | (-0.67, 1.02) | >0.999 |
| 5 days | 0.18 | (-0.67, 1.02) | >0.999 |
| 7 days | 0.25 | (-0.59, 1.10) | >0.999 |
| Neo MTA vs TotalFill |  |  |  |
| 3 days | 0.07 | (-0.78, 0.92) | >0.999 |
| 5 days | 0.27 | (-0.57, 1.12) | >0.999 |
| 7 days | 0.46 | (-0.39, 1.30) | 0.884 |

* Bonferroni corrected

Table 8B. Estimated difference in median RUNX2 (95% Confidence Interval) by time of measurement for each material.

|  | Estimated difference | 95% Conf. Interval* | p-value* |
| --- | --- | --- | --- |
| 5 days vs 3 days |  |  |  |
| ProRoot MTA | 0.01 | (-0.83, 0.86) | >0.999 |
| TotalFill | -0.19 | (-1.04, 0.65) | >0.999 |
| Neo MTA | 0.01 | (-0.83, 0.86) | >0.999 |
| 7 days vs 3 days |  |  |  |
| ProRoot MTA | -0.86 | (-1.70, -0.01) | 0.046 |
| TotalFill | -1.17 | (-2.01, -0.32) | 0.002 |
| Neo MTA | -0.78 | (-1.62, 0.07) | 0.089 |
| 7 days vs 5 days |  |  |  |
| ProRoot MTA | -0.87 | (-1.71, -0.02) | 0.042 |
| TotalFill | -0.97 | (-1.82, -0.13) | 0.015 |
| Neo MTA | -0.79 | (-1.64, 0.05) | 0.080 |

* Bonferroni corrected