Supplementary Information

Data and Source Code Package

Please go to https://github.com/AET-MetallicGlass/Supplementary-Data-Codes and download the package by clicking “Code”. The package contains 9 folders. The procedure on how to test the MATLAB data and source codes is explained below and more details are provided in the README file of the package.

1. Measured_data, which includes 55 experimental projections after denoising and alignment as well as their corresponding angles.

2. RESIRE_package. Run the sample code Main_RESIRE_sample.m in the folder to get the 3D reconstruction of a smaller test object. Run the main code Main_RESIRE_MG.m to obtain the 3D reconstruction of the metallic glass sample.

3. Final_reconstruction_volume, which contains the 3D volume of the metallic glass sample reconstructed from Main_RESIRE_MG.m.

4. Tracing_and_classification. Run the code Main_polynomial_tracing.m to trace the initial atomic positions from the reconstructed 3D volume. After the manual checking of the 3D atomic positions, run the code Main_classification.m to classify the eight elements in the sample into three different types: Co and Ni as type 1, Ru, Rh, Pd and Ag as type 2, and Ir and Pt as type 3.

5. Position_refinement. Run the code Main_position_refinement.m to refine the 3D atomic coordinates in the metallic glass sample.

6. Final_coordinates. The final 3D atomic model and chemical species (i.e. type 1, 2 and 3) of the metallic glass sample.

7. Data_analysis_sro. Run the code Main_1_rdf_and_boo_calculation_all_atoms.m to calculate the radial distribution function and the bond orientation order parameters for all the atoms in the metallic glass sample; Run the code Main_2_rdf_calculation_amorphous_region.m to compute the radial distribution function and pair distribution functions for all the amorphous atoms in the sample; Run the code Main_3_voronoi_calculation_amorphous_region.m to determine the Voronoi indices for all the atoms in the sample.

8. Data_analysis_mro. Run the code Main_1_potential_mro.m to identify the possible MROs based on the breadth first search algorithm; Run the code Main_2_final_mro.m to determine the final MROs in the metallic glass sample.

9. Supplementary Figures. This file contains four Supplementary Figures.

Supplementary Videos

Supplementary Video 1. Temperature measurement of the carbothermal shock process by a high-speed Phantom Miro M110 camera. The movie shows the colormap of the temperature distribution with an interval of 55 ms and a pixel size of 25 m, where the inhomogeneity is due to the difference of the local heat transfer.

Supplementary Video 2. Progressive slices of the 3D reconstruction of the multi-component metallic glass nanoparticle, showing the disordered nature of the nanoparticle and that the majority of type 3 atoms (red blobs) are distributed in the second coordination shell. Each slice corresponds to 0.347 Å thick.

Supplementary Video 3. Experimental 3D atomic model of the multi-component metallic glass nanoparticle with type 1, 2 and 3 atoms in green, blue and red, respectively, which exhibits disordered atomic structure. Compared with type 1 and 2 atoms, type 3 atoms are more uniformly distributed in the 9-nm-diameter nanoparticle.

Supplementary Video 4. 3D distribution of the four types of the MROs in the multi-component metallic glass nanoparticle, where fcc-, hcp-, bcc- and sc-like MROs are in blue, red, green and purple, respectively. To better visualize the networks, only those with eight solute centre atoms or more are shown.