Supplementary Information

In situ wide-field visualization of palladium hydrogenation

Xiaoyi She1,3,5, Huifeng Du2,5, Yang Shen1, Rihui Xin4, Nicholas X. Fang2* & Chongjun Jin1*

1State Key Laboratory of Optoelectronic Materials and Technologies, School of Materials Science and Engineering, Sun Yat-sen University, Guangzhou, China. 2 Department of Mechanical Engineering, Massachusetts Institute of Technology, Cambridge, MA, USA. 3School of Electronics and Information Technology, Sun Yat-sen University, Guangzhou, China. 4China Securities Depository and Clearing Corporation Limited, Beijing, China. 5These authors contributed equally: Xiaoyi She, Huifeng Du. *e-mail: jinchjun@mail.sysu.edu.cn; nicfang@mit.edu

Supplementary Figure 1 Cycle performance of the GPDP. The relationship between the response time of the GPDP and hydrogen treatment cycles. The detect area is with a distance of 100 μm to the edge. The concentration and flow rate of H2 are 4% and 1000 sccm, respectively.

Supplementary Figure 2 Surface deformation of the Pd film on PDMS during hydrogenation. a-d, The microscopic images showing the surface deformation of the 30-nm Pd films on PDMS exposed to 4% H2. Due to the homogenous H2 absorption on the Pd surface, the irregular volume expansion of the Pd film after hydrogenation forms random surface wrinkles. The flow rate of H2 is 400 sccm. Scale bars: 20 μm.

Supplementary Figure 3 Monitoring areas of the reflected light intensity on the GPDP. The variation of reflected light intensities on different monitoring positions are obtained by extracting the grayscale changes at the pixels based on the Supplementary Video 2. To make the optical response only results from the hydrogenation of the GPDP, we kept the detected light intensity and the distance of the sample to the objective unchanged in this monitoring process. The monitoring areas (black line) are parallel to the edge (white dashed line) on the y-direction with the length of 10-μm containing two periods of the 1D ripple, which contain one pixel on the x-direction. The distances between the monitoring positions and the edge y0 are 55 μm, 62 μm, 68 μm, 80 μm, 91 μm, 98 μm, 105 μm and 112 μm, respectively.

Supplementary Figure 4 Naked-detectable hydrogen diffusion. The photos of the GPDP on exposure to H2 were illuminated by fluorescent tubes and recorded by a mobile camera. The concentration and flow rate of H2 are 4% and 1000 sccm, respectively. Scale bars: 0.6 mm.

Supplementary Figure 5 Surface deformation of the GPDP at low H2 concentration. a, The microscopic images showing the surface deformation of the GPDP with a 30-nm Pd film exposed to 0.4% H2. b,c,d, Magnified images of the surface deformation of the GPDP in a, indicating that volume of Pd film at low H2 concentration can not form uniform self-organized patterns.

Supplementary Figure 6 Simulated 1D self-organization of the GPDP with a 30-nm Pd film.

Supplementary Figure 7 Thickness modulation of 1D deformation. a-e, The microscopic images showing the 1D ripples with various thicknesses of Pd films exposed to 4% H2, where the thicknesses of Pd films are 30 nm in a, 40 nm in b, 48 nm in c, 57 nm in d and 67 nm in e, respectively. f, Experimental results (red dot) and theoretical calculation (black line) of the wavelength of the 1D ripple patterns with various thicknesses of the Pd films. Error bars are obtained by measuring the wavelength of the 1D ripple at various points of the GPDPs. Scale bars: 10 μm.

Supplementary Figure 8 Relationship between the β-phase formation time tβ and Pd thickness. The detected area is with a distance of 100 μm to the edge. The concentration and flow rate of H2 are 4% and 1000 sccm, respectively.

Supplementary Figure 9 Surface deformation of a Pd film on hard PDMS during hydrogenation. a,b, The microscopic images showing the surface deformation of the 30-nm GPDP on hard PDMS exposed to 4% H2 with an approximately 2-μm wavelength. Scale bars: 20 μm

Supplementary Figure 10 Process diagram of the diffusion-deformation framework to collect emipiral information and close the model.

Supplementary Figure 11 One-dimensional Fickian diffusion model. a, Schematic representation of the different physical quantities in the model and boundary conditions. b, Simulated results plotted with hydrogen concentration against the distance of monitoring lines from hydrogen entry port. Curves are shifted to the right with increasing time.

In the model we hypothesize that hydrogen diffusivities take concentration-depended values which are separated by diffusion phase fronts. The general solution of equation (7) can be derived by taking the following transformation:

ξi=y2Dit

dCi=Biexp⁡(ξi2)dξi

The boundary conditions to determine the integral constants are based on the concentration values and continuity in flux across the phase boundaries:

C1x=0,t=C0

C1x=Kβt,t=C2x=Kβt,t=Cβ

C2x=Kβt,t=Cα

j1=j2

which yields the following results when numerical values are substituted into them: Cβ-C0=B1012KβDβexp⁡(-ξ2)dξCα-Cβ=B212KβDβ12KaDαexp⁡(-ξ2)dξC∞-Cα=B212KαDα+∞exp⁡(-ξ2)dξDβB1exp-12KβDβ=DαB2exp-12KαDα, B1=-1.069B2=-410.2Dβ=4.5×10-10m2/sDα=0.0944×10-10m2/s

Supplementary Figure 12 a, Electromagnetic simulation of various orders of reflected light on a sinusoidal grating as shown in Fig. 1d with increasing undulating amplitudes. b, The relationship between the amplitude of the 1D ripple with various Pd thicknesses and the stress ratio σxσc1, which is calculated by the equation (5).

Supplementary Figure 13 Thickness modulation of 2D deformation. The microscopic images showing the 2D herringbones with various thicknesses of Pd films exposed to 4% H2, where the thicknesses of Pd films are 30 nm in a, 40 nm in b, 48 nm in c, 57 nm in d, 67 nm in e, respectively.