Supplementary files

Title:

Carbon cloth electrode for electrochemical synthesis of ammonia from nitrogen and water without any catalyst under ambient temperature and pressure

Author:

Seiji Tanahashi1, Kaku Uehara2,3*, and Masakazu Tanahashi1

1Tanah Process Ltd.:  541-0045 Dosho-machi 1-2-11, Chuoh-ku, Osaka City, Japan

tanahashi.seiji@tanap.jp, tanahashi.masakazu@tanap.jp

2Uehara Research Institute of Advanced Science and Technology: 590-0134 Miikedai 4-19-2, Minami-ku, Sakai, Osaka, Japan

kaku_uehara@yahoo.co.jp

3Emeritus Professor of Osaka Prefecture University

*Author for correspondence

Figure S1 High surface area porous activated carbon cloth electrode.

Before      After (900℃)

Figure S2 Before and after heat treatment of carbon cloth.

Figure S3 Volume resistivity of the high surface area porous activated carbon cloth before and after heat treatment at various temperature.

Table S1 The raw data of Figure 2

|  | pH=0 | pH=2 | pH=4 |
| --- | --- | --- | --- |
| blue dashed line | 0.10 volt | 0.10 volt | 0.10 volt |
| red dashed line | -0.14 volt | -0.14 volt | -0.14 volt |

Table S2 The raw data of Figure 3

| volt | -3.53 | -3.04 | -2.84 | -1.50 | 2.84 | 3.04 | 3.53 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| NH3mmol | 2.7 | 2.1 | 1.2 | 0.05 | - | - | - |
| H2 ppm | 0.05 | 0.02 | 0 | 0 | - | - | - |
| O2 ppm | - | - | - | - | 0 | 0.01 | 0.025 |

Table S3 The raw data of Figure S3

| HeatTemper ature ℃ | 25 | 700 | 800 | 900 | 1000 |
| --- | --- | --- | --- | --- | --- |
| VolumeResis tivity Ωcm | 0.71 | 0.62 | 0.50 | 0.25 | 0.14 |