Supplementary Information

Molecular Engineering towards Efficient White-Light-Emitting Perovskite

Mingming Zhang1,†, Lili Zhao2,†, Qian Zhang1, Najma Yaqoob3, Zhengmao Yin4, Payam Kaghazchi3, Weigao Xu2,*, Lei Wang1 & Jun Xing1,*

1Key Laboratory of Eco-Chemical Engineering, Ministry of Education, College of Chemistry and Molecular Engineering, Qingdao University of Science & Technology, Qingdao 266042, China.

2Key Laboratory of Mesoscopic Chemistry, Ministry of Education, School of Chemistry and Chemical Engineering, Nanjing University, Nanjing 210023, China.

3Forschungszentrum Jülich GmbH, Institute of Energy and Climate Research, Materials Synthesis and Processing (IEK-1), Wilhelm-Johnen-Straße, 52425 Jülich, Germany.

4School of Materials Science and Technology, Qingdao University of Science & Technology, Qingdao 266042, China.

*correspondence: xuwg@nju.edu.cn and xingjun@qust.edu.cn

† These authors contributed equally to this work.

Figure S1. Atomic structure of perovskites (PMA)2PBr4, (2-ClPMA)2PBr4, (3-ClPMA)2PBr4 and (4-ClPMA)2PBr4.

Figure S2. PL spectrum of (2-ClPMA)2PbBr4 synthesized by fast reprecipitation method.

a

b

Figure S3. Digital images of (a) (PMA)2PbBr4, (2-FPMA)2PbBr4, (3-FPMA)2PbBr4, (4-FPMA)2PbBr4 and (b) (PMA)2PbBr4, (2-BrPMA)2PbBr4, (3-BrPMA)2PbBr4, (4-BrPMA)2PbBr4 crystals under ambient light (upper) and UV light (lower).

a

b

Figure S4. (a) Powder XRD patterns of perovskites (PMA)2PbBr4 and (2-CH3PMA)2PbBr4. (b) Absorption (dashed line) and PL spectrum (solid line) of (2-CH3PMA)2PbBr4.

a

b

Figure S5. PL spectra of perovskites (a) (PEA)2PbBr4, (2-FPEA)2PBr4, (3-FPEA)2PBr4, (4-FPEA)2PBr4 and (b) (2-ClPEA)2PBr4, (3-ClPEA)2PBr4, (4-ClPEA)2PBr4.

Table S1. Crystal lattice constants of perovskites (PMA)2PbBr4, (2-ClPMA)2PbBr4, (3-ClPMA)2PbBr4 and (4-ClPMA)2PbBr4.

|  | a (Å) | b (Å) | c (Å) |
| --- | --- | --- | --- |
| (PMA)2PbBr4 | 33.11 | 8.08 | 7.97 |
| (2-ClPMA)2PbBr4 | 32.01 | 8.40 | 8.03 |
| (3-ClPMA)2PbBr4 | 35.99 | 8.04 | 8.02 |
| (4-ClPMA)2PbBr4 | 36.18 | 8.06 | 7.94 |

Table S2. The performance of reported low-dimensional hybrid perovskites with BWL emission.

| Compositions | PLQY (%) | CRI | CIE | Ref |
| --- | --- | --- | --- | --- |
| (N-MEDA)PbBr4 | 0.5 | 82 | (0.36, 0.41) | J. Am. Chem. Soc. 2014, 136, 1718 |
| (EDBE)PbBr4 | 9 | 84 | (0.39, 0.42) | J. Am. Chem. Soc. 2014, 136, 13154 |
| (EDBE)PbCl4 | 2 | 81 | (0.33, 0.39) |  |
| (PEA)2PbCl4 | < 1 | 84 | (0.37, 0.42) | Chem. Mater. 2017, 29, 3947 |
| (EA)4Pb3Cl10 | / | 66 | (0.27, 0.39) | J. Am. Chem. Soc. 2017, 139, 11956 |
| (EA)4Pb3Cl9.5Br0.5 | / | 83 | (0.30, 0.35) |  |
| (CyBMA)PbBr4 | 1.5 | / | (0.23, 0.29) | ChemSusChem 2017, 10, 3765 |
| C4N2H14PbBr4 | 20 | 63 | (0.21, 0.28) | Nat. Commun. 2017, 8, 14051 |
| (NAI)2PbCl4 | < 1 | 90 | (0.36, 0.37) | J. Mater. Chem. C 2018, 6, 1171 |
| (2meptH2)PbBr4 | 3.37 | 91 | (0.24, 0.23) | Chem. Commun. 2018, 54, 4053 |
| C5H14N2PbCl4·H2O | 1 | 94 | (0.39, 0.37) | J. Mater. Chem. C 2018, 6, 6033 |
| (BAPP)Pb2Br8 | 1.5 | 87 | (0.37, 0.40) | Adv. Mater. 2019, 31, 1807383 |
| (TDMP)PbBr4 | 46 | 75 | (0.29, 0.37) |  |
| (TDMP)PbCl4 | 7.5 | 74 | / | J. Am. Chem. Soc. 2019, 141, 12619 |
| (C4H9NH3)2PbCl4 | 1 | 86 | (0.37, 0.40) | Adv. Funct. Mater. 2019, 29, 1805038 |
| (AMP)PbCl4 | < 1 | 90 | (0.28, 0.34) |  |
| (1HIEA)PbBr4 | / | 73 | (0.32, 0.41) | J. Mater. Chem. C 2020, 8, 889 |
| (2-ClPMA)2PbBr4 | 32 | 86 | (0.30, 0.33) | This work |

Table S3. The PL decay parameters of (2-ClPMA)2PbBr4 and (3-ClPMA)2PbBr4.

|  | τ1,STEs (ns) | τ2,STEs (ns) | τ1,FEs (ns) | τ2,FEs (ns) |
| --- | --- | --- | --- | --- |
| (2-ClPMA)2PbBr4 | 3.23 | 0.90 | 1.39 | 0.36 |
| (3-ClPMA)2PbBr4 | 3.17 | 0.82 | 1.04 | 0.33 |

According to previous report (Chem. Sci. 2017, 8, 4497), the emission ratio ISTEs/IFEs at a given temperature is related to △Gself-trap (self-trapping depth = ESTEs  EFEs) and the radiative emission rates from the STE and FEs states (kr,STEs and kr,FEs).

lnISTEsIFEs ∝ln kr,STEskr,FEs- △Gself-trapKbT

Equals to 
lnISTEsIFEs ∝ln τr,FEsτr,STEs- △Gself-trap25.7 meV (T=298 K)

In this case, the STEs emission energy is several hundreds of meV lower than that of FEs, implying the STEs state should be much lower than that of FEs state. So,

△Gself-trap25.7 meV ≫ ln 1.393.23((2-ClPMA)2PbBr4) or  ln 1.043.17 ((3-ClPMA)2PbBr4)

Thus, ISTEs/IFEs is dominated by the △Gself-trap.

Table S4. Summaries of atoms distances and Coulomb forces of perovskites (PMA)2PbBr4, (2-ClPMA)2PbBr4, (3-ClPMA)2PbBr4 and (4-ClPMA)2PbBr4.

| Sample | Distance of N-Pb1 (nm) | Distance of N-Pb2 (nm) | Distance of N-Pb3 (nm) | Distance of N-Pb4 (nm) | Average Coulomb force (nN) |
| --- | --- | --- | --- | --- | --- |
| (PMA)2PbBr4 | 0.4305 | 0.4439 | 0.5361 | 0.5494 | 0.7270 |
| (2-ClPMA)2PbBr4 | 0.4313 | 0.4340 | 0.5318 | 0.5333 | 0.8250 |
| (3-ClPMA)2PbBr4 | 0.4314 | 0.4318 | 0.5343 | 0.5380 | 0.7669 |
| (4-ClPMA)2PbBr4 | 0.4309 | 0.4357 | 0.5331 | 0.5341 | 0.7783 |

According to the crystal structure, we summarized the coordinates of atoms N and Pb in a unit cell and assume that the centers of the positive charges of -NH3 cations and the negative charges of PbBr3 anions are located on the N atoms and Pb atoms, respectively. According to Coulomb law F=kq1×q2d2, the average Coulomb force between -NH3 and four adjacent  PbBr3 was calculated.