Synthesis, photophysical, electrochemical, and DFT examinations of two new organic dye molecules based on phenothiazine and dibenzofuran

K. Periyasamy1*, P. Sakthivel2, G.Venkatesh3, P.M. Anbarasan4, P.Vennila5, Y.Sheena Mary6, S.Kaya7, Sultan Erkan8

1Department of Physics, Vaigai Arts and Science Women’s College, Salem – 636 111, India

2 Department of Physics, Selvamm Arts and Science College, Namakkal – 637 003, India

3Department of Chemistry, MMCAS, Rasipuram, Tamil Nadu-637408, India

4Department of Physics, Periyar University, Salem-636 011, India

5Department of Chemistry, Thiruvalluvar Government Arts College, Rasipuram – 637408, India

6Researcher, Thushara, Neethinagar-64, Kollam, Kerala, India

7Department of Chemistry, Cumhuriyet University, Sivas-58140, Turkey

8Department of Chemistry, Cumhuriyet University, Faculty of Science, Sivas-58140, Turkey

1.0 Synthetic procedure for PFCH and BFCH

(Z)-N-((5-(10H-phenothiazin-2-yl)furan-2-yl)methylene)-2-cyanoacetohydrazide (PFCH) and (Z)-2-cyano-N'-((5-(dibenzo[b,d]furan-4-yl)furan-2-yl)methylene)acetohydrazide (BFCH) were synthesized using (Pd(Ph3)4 as a catalyst in Suzuki coupling and Knoevenagel condensation reactions with (5-formylfuran-2-yl)boronic acid, as seen in Fig.1. 2-Chlorophenothiazine (0.47 g, 2 mmol), (5-formylfuran-2-yl)boronic acid (82.1 mg, 0.53 mmol), (Pd(Ph3)4 (0.05 g, 0.04 mmol), sodium carbonate (20 ml (2 M)), THF 10 ml, and purified water  5 ml are added to round-bottom flasks and boiled for one hour at 45C. After cooling and quenching with 50 ml of distilled water, the mixture was isolated with CH2Cl2 (30 ml). The organic process is washed (50 ml) with purified water, dried with anhydrous sodium sulphate, and filtered. The compound was purified using column chromatography by silica gel with a mixture of CH2Cl2 and Hexane (1:6), then recrystallized with methanol/CH2Cl2, yielding a brown solid of 5-(10H-phenothiazin-2-yl)furan-2-carbaldehyde. A brown solid of 5-(10H-phenothiazin-2-yl)furan-2-carbaldehyde (0.34g, 1.09 mmol), 2-cyanoacetohydrazide (0.17 g, 1.72 mmol), piperidine (3 ml), and acetic acid (10 ml) was thoroughly mixed in a round-bottom flask. The round-bottom flask is connected to the reflux condenser, and the mixture has been heated at a constant temperature of 120C for 12 hours. The mixture was allowed to cool to room temperature before being quenched with 5 ml of distilled water and the precipitate was purified and cleaned with distilled water. The residue was purified by column chromatography on silica (CH2Cl2/Ethanol 10:1) to yield 0.22 g of brown solid.

4-Bromodibenzofuran (0.5 g, 2.02 mmol), (5-formylfuran-2-yl)boronic acid (82.1 mg, 0.53 mmol), (Pd(Ph3)4 (0.05 g, 0.04 mmol, Sodium carbonate (20 ml 2 M), THF 15 ml, and purified water 10 ml are placed in round-bottom flasks and heated for two hours at 60C. The mixture was subjected and quenched with purified water (30 ml) before being removed with CH2Cl2 (15ml). The mixture was cooled, and quenched with distilled water (30 ml), extracted with CH2Cl2 (30 ml). The residual is cleaned, dried, purified, and recrystallized using the same process. The mixture of 5-(dibenzo[b,d]furan-4-yl)furan-2-carbaldehyde (0.34 g, 1.078 mmol), 2-cyanoacetohydrazide (0.17 g, 1.72 mmol), piperidine (3ml), and acetic acid (10 ml) was stirred continuously for 12 hours at a steady temperature of 100 C. Following closure, the reaction was cooling and purified using the same procedure. Column chromatography on silica (CH2Cl2/Ethanol 10:1) was used to effectively purify the BFCH dye compound, yielding 0.18 g of brown solid.

2.0 Fabrication of the dye-sensitized solar cells

A fluorine-doped tin oxide conducting glass is washed in an ultrasonic bath with distilled water, alcohol and followed acetone to remove unnecessary objects. According to the previously study, titanium oxide nanoparticles (20 nm) have been prepared through a hydrothermal treatment with a precursor solution containing Ti(OBu)4 (10 mL), ethanol (20 mL), acetic acid (18 mL), and distilled water (50 mL). The TiO2 powder (1.0 g) had been ground for 40 minutes in a solution of ethanol (8.0 mL), acetic acid (0.2 mL), terpineol (3.0 g), and ethyl cellulose (0.5 g). The homogenized slurry was then sonicated in an ultrasonic bath for 15 minutes to create a viscous white titanium oxide paste. The paste was then screen-printed onto FTO glass and titanium oxide photoanodes (approximately 16 m thickness) have been prepared. To extract the organic material, the primed films were annealed in a muffle furnace. Titanium oxide films have been soaking in TiCl4 (0.04 M) aqueous phase for 30 minutes at 70C to increase photocurrent and photovoltaic efficiency. The treated films are again cleaned with distilled water and ethanol before being sintered again at 520C for 30 minutes. Since cooling to 80C, the films are soaked in a 5.0  10-4 M solution of both dyes for 10 hours. Films is removed from solution and rinsed with CH2Cl2 to remove physical adsorbed organic dye. To evaluate the photovoltaic efficiency of dye-sensitized TiO2/FTO glass films, they were sandwiched with a Pt/FTO counter electrode. The counter electrode is generated by thermally depositing a hexachloroplatinic acid hexahydrate (5 mM in isopropanol) solution onto FTO glass and then heating for 15 minutes in air at 400C. The electrolyte (0.6 M 1-methyl-3-propylimidazolium iodide (PMII), 0.10 M guanidinium thiocyanate, 0.05 M LiI, 0.03 MI2 and 0.5 M tert-butylpyridine) in acetonitrile/valeronitrile (85:15) was inserted into the inter space between the photo anode and counter electrode through a hole created on the reference electrode. The dye coated TiO2 film's active region was 0.16 cm2, and the aspect ratio of the black mask used was approximately 0.25 cm2.

Figure S1: Calculated UV spectra of title compounds using 6-311G/CAM-B3LYP

Figure S2: Vibrational spectra of PFCH

Figure S3: Vibrational spectra of BFCH

Figure S4: 13C NMR of PFCH

Figure S5: 1H NMR of PFCH

Figure S6: 13C NMR of BFCH

Figure S7: 1H NMR of BFCH

Table S1: Natural bond orbital analysis of PFCH

| Donor NBO(i) | Acceptor NBO(j) | E(2) kcal/mol | E(j)-E(i) au | F(i,j) au |
| --- | --- | --- | --- | --- |
| C9-C10 | N5-C8 | 19.43 | 0.28 | 0.066 |
| C9-C10 | C11-C12 | 14.44 | 0.30 | 0.060 |
| C11-C12 | C9-C10 | 18.16 | 0.29 | 0.066 |
| C11-C12 | C14-C15 | 12.99 | 0.31 | 0.059 |
| C13-C26 | C14-C15 | 20.23 | 0.29 | 0.070 |
| C13-C26 | C16-C17 | 16.67 | 0.28 | 0.062 |
| C14-C15 | C11-C12 | 19.90 | 0.27 | 0.066 |
| C14-C15 | C13-C26 | 18.57 | 0.27 | 0.064 |
| C14-C15 | C16-C17 | 22.63 | 0.27 | 0.070 |
| C16-C17 | C13-C26 | 20.80 | 0.28 | 0.070 |
| C16-C17 | C14-C15 | 17.14 | 0.29 | 0.065 |
| C19-C20 | C17-S18 | 16.35 | 0.29 | 0.063 |
| C19-C20 | C23-C24 | 20.97 | 0.28 | 0.071 |
| C21-C22 | C19-C20 | 22.72 | 0.27 | 0.071 |
| C21-C22 | C23-C24 | 18.91 | 0.27 | 0.065 |
| C23-C24 | C19-C20 | 17.62 | 0.28 | 0.063 |
| C23-C24 | C21-C22 | 21.37 | 0.29 | 0.070 |
| O3 | C1-C2 | 21.39 | 0.61 | 0.103 |
| O3 | C1-N4 | 24.38 | 0.68 | 0.117 |
| N4 | C1-O3 | 54.25 | 0.28 | 0.113 |
| N4 | N5-C8 | 28.56 | 0.28 | 0.082 |
| N5 | C8-C9 | 11.13 | 0.89 | 0.090 |
| N7 | C2-C6 | 11.78 | 0.96 | 0.095 |
| S18 | C16-C17 | 11.71 | 0.26 | 0.053 |
| S18 | C19-C20 | 10.84 | 0.27 | 0.051 |
| N25 | C13-C26 | 34.04 | 0.28 | 0.090 |
| N25 | C23-C24 | 31.88 | 0.29 | 0.088 |
| O41 | C9-C10 | 23.54 | 0.34 | 0.082 |
| O41 | C11-C12 | 25.62 | 0.35 | 0.087 |

Table S2: Natural bond orbital analysis of BFCH

| Donor NBO(i) | Acceptor NBO(j) | E(2) kcal/mol | E(j)-E(i) au | F(i,j) au |
| --- | --- | --- | --- | --- |
| N5-C6 | C7-C8 | 10.28 | 0.35 | 0.057 |
| C7-C8 | N5-C6 | 22.19 | 0.28 | 0.071 |
| C7-C8 | C9-C10 | 15.05 | 0.30 | 0.061 |
| C9-C10 | C7-C8 | 17.76 | 0.29 | 0.066 |
| C9-C10 | C18-C19 | 13.83 | 0.30 | 0.060 |
| C12-C13 | C14-C15 | 14.73 | 0.28 | 0.059 |
| C12-C13 | C16-C17 | 19.32 | 0.29 | 0.068 |
| C12-C13 | C18-C19 | 18.91 | 0.28 | 0.066 |
| C14-C15 | C12-C13 | 15.05 | 0.28 | 0.058 |
| C14-C15 | C20-C21 | 18.93 | 0.28 | 0.066 |
| C14-C15 | C22-C23 | 19.43 | 0.28 | 0.068 |
| C16-C17 | C12-C13 | 19.51 | 0.27 | 0.067 |
| C16-C17 | C18-C19 | 21.44 | 0.27 | 0.070 |
| C18-C19 | C9-C10 | 20.09 | 0.27 | 0.067 |
| C18-C19 | C12-C13 | 22.28 | 0.28 | 0.071 |
| C18-C19 | C16-C17 | 18.12 | 0.28 | 0.065 |
| C20-C21 | C14-C15 | 22.36 | 0.28 | 0.072 |
| C20-C21 | C22-C23 | 18.31 | 0.28 | 0.064 |
| C22-C23 | C14-C15 | 19.14 | 0.27 | 0.067 |
| C22-C23 | C20-C21 | 20.68 | 0.28 | 0.068 |
| O3 | C1-C2 | 21.44 | 0.60 | 0.103 |
| O3 | C1-N4 | 23.82 | 0.69 | 0.116 |
| N4 | C1-O3 | 57.43 | 0.27 | 0.115 |
| N4 | N5-C6 | 31.77 | 0.27 | 0.084 |
| N5 | C6-C7 | 11.51 | 0.89 | 0.091 |
| O11 | C12-C13 | 22.87 | 0.35 | 0.084 |
| O11 | C14-C15 | 21.48 | 0.35 | 0.082 |
| N25 | C2-C24 | 11.74 | 0.96 | 0.095 |
| O39 | C7-C8 | 22.10 | 0.36 | 0.081 |
| O39 | C9-C10 | 23.63 | 0.36 | 0.084 |

Table S3: Vibrational assignments of PFCH

| S.No. | Experimental | Calculated | IR Intensity | TED (%) |
| --- | --- | --- | --- | --- |
| 1 | 3503 | 3512 | 2.39 | NH(100) |
| 2 | 3356 | 3354 | 0.96 | NH(94) |
| 3 | 3152 | 3145 | 0.52 | CH(100) |
| 4 | 3122 | 3124 | 2.65 | CH(98) |
| 5 | - | 3097 | 2.38 | CH(83) |
| 6 | 3088 | 3089 | 3.72 | CH(95) |
| 7 | - | 3087 | 0.90 | CH(92) |
| 8 | - | 3078 | 0.25 | CH(94) |
| 9 | 3048 | 3055 | 1.69 | CH(86) |
| 10 | - | 3043 | 0.41 | CH(99) |
| 11 | 3028 | 3036 | 1.00 | CH(86) |
| 12 | 2988 | 2981 | 1.13 | CH(94) |
| 13 | 2872 | 2864 | 0.01 | CH(99) |
| 14 | 2851 | 2845 | 0.38 | CH(100) |
| 15 | 2341 | 2342 | 1.28 | NC(89) |
| 16 | 1801 | 1796 | 50.92 | OC(15) |
| 17 | 1592 | 1594 | 2.64 | CC(42) |
| 18 | 1588 | 1591 | 0.47 | CC(23) |
| 19 | 1581 | 1584 | 0.17 | CCNC(14) |
| 20 | - | 1575 | 1.67 | CC(24) |
| 21 | 1552 | 1563 | 2.48 | CC(26) |
| 22 | - | 1558 | 1.04 | CC(18) |
| 23 | 1514 | 1520 | 3.40 | CC(24) |
| 24 | 1488 | 1497 | 1.06 | CC(31) |
| 25 | - | 1475 | 9.13 | OC(54) |
| 26 | 1466 | 1462 | 10.09 | CC(41), HCN(11) |
| 27 | - | 1455 | 100.00 | CC (22) |
| 28 | 1429 | 1438 | 5.25 | CC (12) |
| 29 | - | 1438 | 7.42 | CC (22) |
| 30 | - | 1390 | 0.73 | CC (18) |
| 31 | 1381 | 1383 | 3.04 | CC(21), HCN(14) |
| 32 | - | 1371 | 16.08 | CC (11) |
| 33 | - | 1321 | 4.44 | CC (18) |
| 34 | 1301 | 1305 | 20.88 | HCC(54) |
| 35 | 1294 | 1298 | 0.64 | HCC(42) |
| 36 | 1292 | 1288 | 4.70 | HCC(12) |
| 37 | - | 1266 | 1.39 | HCC(24) |
| 38 | - | 1251 | 13.92 | HCC(19) |
| 39 | 1224 | 1227 | 0.01 | CCC(18) HCC(8) |
| 40 | 1218 | 1222 | 4.26 | SC(24) |
| 41 | - | 1215 | 4.45 | HCC(28) |
| 42 | - | 1189 | 0.16 | HCC(28) |
| 43 | 1179 | 1181 | 0.06 | NC(14) |
| 44 | 1166 | 1158 | 11.74 | NC(26) |
| 45 | - | 1152 | 29.56 | NN(11) |
| 46 | - | 1145 | 5.36 | HCC(22) |
| 47 | 1133 | 1139 | 43.87 | SC(14) |
| 48 | - | 1104 | 2.16 | NN(31) |
| 49 | 1097 | 1084 | 0.83 | OC(36), HCN(24) |
| 50 | - | 1065 | 41.15 | CCCC(16) |
| 51 | 1042 | 1046 | 2.70 | HCC(12) |
| 52 | - | 1032 | 1.23 | CSC(18) |
| 53 | - | 1023 | 4.35 | CCO(22) |
| 54 | 977 | 978 | 3.66 | HCC(14) |
| 55 | - | 976 | 0.01 | CCN(11) |
| 56 | 972 | 970 | 0.04 | COC(17) |
| 57 | - | 968 | 0.18 | COC(11) |
| 58 | - | 967 | 2.32 | HCCC(8) |
| 59 | - | 932 | 0.35 | HCCN(11) |
| 60 | 918 | 926 | 2.27 | CCO(12) |
| 61 | - | 923 | 4.05 | CS(33) |
| 62 | 878 | 870 | 2.07 | CCC(13), HCC(14) |
| 63 | - | 855 | 6.68 | CCCC(12) |
| 64 | - | 851 | 0.54 | HCC(24) |
| 65 | 844 | 847 | 0.16 | NCC(18), HCC(18) |
| 66 | - | 834 | 1.41 | CCC(10) |
| 67 | 828 | 831 | 9.50 | CS(12) |
| 68 | - | 826 | 0.18 | COC(14) |
| 69 | - | 784 | 21.45 | CCCC(22) |
| 70 | 758 | 761 | 11.32 | HCC(18) |
| 71 | - | 758 | 18.63 | SCCC(22) |
| 72 | 715 | 717 | 0.18 | HCC(24), CCNC(12) |
| 73 | 716 | 714 | 0.13 | CNC(14) |
| 74 | - | 706 | 0.49 | CCCN(12) |
| 75 | 696 | 699 | 0.50 | COC(18) |
| 76 | - | 684 | 0.39 | CCNC(22), CNC(10) |
| 77 | - | 676 | 0.67 | OCN(19) |
| 78 | - | 672 | 6.26 | CSC(15), CNC(11) |
| 79 | 644 | 646 | 0.24 | OCN(11) |
| 80 | - | 638 | 0.64 | CCC(18) |
| 81 | 518 | 617 | 0.14 | NNC(22) |
| 82 | - | 598 | 7.21 | CNC(21) |
| 83 | - | 566 | 4.26 | CNC(14) |
| 84 | 562 | 564 | 2.78 | COC(11) |
| 85 | - | 559 | 0.20 | CCC(14) |
| 86 | 522 | 528 | 2.04 | NCC(16) |
| 87 | - | 527 | 0.66 | NCCC(10) |
| 88 | - | 510 | 2.49 | CSCC(9) |
| 89 | 488 | 490 | 1.44 | CSCC(11) |
| 90 | - | 468 | 4.09 | OCCC(12) |
| 91 | 446 | 448 | 0.91 | CNN(14) |
| 92 | - | 447 | 0.37 | CCNC(12) |
| 93 | 438 | 437 | 0.16 | CNNH(26) |
| 94 | - | 371 | 1.90 | CNNH (18) |
| 95 | - | 370 | 1.39 | CNCC(11) |
| 96 | - | 349 | 1.00 | CNCC(14) |
| 97 | - | 347 | 0.15 | CCCC(15) |
| 98 | - | 325 | 0.15 | CCNN(11) |
| 99 | - | 286 | 0.32 | NCCC(14) |
| 100 | - | 268 | 0.07 | NCCC(15) |
| 101 | - | 244 | 0.04 | CNN(10) |
| 102 | - | 237 | 0.03 | NCC(34) |
| 103 | - | 212 | 0.04 | CNCC(25) |
| 104 | - | 177 | 0.80 | NCC(34) |
| 105 | - | 150 | 0.03 | CNC(11) |
| 106 | - | 136 | 0.01 | NCC(14) |
| 107 | - | 126 | 0.13 | CCS(12) |
| 108 | - | 123 | 0.15 | CNNC(11) |
| 109 | - | 102 | 0.05 | NCCC(15) |
| 110 | - | 98 | 0.42 | CCNN(28) |
| 111 | - | 84 | 0.01 | SCCC(11) |
| 113 | - | 66 | 0.01 | CNC(12) |
| 114 | - | 59 | 0.02 | OCNC(10) |
| 115 | - | 48 | 0.07 | CCOC(12) |
| 116 | - | 41 | 0.60 | CCCC(33) |
| 117 | - | 33 | 0.81 | CCCC(12) |

Table S4: Vibrational assignments of BFCH

| S.No. | Experimental | Calculated | IR Intensity | TED (%) |
| --- | --- | --- | --- | --- |
| 1 | 3446 | 3452 | 1.95 | NH(100) |
| 2 | 3202 | 3208 | 0.94 | CH(97) |
| 3 | - | 3081 | 2.08 | CH(94) |
| 4 | 3096 | 3089 | 1.68 | CH(74) |
| 5 | - | 3072 | 4.35 | CH(66) |
| 6 | 3069 | 3066 | 6.92 | CH(84) |
| 7 | - | 3061 | 0.64 | CH(57) |
| 8 | 3052 | 3053 | 2.07 | CH(64) |
| 9 | - | 3048 | 1.04 | CH(50) |
| 10 | 3046 | 3042 | 0.25 | CH(52) |
| 11 | - | 3025 | 0.96 | CH(59) |
| 12 | 2954 | 2948 | 0.01 | CH(78) |
| 13 | 2918 | 2916 | 0.63 | CH(99) |
| 14 | 2229 | 2223 | 2.47 | NC(88) |
| 15 | 1658 | 1652 | 97.55 | CC(75) |
| 16 | - | 1607 | 0.90 | CC(58) |
| 17 | 1575 | 1578 | 0.11 | OC(14) |
| 18 | 1562 | 1571 | 3.72 | CC(62) |
| 19 | - | 1566 | 2.59 | CC(33) |
| 20 | - | 1563 | 4.95 | CC(16) |
| 21 | 1518 | 1522 | 3.30 | CC(47) |
| 22 | - | 1472 | 7.60 | CC(69) |
| 23 | - | 1458 | 13.83 | CC(49) |
| 24 | 1448 | 1453 | 19.30 | CC(38), HCN(24) |
| 25 | - | 1433 | 26.26 | CC(19) |
| 26 | 1422 | 1420 | 10.86 | CC(28) |
| 27 | - | 1403 | 7.65 | CC(10) |
| 28 | 1388 | 1386 | 11.12 | NC(30) |
| 29 | - | 1361 | 10.75 | CC (18), HCN(10) |
| 30 | - | 1356 | 3.96 | CC (11) |
| 31 | 1333 | 1339 | 78.67 | HCC(41),NC(14) |
| 32 | - | 1329 | 0.31 | HCC(17) |
| 33 | 1301 | 1305 | 1.05 | HCC(18), HCN(11) |
| 34 | - | 1297 | 1.21 | HCH(8), CC(13) |
| 35 | - | 1248 | 1.31 | CC (25) |
| 36 | 1236 | 1237 | 100.00 | HCC(18),NC(11) |
| 37 | - | 1220 | 7.38 | HCC(26) |
| 38 | - | 1203 | 6.65 | HCC(21), HCN(8) |
| 39 | - | 1190 | 0.01 | NC(15), CCC(10) |
| 40 | - | 1174 | 16.09 | CCCC(16) |
| 41 | - | 1164 | 16.24 | HCCN(11) |
| 42 | 1158 | 1159 | 2.00 | HCC(28) |
| 43 | 1149 | 1147 | 26.82 | HCC(18) |
| 44 | - | 1119 | 16.34 | NC(8) |
| 45 | 1098 | 1100 | 0.91 | CCN(18), HCC(14) |
| 46 | - | 1067 | 19.43 | OC(12) |
| 47 | - | 1053 | 25.48 | HCC(17) |
| 48 | 1042 | 1040 | 14.48 | NN(44), OC(12) |
| 49 | - | 1004 | 0.57 | CCC(18) |
| 50 | - | 1001 | 0.88 | NN(18) |
| 51 | - | 969 | 0.00 | CCCC(16) |
| 52 | - | 967 | 2.48 | HCCC(22), CNC(11) |
| 53 | 964 | 966 | 0.19 | HCC(22) |
| 54 | - | 929 | 1.87 | HCC(10) |
| 55 | - | 927 | 0.45 | HCC(22) |
| 56 | 918 | 921 | 0.17 | HCCC(52) |
| 57 | - | 905 | 0.10 | CCCC(14) |
| 58 | 891 | 884 | 0.38 | CCN(11) |
| 59 | - | 851 | 3.96 | HCCN(14) |
| 60 | - | 850 | 2.16 | CCO(20) |
| 61 | 826 | 825 | 1.57 | CCC(19), HCC(11) |
| 62 | - | 816 | 29.15 | HCCC(15) |
| 63 | - | 813 | 0.21 | CCCC(12) |
| 64 | - | 788 | 0.12 | HCC(16) |
| 65 | - | 781 | 16.54 | HCCC(16) |
| 66 | - | 764 | 11.76 | CCC(19) |
| 67 | 746 | 748 | 23.58 | HCC(26), CCCN(11) |
| 68 | - | 740 | 8.75 | CCC(10) |
| 69 | - | 717 | 0.01 | CCC(14) |
| 70 | - | 701 | 26.86 | COCC(11) |
| 71 | 702 | 700 | 1.72 | COCC(18) |
| 72 | - | 669 | 0.29 | CCNC(17) |
| 73 | 632 | 635 | 1.46 | CNC(23) |
| 74 | - | 609 | 0.04 | CCC(14) |
| 75 | - | 592 | 3.55 | CCCC(20) |
| 76 | - | 581 | 2.65 | CCCC(61) |
| 77 | - | 569 | 2.67 | CCCC(35) |
| 78 | - | 565 | 1.61 | COCC(34) |
| 79 | 555 | 557 | 0.06 | HNNC(43) |
| 80 | - | 547 | 9.13 | CCCC(34) |
| 81 | - | 545 | 0.09 | CCOC(21) |
| 82 | 522 | 523 | 0.48 | CCC(24) |
| 83 | - | 497 | 0.24 | CCC(27) |
| 84 | - | 482 | 8.57 | CCCC(36) |
| 85 | - | 464 | 3.62 | CCCC(31) |
| 86 | - | 457 | 9.61 | CNN(12) |
| 87 | - | 423 | 0.68 | OCC(24) |
| 88 | - | 393 | 2.59 | NNCC(12) |
| 89 | - | 358 | 0.51 | OCCC(30) |
| 90 | - | 344 | 1.76 | CCOC(16) |
| 91 | - | 343 | 0.00 | OCN(23) |
| 92 | - | 325 | 0.28 | CCC(25) |
| 93 | - | 287 | 0.01 | CCO(36) |
| 94 | - | 279 | 0.19 | CCOC(17) |
| 95 | - | 267 | 0.08 | OCCC(19) |
| 96 | - | 228 | 0.31 | NCC(20) |
| 97 | - | 222 | 1.05 | CCC(18) |
| 98 | - | 187 | 1.70 | CCC(29) |
| 99 | - | 182 | 0.80 | NCCC(14) |
| 100 | - | 164 | 0.00 | CCC(11) |
| 101 | - | 138 | 0.79 | CCCC(77) |
| 102 | - | 109 | 0.05 | CCC(22) |
| 103 | - | 98 | 0.55 | CCCC(13) |
| 104 | - | 90 | 0.53 | OCC(14) |
| 105 | - | 84 | 0.60 | NCCC(28) |
| 106 | - | 76 | 0.00 | NCCC(18) |
| 107 | - | 58 | 2.31 | NNCC(20) |
| 108 | - | 44 | 0.58 | CNNC(10) |
| 109 | - | 36 | 0.24 | NCCC(18) |
| 110 | - | 28 | 0.25 | CCNN(10) |
| 111 | - | 22 | 5.66 | CCCN(25) |