Palladium Nanoparticles Supported on Activated Carbon (C)) for the Catalytic Hexavalent Chromium Reduction

İbrahim Gözetena, Mehmet Tunça

aDepartment of Chemistry, Faculty of Science, Van Yüzüncü Yıl University, 65080, Tuşba, Van, Turkey

(SUPPORTING INFORMATION)

Fig. S-1 The volume of gas versus time graph for the decomposition of FA aqueous solution (10.0 mL H2O, 250 mM FA, 250 mM SF ) over Pd@C catalyst at 298 K.in the without trap and with trap.

Fig. S-2 UV-Vis spectra for the reduction of chromium (VI) to chromium (III)  using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 ml H2O) on Ni@C nanocatalyst (10 mg; 1.40  wt %; 0.238 mM Pd) at 298 K.

Fig. S-3 UV-Vis spectra for the reduction of chromium (VI) to chromium (III)  using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 mL H2O) on Ru@C nanocatalyst (10 mg; 1.37  wt %; 0.136 mM Pd) at 298 K.

Fig. S-4 UV-Vis spectra for the reduction of chromium (VI) to chromium (III)  by using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 mL H2O) on Pd@C nanocatalyst (10 mg; 1.37 wt %; 0.129 mM Pd) at 298 K.

Fig. S-5 UV-Vis spectra for the reduction of chromium (VI) to chromium (III)  using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 mL H2O) on Pd@C nanocatalyst (10 mg; 1.37  wt %; 0.129 mM Pd) at 298K. by different FA concentrations.

Fig. S-6 UV-Vis spectra for the reduction of chromium (VI) to chromium (III)  using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 mL H2O) on Pd@C nanocatalyst (10 mg; 1.37 wt %; 0.129 mM Pd) at 298 K.  by different SF concentrations.

Fig. S-7 UV-Vis spectra for the reduction chromium (VI) to chromium (III)  using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 mL H2O) on Pd@C nanocatalyst (10 mg; 1.37  wt %; 0.129 mM Pd) at 298K by different Cr2O72- concentrations (a) 1.0 mM, (b) 2.0 mM, (c) 4.0 mM, (d) 8.0 mM.

Fig. S-8 UV-Vis spectra for the reduction of chromium (VI) to chromium (III)  using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 mL H2O) on Pd@C nanocatalyst (10 mg; 1.37  wt %; 0.129 mM Pd) and different Pd concentrations (a) 6.4 µmol, (b) 97 µmol, (c) 129 µmol, (d) 193 µmol at 298K.

Fig. S-9 UV-Vis spectra for the reduction of chromium (VI) to chromium (III)  using FA by (2.103- M K2Cr2O7, 450 mM HCOOH, 450 mM HCOONa in 10 mL H2O) on Pd@C nanocatalyst (10 mg; 1.37 wt%; 0.129 mM Pd)  in the different  (a) 298K, (b) 303K, (c) 308K, (d) 313K and (e) 318K temperatures.

Author to whom correspondence should be addressed: E-mail address: ibrahim6349@hotmail.com  (İ. Gözeten)