Supplemental Table 1. FTIR characteristic peak assignment for our plastic standards

| Polymer | FTIR Transmission Assignment | Characteristic Peaks (cm -1) |
| --- | --- | --- |
| Polyester (PE) | C = O stretching C – O stretching Aromatic CH out-of-plane bending | 1711 1242, 1095 722 |
| High density polyethylene (HDPE) | C-H stretching CH2 bending | 2913, 2847 1471 |
| Polyvinyl chloride (PVC) | CH2 bending CH bending C – C stretching CH2 rocking C – Cl stretching | 1424 1331, 1243 1099 965 610 |
| Low density polyethylene (LDPE) | C – H stretching CH2 bending CH2 rocking | 2914, 2848 1471 716 |
| Polypropylene (PP) | C – H stretching CH2 bending CH3 bending CH bending, CH3 rocking, C – C stretching CH3 rocking, CH3 bending, CH bending CH3 rocking, C – C stretching CH2 rocking, C- CH3 stretching CH2 rocking, C – C stretching, C – CH stretching | 2949, 2916, 2866, 2837 1455 1375 1166 997 972 840 808 |
| Polystyrene (PS) | Aromatic C – H stretching C – H stretching Aromatic ring stretching CH2 bending Aromatic CH bending Aromatic CH out-of-plane bending | 3024 2847 1601, 1492 1450 1027 695 |
| Nylon (all polyamides) | N – H Stretching CH stretching C = O stretching NH bending, C – N stretching CH2 bending NH bending, C = O bending | 3291 2930, 2857 1630 1530 1463, 1369 680 |