Supplementary Information for“Thermal-induced dielectric response in mechanically durable polyvinylidene fluoride/tubular kapok fiber encapsulated polyethylene glycol composite films”

Wenqi Wua, Xianglin Peib, Hairong Lic, Junyang Tua, Qiong Lia, Weijie Zhoua, Yutie Gonga, Ming Jianga,*, Wei Gongb,*

a State Key Laboratory for New Textile Materials & Advanced Processing Technology, School of Materials Science and Engineering, Wuhan Textile University, Wuhan 430200, PR China

b School of Materials and Architectural Engineering, Guizhou Normal University, Guiyang 550025, PR China.

c Mechanical Metrology Division, Hubei Institute of Measurement and Testing Technology, Wuhan 430223, PR China

Correspondence to M. Jiang (mjiang@wtu.edu.cn) or W. Gong (gongw@gznu.edu.cn)

Supporting Information

Figure S1 X-ray diffraction curves of PEG800, PEG 2K, PEG10K.

Table S1The proportion of PEG in KF/PEG800、KF/PEG2k and KF/PEG10k composite fibers

| Sample | PVDF/KF/PEG800 | PVDF/KF/PEG2k | PVDF/KF/PEG10k |
| --- | --- | --- | --- |
| Residual carbon rates (wt%) | 27.5 | 31 | 24 |
| PEG content（wt%） | 17.3 | 16.6 | 10.9 |

Table S2 Thermal analysis of the PVDF/KF/PEG with varying molecular weights

| Sample | Melting |  |  |  | Crystallization |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Tm(on)/℃ | Tm/℃ | Tm(end)/℃ | ΔHm /J*g-1 | Tc(on)/℃ | Tc/℃ | Tc(end)/℃ | ΔHc /J*g-1 |
| PEG800 | 17.8 | 29.9 | 37.7 | 122.78 | 11.7 | 21 | 27.0 | 118.99 |
| PEG2k | 42.4 | 53.1 | 57.2 | 181.82 | 24.9 | 29.8 | 37.6 | 179.81 |
| PEG10k | 57.5 | 61.6 | 67.9 | 255.78 | 27.3 | 36.1 | 41.9 | 254.63 |
| KF/PEG800 | 14.0 | 19.6 | 24.6 | 18.32 | 2.8 | 7.9 | 15.2 | 17.65 |
| KF/PEG2k | 49.9 | 53.8 | 64.5 | 48.05 | 23.3 | 30.4 | 37.3 | 42.24 |
| KF/PEG10k | 51.8 | 61.9 | 65.8 | 27.19 | 28.7 | 34.4 | 40.8 | 28.44 |
| PVDF/KF/PEG800 | 27.8 | 33.1 | 38.0 | 27.34 | 14.2 | 19.8 | 24.0 | 27.06 |
| PVDF/KF/PEG2k | 49.6 | 56.1 | 61.3 | 33.18 | 27.7 | 33.4 | 37.4 | 33.14 |
| PVDF/KF/PEG10k | 56.6 | 63.5 | 70.1 | 34.76 | 32.1 | 38.8 | 45.6 | 35.7 |

(d)

(c)

(b)

(a)

Figure S2 DSC cooling (a, c) and heating (b, d) curves of pristine PEG800, PEG2k, PEG10k, and their shape-stabilized KF/PEG fibers.

Figure S3 Stress-strain curve of PVDF/KF composite film with different KF content.

Figure S4 The admittance of PVDF/KF, PVDF/KF/PEG800, PVDF/KF/PEG2k and PVDF/KF/PEG10k Composite materials at 1kHz.

Table S3 PVDF/KF/PEG800, PVDF/KF/PEG2k, PVDF/KF/PEG10k composite dielectric transition-temperature data

| Sample | Theating/℃ | Tcooling/℃ | Width of the dielectric hysteresis loop |
| --- | --- | --- | --- |
| PVDF/KF/PEG800 | 11.5 | 10.8 | 0.7 |
| PVDF/KF/PEG2k | 44.1 | 34.5 | 9.6 |
| PVDF/KF/PEG10k | 60.0 | 43.5 | 16.5 |