Supplementary Information

Solvothermal synthesis and efficient visible light-driven photocatalytic property of 2-D iodoargentate hybrid directed by solvated Fe(III) cation

Hongjin Zhu, and Dingxian Jia*

College of Chemistry, Chemical Engineering and Materials Science, Soochow University, Suzhou 215123, People’s Republic of China.

Table S1. Crystallographic data of 1

| CCDC | 2528821 |
| --- | --- |
| Empirical formula | C12H36Ag10FeI13O6S6 |
| Formula weight | 3253.02 |
| Crystal system | Monoclinic |
| Space group | P21/c |
| a (Å) | 11.9829(7) |
| b (Å) | 19.7853(12) |
| c (Å) | 24.8204(15) |
| α (°) | 90 |
| β (°) | 91.480(2) |
| γ (°) | 90 |
| V (Å3) | 5882.6(6) |
| Z | 4 |
| T (K) | 296(2) |
| 2θ (max) (deg) | 50.70 |
| Total reflections | 160166 |
| Unique reflections | 10767 |
| Rint | 0.1261 |
| Reflections with [I > 2σ(I)] | 8495 |
| No. of parameters | 448 |
| R1 [I > 2σ(I)] | 0.0359 |
| wR2 [I > 2σ(I)] | 0.0752 |
| GOF on F2 | 1.032 |

Table S2. Selected Bond Lengths (Å) and Angles (deg) for 1

| Ag(1)–I(3) | 2.7895(9) | Ag(1)–I(1) | 2.8634(9) |
| --- | --- | --- | --- |
| Ag(1)–I(2) | 2.8301(9) | Ag(1)–I(4) | 2.9613(9) |
| Ag(2A)–I(1) | 3.1727(15) | Ag(2A)–I(11)#4 | 2.8207(12) |
| Ag(2A)–I(13)#6 | 2.7919(12) | Ag(2A)–I(2) | 2.8022(12) |
| Ag(2B)–I(2) | 2.884(8) | Ag(2B)–I(10)#4 | 3.234(11) |
| Ag(2B)–I(11)#4 | 2.838(8) | Ag(2B)–I(13)#6 | 2.755(8) |
| Ag(3)–I(5) | 2.7867(10) | Ag(3)–I(4) | 2.8834(9) |
| Ag(3)–I(1) | 2.8122(9) | Ag(3)–I(11)#4 | 2.8884(10) |
| Ag(4)–I(8) | 2.7637(9) | Ag(4)–I(6) | 2.8787(9) |
| Ag(4)–I(3) | 2.7720(9) | Ag(4)–I(4) | 2.9360(9) |
| Ag(5)–I(6) | 2.8350(9) | Ag(5)–I(7)#3 | 2.8669(9) |
| Ag(5)–I(1) | 2.8470(10) | Ag(6)–I(5) | 2.8405(9) |
| Ag(5)–I(7) | 2.8611(10) | Ag(6)–I(6) | 2.9649(9) |
| Ag(6)–I(9) | 2.7811(9) | Ag(7)–I(4) | 2.8990(10) |
| Ag(6)–I(7) | 2.8163(9) | Ag(7)–I(5) | 2.9344(10) |
| Ag(7)–I(10) | 2.8424(9) | Ag(8)–I(8) | 2.7511(10) |
| Ag(7)–I(6) | 2.8630(9) | Ag(8)–I(12) | 2.8095(10) |
| Ag(8)–I(11) | 2.9974(10) | Ag(9A)–I(9) | 2.7532(17) |
| Ag(8)–I(10) | 2.8623(9) | Ag(9A)–I(10) | 2.8973(13) |
| Ag(9A)–I(11) | 2.9738(19) | Ag(9A)–I(2)#1 | 2.9369(18) |
| Ag(9B)–I(11) | 2.889(13) | Ag(9B)–I(2)#1 | 2.871(13) |
| Ag(10)–I(13) | 2.8502(11) | Ag(10)–I(12) | 2.7426(11) |
| Ag(2A)–Ag(9A)#4 | 3.062(2) | Ag(10)–I(13)#5 | 2.8490(11) |
| Ag(2B)–Ag(10)#4 | 2.965(8) | Ag(2B)–Ag(9B)#4 | 2.912(15) |
| Ag(5)–Ag(5)#3 | 2.9841(14) | Ag(9A)–Ag(2A)#1 | 3.062(2) |
| Ag(10)–Ag(2B)#1 | 2.965(8) | Ag(10)–Ag(10)#5 | 3.295(2) |
| Fe(1)–O(1) | 1.988(5) | Fe(1)–O(2) | 2.032(6) |
| Fe(1)–O(3) | 1.995(6) | Fe(1)–O(4) | 1.981(6) |
| Fe(1)–O(5) | 1.992(6) | Fe(1)–O(6) | 1.983(5) |
| I(3)–Ag(1)–I(2) | 114.04(3) | I(3)–Ag(1)–I(4) | 111.81(3) |
| I(3)–Ag(1)–I(1) | 114.78(3) | I(2)–Ag(1)–I(4) | 98.70(3) |
| I(2)–Ag(1)–I(1) | 112.84(3) | I(1)–Ag(1)–I(4) | 102.90(3) |
| I(13)#6–Ag(2A)–I(2) | 112.33(4) | I(2)–Ag(2A)–I(11)#4 | 118.08(4) |
| Ag(2B)–Ag(2A)–I(11)#4 | 80.6(4) | I(13)#6–Ag(2A)–I(1) | 90.61(3) |
| I(13)#6–Ag(2A)–I(11)#4 | 121.86(4) | I(2)–Ag(2A)–I(1) | 104.93(4) |
| I(11)#4–Ag(2A)–I(1) | 102.27(4) | I(13)#6–Ag(2B)–I(11)#4 | 122.6(3) |
| I(11)#4–Ag(2B)–I(2) | 114.8(2) | I(2)–Ag(2B)–I(10)#4 | 96.1(3) |
| I(13)#6–Ag(2B)–I(10)#4 | 120.3(3) | I(13)#6–Ag(2B)–I(2) | 111.0(3) |
| I(11)#4–Ag(2B)–I(10)#4 | 87.4(2) | I(5)–Ag(3)–I(11)#4 | 110.55(3) |
| I(5)–Ag(3)–I(1) | 115.64(3) | I(1)–Ag(3)–I(11)#4 | 110.07(3) |
| I(5)–Ag(3)–I(4) | 111.91(3) | I(4)–Ag(3)–I(11)#4 | 101.44(3) |
| I(1)–Ag(3)–I(4) | 106.23(3) | I(8)–Ag(4)–I(4) | 102.00(3) |
| I(8)–Ag(4)–I(3) | 123.80(3) | I(3)–Ag(4)–I(4) | 113.10(3) |
| I(8)–Ag(4)–I(6) | 95.99(3) | I(6)–Ag(4)–I(4) | 101.79(3) |
| I(3)–Ag(4)–I(6) | 116.71(3) | I(6)–Ag(5)–I(1) | 114.12(3) |
| I(6)–Ag(5)–I(7) | 108.41(3) | I(7)–Ag(5)–I(7)#3 | 117.21(3) |
| I(1)–Ag(5)–I(7) | 110.00(3) | I(1)–Ag(5)–I(7)#3 | 101.52(3) |
| I(6)–Ag(5)–I(7)#3 | 105.63(3) | I(9)–Ag(6)–I(7) | 115.53(3) |
| I(9)–Ag(6)–I(5) | 113.63(3) | I(9)–Ag(6)–I(6) | 98.66(3) |
| I(7)–Ag(6)–I(5) | 109.58(3) | I(7)–Ag(6)–I(6) | 106.07(3) |
| I(10)–Ag(7)–I(6) | 120.24(3) | I(5)–Ag(6)–I(6) | 112.75(3) |
| I(10)–Ag(7)–I(4) | 104.38(3) | I(10)–Ag(7)–I(5) | 107.67(3) |
| I(6)–Ag(7)–I(4) | 103.09(3) | I(6)–Ag(7)–I(5) | 113.01(3) |
| I(8)–Ag(8)–I(12) | 103.22(3) | I(4)–Ag(7)–I(5) | 107.31(3) |
| I(8)–Ag(8)–I(10) | 121.55(3) | I(8)–Ag(8)–I(11) | 112.02(3) |
| I(12)–Ag(8)–I(10) | 116.21(3) | I(12)–Ag(8)–I(11) | 112.12(3) |
| I(9)–Ag(9A)–I(2)#1 | 105.97(5) | I(10)–Ag(8)–I(11) | 91.70(3) |
| I(10)–Ag(9A)–I(11) | 91.49(5) | I(9)–Ag(9A)–I(10) | 123.86(6) |
| I(9)–Ag(9A)–I(11) | 121.62(6) | I(2)#1–Ag(9A)–I(11) | 109.33(6) |
| I(9)–Ag(9B)–I(11) | 132.8(5) | I(10)–Ag(9A)–I(2)#1 | 102.63(5) |
| I(2)#1–Ag(9B)–I(11) | 113.7(4) | I(9)–Ag(9B)–I(2)#1 | 113.3(5) |
| I(12)–Ag(10)–I(13) | 121.30(4) | I(13)#5–Ag(10)–I(13) | 109.34(3) |
| I(12)–Ag(10)–I(13)#5 | 112.37(4) | Ag(3)–I(1)–Ag(2A) | 67.09(3) |
| Ag(3)–I(1)–Ag(5) | 96.60(3) | Ag(5)–I(1)–Ag(2A) | 159.94(3) |
| Ag(3)–I(1)–Ag(1) | 74.62(3) | Ag(1)–I(1)–Ag(2A) | 65.48(3) |
| Ag(5)–I(1)–Ag(1) | 99.83(3) | Ag(2A)–I(2)–Ag(1) | 71.10(4) |
| Ag(1)–I(2)–Ag(2B) | 91.5(2) | Ag(1)–I(2)–Ag(9B)#4 | 88.0(4) |
| Ag(1)–I(2)–Ag(9A) | 101.51(3) | Ag(4)–I(3)–Ag(1) | 65.79(2) |
| Ag(3)–I(4)–Ag(7) | 65.75(3) | Ag(3)–I(4)–Ag(4) | 104.03(3) |
| Ag(7)–I(4)–Ag(4) | 74.75(2) | Ag(3)–I(4)–Ag(1) | 72.11(2) |
| Ag(7)–I(4)–Ag(1) | 107.32(3) | Ag(4)–I(4)–Ag(1) | 61.62(2) |
| Ag(3)–I(5)–Ag(6) | 98.39(3) | Ag(3)–I(5)–Ag(7) | 66.48(3) |
| Ag(6)–I(5)–Ag(7) | 63.45(2) | Ag(5)–I(6)–Ag(7) | 99.41(3) |
| Ag(5)–I(6)–Ag(4) | 98.63(3) | Ag(7)–I(6)–Ag(4) | 76.18(3) |
| Ag(5)–I(6)–Ag(6) | 65.80(2) | Ag(7)–I(6)–Ag(6) | 62.80(2) |
| Ag(4)–I(6)–Ag(6) | 131.39(3) | Ag(6)–I(7)–Ag(5) | 67.45(2) |
| Ag(6)–I(7)–Ag(5)#3 | 121.01(3) | Ag(5)–I(7)–Ag(5)#3 | 62.79(3) |
| Ag(8)–I(8)–Ag(4) | 114.23(3) | Ag(9A)–I(9)–Ag(6) | 102.71(4) |
| Ag(9B)–I(9)–Ag(6) | 116.9(4) | Ag(7)–I(10)–Ag(9A) | 87.97(4) |
| Ag(7)–I(10)–Ag(8) | 93.64(3) | Ag(7)–I(10)–Ag(2B)#1 | 136.92(12) |
| Ag(8)–I(10)–Ag(9A) | 89.11(4) | Ag(2A)#1–I(11)–Ag(3)#1 | 71.13(4) |
| Ag(8)–I(10)–Ag(2B)#1 | 73.30(15) | Ag(3)#1–I(11)–Ag(9B) | 85.2(4) |
| Ag(2B)#1–I(11)–Ag(3)#1 | 91.6(2) | Ag(2A)–I(11)–Ag(9A) | 63.73(4) |
| Ag(2B)#1–I(11)–Ag(9B) | 61.1(3) | Ag(3)#1–I(11)–Ag(9A) | 98.64(3) |
| Ag(2A)#1–I(11)–Ag(8) | 96.81(4) | Ag(2B)#1–I(11)–Ag(8) | 77.40(19) |
| Ag(3)#1–I(11)–Ag(8) | 163.61(3) | Ag(9B)–I(11)–Ag(8) | 99.7(4) |
| Ag(9A)–I(11)–Ag(8) | 85.18(3) | Ag(10)–I(12)–Ag(8) | 69.58(3) |
| Ag(2B)#2–I(13)–Ag(10)#5 | 63.87(19) | Ag(2A)#2–I(13)–Ag(10) | 121.17(4) |
| Ag(2A)#2–I(13)–Ag(10)#5 | 83.75(4) | Ag(10)#5–I(13)–Ag(10) | 70.65(3) |
| O(4)–Fe(1)–O(6) | 90.4(2) | O(6)–Fe(1)–O(3) | 93.4(2) |
| O(4)–Fe(1)–O(1) | 89.2(2) | O(1)–Fe(1)–O(3) | 90.0(2) |
| O(6)–Fe(1)–O(1) | 176.5(2) | O(5)–Fe(1)–O(3) | 88.0(3) |
| O(4)–Fe(1)–O(5) | 179.0(2) | O(4)–Fe(1)–O(2) | 90.4(2) |
| O(6)–Fe(1)–O(5) | 88.7(2) | O(6)–Fe(1)–O(2) | 88.8(2) |
| O(1)–Fe(1)–O(5) | 91.7(2) | O(1)–Fe(1)–O(2) | 87.7(2) |
| O(4)–Fe(1)–O(3) | 91.6(3) | O(5)–Fe(1)–O(2) | 90.0(2) |
| O(3)–Fe(1)–O(2) | 176.9(3) |  |  |

Symmetry transformations used to generate equivalent atoms: #5 x, –y+1, z–1/2; #7 –x, y+1/2, –z+1/2; #8 –x, y–1/2, –z+1/2; #9 –x, –y, –z+1; #10 –x, –y, –z; #11 –x, –y+1/2, z+1/2.

Fig. S1. IR spectrum of 1.

Fig. S2. Simulated powder XRD patterns based on single crystal data of compound 1, and experimental powder XRD patterns of compound 1.

Fig. S3. The Ag7I7 circle in the [Ag10I13]n3n– layer showing sectional dimension in 1.