Supplementary Information
Spatial Coherence Manipulation on the Statistical 
Photonic Platform
Leixin Liu1, Wenwei Liu2,*, Fei Wang1, Hua Cheng2,*, Duk-Yong Choi4, Jianguo Tian2, Yangjian Cai1,3,*, and Shuqi Chen2,5,6,*
1School of Physical Science and Technology, Soochow University, Suzhou 215006, China

2The Key Laboratory of Weak Light Nonlinear Photonics, Ministry of Education, Renewable Energy Conversion and Storage Center, School of Physics and TEDA Institute of Applied Physics, Nankai University, Tianjin 300071, China

3Shandong Provincial Engineering and Technical Center of Light Manipulation & Shandong Provincial Key Laboratory of Optics and Photonic Device, School of Physics and Electronics, Shandong Normal University, Jinan 250014, China

4Laser Physics Centre, Research School of Physics, Australian National University, Canberra, ACT 2601, Australia

5The Collaborative Innovation Center of Extreme Optics, Shanxi University, Taiyuan, Shanxi 030006, China.

6The Collaborative Innovation Center of Light Manipulations and Applications, Shandong Normal University, Jinan 250358, China

*Corresponding author, email: wliu@nankai.edu.cn; hcheng@nankai.edu.cn; yangjiancai@suda.edu.cn; schen@nankai.edu.cn
SUPPLEMENTARY FIGURES

[image: image1.png]Q

Information Entropy

Region

o

Information Entropy

RN
o
L

o
&)
|

o
o
|

#1

#2

#3 #4
Region





Supplementary Figure 1 | Calculated information entropy of the designed statistical metasurface with different definitions. The information entropy is defined as a 
[image: image2.wmf]2

1/log

pp

-

å

 and b 
[image: image3.wmf]1/log

N

pp

-

å

 for uniformly N-divided phase in the phase interval of 0. The difference between the two definitions is different unit systems.

[image: image4.png][u(ry,0)°

0.2
7.5 10.0 125
1 X (um)
0.0{A¢ = 0.4
-20 -10 0 10 20
X (Um)
1.0 ——0=0° a 075
——6=5° =
0'8'__9=45o 50.60
06- 6 = 90° 1.5 xa]?n) 45
|——6=135°
0.4
0.2
O.O—A(p = 1.21
-20 -10 0 10 20
X (um)

[u(ry,0)°

1.0
0.8
0.6
0.4 -
0.2

] 5.0 x(?n )1o.o
0.0 0.8 "

-20 -10 0 10 20
X (Mm)
1'0—0=0° o 075

—e6=5° 2
0-8'__ 0 = 45° 30.60 \

— 0 =90° 15 3.0 45
06' 0 = 135° X (um)
0.4
0.2
00 A = 1.6 ‘

-20 -10 0 10 20

X (um)




Supplementary Figure 2 | Gaussian curve-fitting of |(r1, 0)|2 for a 0.4π, b 0.8π, c 1.2π and d 1.6π for different cut-line orientation angles , which is defined as the intersection with the y direction shown in Figure 4a. Inset: zoom in the influence of The coherence distributions for different angles with limited fluctuation results from the fabrication imperfection and are statistically analyzed to obtain the DOC. 
[image: image5.png]Fresnel Diffraction
Source




Supplementary Figure 3 | Schematic of the propagation of the generated partially coherent beams captured in different z locations.
[image: image6.png]Coherent Length (um)

2.7

oobpo — -

20 40 60 80 100 120
Z (Mm)




Supplementary Figure 4 | Theoretical and experimental results of coherent lengths at different transmission distances when the PFR covers [0, 2π]. The error bar indicates the statistical fluctuation induced by the incomplete sets of cut-lines and measurements.
[image: image7.png]Global Coherence n

1.0

—— A = 04T
—0— A = 0.8T

084 —A—Ap=1.2m
—v—A@p = 1.6m
—0— Ap =21
0.6 -
0.4 -
] —A
0.2 v
—é
0.0 -
I ' I I I I I
20 40 60 80 100 120

Z (Mm)





Supplementary Figure 5 | The global coherence of each phase distribution at different distances from the statistical metasurface. The experimental results show that the global coherence of each phase distribution increases with the increase of distance from the metasurface and finally tends to converge. It is conformed with the van Cittert-Zernike theorem1.

SUPPLEMENTARY NOTE S1: DESIGN PRINCIPLE OF PHASE DISTRIBUTIONS OF THE STATISTICAL METASURFACES

The concept of statistical metasurface is introduced to manipulate the spatial coherence of the beams, by loading a random phase distribution onto the wavefront, and performing a scanning process to obtain a series of instantaneous intensities that can be statistically analyzed. The phase distributions of the statistical metasurface can be expressed as:


[image: image8.wmf](

)

(

)

12

irandi

fpp

=-+

,                      (1)
where i denotes a parameter of coherence manipulation and rand(2iπ) is a function to generate a random distribution. Generally, the randomly distributed phase can be arbitrarily designed, leading to partially coherent beams with different coherent lengths. Specifically, we realize a statistical metasurface of 6 regions with different uniform phase distributions for 6 parameters in Eq. (1), i.e. i = 0, 0.2, 0.4, 0.6, 0.8, 1, and the corresponding phase fluctuation range (PFR) is 0, 0.4, 0.8, 1.2, 1.6, 2, respectively. 
SUPPLEMENTARY NOTE S2. NUMERICAL SIMULATION OF THE TRANSMITTED BEAM FROM THE STATISTICAL METASURFACE
To verify the convergence of the measured degree of coherence (DOC) of the generated beams, the experimental process is simulated through the commercial software MATLAB. The electric fields distribution of the source field beam is defined as:

[image: image9.wmf](

)

(

)

,exp

j

EAi

xhj

=-

,                      (2)
where Aj and φ denote the amplitude and phase of the electric fields of the light transmitting from the statistical metasurface. The source intensity with transverse coordinates (ξ , η) is defined by a function I0 (ξ , η), which locates at the plane of the statistical metasurface. The source fields propagate to the observation plane with transverse coordinates (xn , yn). Such propagation can be calculated through an ABCD optical system:

[image: image10.wmf](

)

(

)

(

)

(

)

22

22

,exp,

22

expexp

2

nn

nn

nn

ikDxy

ik

ExyE

BB

ikAikik

xydd

BBB

xh

p

xhxhxh

éù

+

êú

=

êú

ëû

éù

éùæö

´+--

ç÷

êú

êú

ëûèø

ëû

òò

 .        (3)
Generally, it is challenging to find an analytical solution of Eq. (3). To evaluate the output modes, we define a new function f:

[image: image11.wmf](

)

(

)

(

)

22

,,exp

2

ikA

fE

B

xhxhxh

éù

=+

êú

ëû

.               (4)
Substituting Eq. (4) into Eq. (3), the propagation of the source fields can be evaluated using the FFT algorithm, i.e.,


[image: image12.wmf](

)

(

)

(

)

{

}

22

,,exp,

22

nn

nnn

ikDxy

ik

ExyzFf

BB

xh

p

éù

+

êú

=

êú

ëû

,          (5)
where the operator F is the Fourier transform operator. Therefore, the ith instantaneous intensity of the partially coherent beams in the output plane can be expressed as:

[image: image13.wmf](

)

(

)

2

,,,,

innninnn

IxyzExyz

=

.                   (6)
To implement the statistical ensemble average, K instantaneous intensities are further generated with varied phase distributions in the source plane due to the random process, and the average light intensity in the observation plane can be written as:

[image: image14.wmf](

)

(

)

2

1

1

,,,,

K

nnninnn

i

IxyzExyz

K

=

=

å

.                 (7)
Moreover, the coherence of the generated beams can be calculated through:

[image: image15.wmf](

)

(

)

(

)

(

)

(

)

*

1

,,

,,

,,

K

nn

i

nnn

nn

EzEz

xyz

IzIz

m

=

éù

ëû

=

å

12

12

ρ

ρ

ρ

ρ

,              (8)
where ρ1 and ρ2 are two position vectors in the transverse plane. Equations (2)-(8) provide a convenient way to numerically study the intensity and the coherence of the generated beams in the ABCD optical system. 

An illustration of the numerical simulation process of the beam generated from the statistical metasurface is shown in Supplementary Fig. 3. The metasurface located at the source plane can generate a temporal phase distributions within a limited PFR. The transmitted light was captured by an imaging system to record the light distributions with a total number of K. By moving the imaging system along the z direction, the instantaneous intensity distributions at different distances z1, z2, …, zn are obtained and the coherent lengths of the beams at the corresponding plane are calculated, respectively. Generally, the coherent length of the light gradually increases as the transmission distance zn increases until the coherence of the light converges.
We also simulated the experimental process considering the devices parameters in our experimental setup. We chose a series of statistical metasurfaces whose phase randomly and uniformly covers the PFR with [0, 2π] to simulate the partially coherent light at different transmission distances. According to Eq. (8), we simulated the coherent lengths of the generated beams at different transmission distances (Supplementary Fig. 4), which meet well with the measured ones. The theoretical and the experimental results with the PFR of [0, 2π] show that the measured coherent length will converge when the transmission distance is large enough. The experimental results for other PFR setups at different transmission distances also verify the convergence of the DOC as shown in Supplementary Fig. 5.
SUPPLEMENTRAY VIDEO LEGENDS

Supplementary Video 1 | Measured instantaneous intensity distributions for different PFRs while scanning. The video shows the continuous instantaneous intensity distributions for the 6 regions of the statistical metasurfaces. When the scanning speed is fast enough, the intensity distribution of the generated beam will be homogeneous captured by the CCD camera in the experiment.
Supplementary Reference

1
Zernike & Frederik. The concept of degree of coherence and its application to optical problems. Physica 5, 785-795 (1938).



8

_1234567893.unknown

_1234567898.unknown

_1234567899.unknown

_1234567895.unknown

_1234567896.unknown

_1234567897.unknown

_1234567894.unknown

_1234567891.unknown

_1234567892.unknown

_1234567890.unknown

