Supplementary Information

Transmissible plasma-evolved suspended graphene near room temperature

Kamal Prasad Sharma1,2*, Aliza Khaniya Sharma1, Toru Asaka3,4, Takahiro Maruyama1,2*

1Department of Applied Chemistry, 2Nanomaterial Research Center,

Meijo University, Tempaku-ku, Nagoya 468-8502, Japan

3Department of Life Science and Applied Chemistry, 4Frontier Research Institute for

Materials Science,

Nagoya Institute of Technology, Showa-ku, Nagoya 466-8555, Japan

Supplementary Fig. 1 Schematic of a) dual arc plasma system (APS), and b) negatively biased target used in APS source.

Supplementary Fig. 2 TPEG utilizing PMMA support. a) OM image of graphene produced with Protocol P4'_Ir on SiO2/Si (PMMA was removed after transfer onto SiO2/Si using acetone), b) Raman spectra observed at various points (coloured spectra are assigned to their respective points in Fig. 2 (a)). c) OM image (coloured) of graphene after transfer onto SiO2/Si.

Supplementary Fig. 3 a) OM image of CVD graphene crystals transferred onto SiO2/Si (using the method reported elsewhere 34). b) OM image of Fig. 3a after Protocol P2_Ir plasma. c) Typical Raman spectra of CVD graphene transferred onto SiO2/Si with different treatments, as indicated by their respective colours.

Supplementary Table S1 Table showing the details of the protocols employed in this research. Raman analysis was performed after pulsed APD of each protocol (see physical state of a-C mesh on TEM grids in Extended Data Fig. 10), graphene (Gr), Partial Gr, and No Gr were defined based on the frequency of observable 2D band in Raman spectra.

| S. N. | Protocol | Element | Carbon source | APD conditions |  |  | Raman analysis |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Voltage | Pulses | Frequency |  |
| 1 | P1_Co | Co | a-C mesh of TEM grid | 70 | 3 | 3 | No Gr |
| 2 | P2_Co |  |  | 100 | 3 | 3 | Partial Gr |
| 3 | P2'_Co |  |  | 100 | 10 | 3 | Gr |
| 4 | P3_Co |  |  | 140 | 3 | 3 | Gr |
| 5 | P4_Co |  |  | 170 | 3 | 3 | Gr |
| 6 | P5_Co |  |  | 210 | 3 | 3 | Gr |
| 7 | P6_Co |  |  | 250 | 3 | 3 | Gr |
| 8 | P1_Co+W | W (+P1_Co) |  | 100 | 3 | 3 | No Gr |
| 9 | P1'_Co+W |  |  | 100 | 10 | 3 | Gr |
| 10 | P2_Co+W |  |  | 140 | 3 | 3 | Gr |
| 11 | P3_Co+W |  |  | 180 | 3 | 3 | Gr |
| 12 | P4_Co+W |  |  | 210 | 3 | 3 | Gr |
| 13 | P3'_Co+W_500oC |  |  | 180 | 3 | 3 | Gr |
| 14 | P1_Ir | Ir |  | 70 | 3 | 3 | No Gr |
| 15 | P2_Ir |  |  | 100 | 3 | 3 | Partial Gr |
| 16 | P2'_Ir |  |  | 100 | 10 | 3 | Gr |
| 17 | P3_Ir |  |  | 140 | 3 | 3 | Gr |
| 18 | P4_Ir |  |  | 170 | 3 | 3 | Gr |
| 19 | P1_Pt | Pt |  | 70 | 3 | 3 | No Gr |
| 20 | P2_Pt |  |  | 100 | 3 | 3 | Partial Gr |
| 21 | P2'_Pt |  |  | 100 | 10 | 3 | Gr |
| 22 | P3_Pt |  |  | 140 | 3 | 3 | Gr |
| 23 | P4_Pt |  |  | 170 | 3 | 3 | Gr |
| 24 | P1_W | W |  | 100 | 3 | 3 | No Gr |
| 25 | P2_W |  |  | 180 | 3 | 3 | Partial Gr |
| 26 | P3_W |  |  | 210 | 3 | 3 | Gr |
| 27 | P4_W |  |  | 250 | 3 | 3 | Gr |
| 28 | P4'_Ir | Ir | a-C on PMMA | 170 | 10 | 3 | Gr |
| 29 | P4''_Ir |  |  | 170 | 5 | 3 | Gr |