Polymer Grafting of Graphene Oxide through Esterification of Terephthalic Acid and Allyl Alcohol for Metronidazole Drug Delivery: Central Composite Design Optimization Study

Niloufar Torabi Fard a, Fariba Tadayon a,*, Homayon Ahmad Panahi b, Elham Moniri c

a Department of Chemistry, North Tehran Branch, Islamic Azad University, Tehran, Iran

b Department of Chemistry, Central Tehran Branch, Islamic Azad University, Tehran, Iran

c Department of Chemistry, Varamin (Pishva) Branch, Islamic Azad University, Varamin, Iran

*Corresponding author: F_tadayon@iau-tnb.ac.ir

The following is included as additional Supporting Information for this paper:

Figure Captions:

Fig. S1. TGA thermogram of GO/TPAA cl-poly (AA)/TPA.

Fig. S2. XRD pattern of GO/TPAA cl-poly (AA)/TPA.

Fig. S3. FT-IR spectra of GO/TPAA (a) and GO/TPAA cl-poly (AA)/TPA (b).

Fig. S4. N2 adsorption–desorption isotherm of GO/TPAA cl-poly (AA)/TPA.

Fig. S5. plot of ln (KL) versus 1/T.

Fig. S6. Influence of reusability on MNZ adsorption.

Table captions:

Table S1. Isotherm model parameters for the adsorption of MNZ onto GO/TPAA cl-poly (AA)/TPA.

Table S2. Kinetic model parameters for the adsorption of MNZ onto GO/TPAA cl-poly (AA)/TPA.

Table S3. Thermodynamics parameters for the adsorption of MNZ onto GO/TPAA cl-poly (AA)/TPA.

Table S4. Results of the correlation coefficients and rate constants of different models for release curve of MNZ from GO/TPAA cl-poly (AA)/TPA (pH=1.2 and 7.4).

Fig. S1

Fig. S2

Fig. S3

Fig. S4

Fig. S5

Fig. S6

Table S1

| Model | Parameter T=298.15K |  | Value T= 308.15 K T= 323.15K |  |
| --- | --- | --- | --- | --- |
| Langmuir | qm (mg g-1) kl (L mg-1) Rl R2 | 7.776 0.024 0.287 0.9956 | 10.582 0.043 0.186 0.9932 | 11.098 0.109 0.083 0.9913 |
| Ferundlich | n Ln(kf) kf(mg11/nL1/ng-1) R2 | 1. 508 -1.088 0.336 0.9947 | 1.594 -0.32 0.726 0.9836 | 1.692 0.301 1.351 0.9885 |
| Temkine | B AT (L mg-1) R2 | 1.295 0.419 0.9515 | 2.227 0.469 0.9945 | 2.433 1.061 0.9828 |
| Dubinin-Radushkevich | Kad (mol2 kJ-2) Ln (qs) qs (mg g-1) R2 | 0.00002 1.344 3.834 0.8863 | 0.000007 1.735 5.672 0.9141 | 0.000002 1.901 6.694 0.8406 |

Table S2

| Model | Parameter | Value |
| --- | --- | --- |
| Pseudo-first-order model | qe (mg g-1) K1 (min-1) R2 | 4.073 0.0039 0.9486 |
| Pseudo-second-order model | qe (mg g-1) K2 (g mg-1min-1) R2 | 1.694 1.779 0.9999 |
| Intra-particle diffusion | Ki (g mg-1min-1/2) Ci (mg g-1) R2 | 0.081 1.365 0.9419 |

Table S3

| Sample | Temperature (K) | ΔHo (J mol-1) | ΔSo (J mol-1 K-1) | ΔGo (J mol-1) |
| --- | --- | --- | --- | --- |
| GO/TPAA cl-poly (AA)/TPA | 298.15 308.15 323.15 | 47637.56 | 186.2918 | -7.905 -9.768 -12.562 |

Table S4

| Zero order pH=1.2 pH=7.4 | First order pH=1.2 pH=7.4 | Higuchi pH=1.2 pH=7.4 | Korsmeyer – Peppas pH=1.2 pH=7.4 |
| --- | --- | --- | --- |
| K0 R2 K0 R2 | K1 R2 K1 R2 | KH R2 KH R2 | n KKP R2 KKP R2 |
| 5.226 0.9919 5.362 0983 | 0.151 0.9562 0.255 0.9863 | 34.579 0.9871 34.03 0.9286 | 0.5 34.077 0.9889 34.03 0.9286 0.6 26.015 0.9937 26.132 0.9441 0.7 20.318 0.9962 20.525 0.9571 0.8 16.118 0.9966 16.37 0.9679 0.9 12.928 0.9951 13.198 0.9765 1 10.454 0.9919 10.724 0.9830 |