Supplementary Data

(b)

(a)

Figure 1 : Acidic digestion of blood with acids (HCl and HNO3) was observed at 0h and 24 h.  a) shows the clumping of blood with acids at 0h. b) shows the digestion of blood with acids at 24h.

(b)

(a)

Figure 2: Alkaline digestion of blood with bases (NaOH and KOH) was observed at 0h and 24h. a) shows the clumping of blood with bases at 0h. b) shows the complete digestion of blood with bases at 24h.

(a)

(b)

(d)

(c)

Figure 3 : Acid digestion of normal and immunocompromised blood sample using 1M HNO3 at 4x. (a) No digestion in normal blood sample at 0h of incubation at 37 °C. (b) Partial digestion in normal blood sample at 24h of incubation at 37°C with elongated fibrous microplastic-like fragments. (c) No digestion and clumping found in immunocompromised blood sample at 0h of incubation at 37°C. (d) Partial digestion and small residues in immunocompromised blood sample at 24h of incubation at 37°C. Arrow indicates microplastic fragments.

(b)

(a)

(d)

(c)

Figure 4 : Alkaline digestion of normal and immunocompromised blood sample using 1M sodium hydroxide (NaOH) at 10x by light microscope. (a) Normal blood sample showed thread-like tendencies of branching structures with no digestion (b) This microscopic image shows incomplete digestion of organic matter. (c) At 0h, dense, web-like filamentous structures with early branching patterns observed showing no digestion in immunocompromised blood samples. (d) After 24h, least digestion appears showing coagulated residue and thickened filamentous networks.

(b)

(a)

(d)

(c)

Figure 7 : Alkaline digestion of normal and immunocompromised blood sample using 1.8 M Potassium hydroxide (KOH) at 10x. (a) Indigested plasma components forming delicate and dense branching patterns across the slide showing no digestion. (b) The filamentous residues appear thin and discontinuous, indicating no digestion. (c) At 0h, no digestion in immunocompromised blood sample appears. (d) After 24 h of alkaline digestion, least digestion and small residues was observed in immunocompromised blood samples. Arrow indicates microplastic fragments.

Table 1: The table shows FTIR Results of MP polymers that met the LOQ threshold. Additional columns determine the Limit of Quantification and Limit of Detection values.

| Polymer and Sample ID | Polymer quantity in 0.5 mL samples (A) | Mean polymer quantity in parallel controls ±SD (B) | Blank Correction (A-B) (C) | Limit of Detection 4*SD of B (LoD) | Limit of Quantification 10*SD of B (LoQ) | LoQ corrected value/10g of blood sample |
| --- | --- | --- | --- | --- | --- | --- |
| PAM 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33 NaOH 34 NaOH 35 KOH | 67 82 63 78 74 79 73 60 75 76 71 70 77 85 74 | 0.004±0.0015 | 66.996 81.996 62.996 77.996 73.996 78.996 72.996 59.996 74.996 75.996 70.996 69.996 76.996 84.996 73.996 | 0.006 | 0.015 | 66.996 81.996 62.996 77.996 73.996 78.996 72.996 59.996 74.996 75.996 70.996 69.996 76.996 84.996 73.996 |
| PBT 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33 NaOH 34 NaOH 35 KOH | 67 65 49 73 57 70 57 67 72 71 | 0.0035±0.0011 | 66.9965 64.9965 47.9965 72.9965 56.9965 69.9965 56.9965 66.9965 71.9965 70.9965 | 0.0044 | 0.011 | 66.9965 64.9965 47.9965 72.9965 56.9965 69.9965 56.9965 66.9965 71.9965 70.9965 |
| PVC 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 61 53 63 59 54 61 62 | 0.0042±0.0015 | 60.9958 52.9958 62.9958 58.9958 53.9958 60.9958 61.9958 | 0.006 | 0.015 | 60.9958 52.9958 62.9958 58.9958 53.9958 60.9958 61.9958 |
| PU 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 57 65 61 61 | 0.003±0.0007 | 56.997 64.997 60.997 60.997 | 0.0028 | 0.007 | 56.997 64.997 60.997 60.997 |
| PE Rubber 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 56 | 0.0042±0.0011 | 55.9958 | 0.0044 | 0.011 | 55.9958 |
| PA 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 55 57 65 61 64 | 0.003±0.001 | 54.997 56.997 64.997 60.997 63.997 | 0.004 | 0.01 | 54.997 56.997 64.997 60.997 63.997 |
| PAr 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 65 67 60 79 57 71 76 69 54 65 74 80 56 | 0.005±0.003 | 64.995 66.995 59.995 78.995 56.995 70.995 75.995 68.995 53.995 64.995 73.995 79.995 55.995 | 0.012 | 0.03 | 64.995 66.995 59.995 78.995 56.995 70.995 75.995 68.995 53.995 64.995 73.995 79.995 55.995 |
| PA6/PCL 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 59 70 55 67 67 65 62 66 67 56 | 0.003±0.0015 | 58.997 69.997 54.997 66.997 66.997 64.997 61.997 65.997 66.997 55.997 | 0.006 | 0.015 | 58.997 69.997 54.997 66.997 66.997 64.997 61.997 65.997 66.997 55.997 |
| PPS 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 50 | 0.0042±0.0008 | 49.9958 | 0.0032 | 0.008 | 49.9958 |
| PIB 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 50 | 0.004±0.0015 | 49.996 | 0.006 | 0.015 | 49.996 |
| PVA 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 54 | 0.006±0.003 | 53.994 | 0.012 | 0.03 | 53.994 |
| Copolymer 3 HNO3 6 HCL 8 KOH 11NaOH 20 HCL 22 HCL 25 NaOH 26 KOH 28 HNO3 30 HCL 32 HCL 33 HCL 33NaOH 34 NaOH 35 KOH | 50 50 | 0.003±0.001 | 49.997 49.997 | 0.004 | 0.01 | 49.997 49.997 |

Calculation 1:  Conventional Pellet Mass–Based Quantification

Table 2: Reporting the number of MPs found in the blood sample of healthy and immune-compromised patients. All Polymer types that met the LOQ criteria are displayed in units of no. of MP/L.

| Sample ID | PAM | PBT | PVC | PU | PE | PA | PAr | PA6/ PCL | PPS | PIB | PVA | Copolymer |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3 HNO3 | 2680 | 2680 | 2440 | 2280 | 2240 | _ | 2600 | 2360 | _ | _ | _ | _ |
| 6HCL | 4920 | 3900 | _ | _ | _ | 3300 | 4020 | 4200 | _ | _ | _ | _ |
| 8KOH | 2520 | 1960 | 2120 | _ | _ | _ | 2400 | 2200 | 2000 | 2000 | _ | _ |
| 11NaOH | 1560 | 1460 | _ | 1300 | _ | _ | 1580 | 1340 | _ | _ | _ | _ |
| 20HCL | 4440 | 3420 | _ | _ | _ | - | 3420 | _ | _ | _ | _ | _ |
| 22HCL | 4740 | _ | 3780 | _ | _ | 3420 | 4260 | 4020 | _ | _ | _ | _ |
| 25NaOH | 1460 | _ | _ | _ | _ | 1300 | 1520 | _ | _ | _ | _ | _ |
| 26KOH | 3600 | _ | _ | _ | _ | _ | _ | _ | _ | _ | _ | _ |
| 28HNO3 | 3000 | 2800 | 2360 | 2440 | _ | _ | 2760 | 2600 | _ | _ | _ | _ |
| 30HCL | 6080 | 4560 | _ | _ | _ | - | _ | _ | _ | _ | _ | _ |
| 32HCL | 4260 |  | 3240 | _ | _ | 3660 | 3240 | _ | _ | _ | 3240 |  |
| 33NaOH | 1540 | 1440 | 1240 | 1220 | _ | 1280 | 1480 | 2680 | _ | _ | _ | _ |
| 34NaOH | 3400 | 2840 | _ | _ | _ | _ | 3200 | 2680 | _ | _ | _ | 2000 |
| 35KOH | 2960 | _ | _ | _ | _ | _ | 2240 | 2240 | _ | _ | _ | _ |

Calculation 2 Modified Residue-Corrected Polymer Mass Quantification Approach

Table 3 : Reporting the number of MPs found in the blood sample of healthy and immune-compromised patients by FTIR Spectroscopy. All Polymer types that met the LOQ criteria are displayed in units of MP/L.

| Sample ID | PAM | PBT | PVC | PU | PE | PA | PAr | PA6/ PCL | PPS | PIB | PVA | Copolymer |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3 HNO3 | 1876 | 1876 | 1708 | 1596 | 1568 | _ | 1820 | 1652 | _ | _ | _ | _ |
| 6HCL | 3444 | 2730 | _ | _ | _ | 2310 | 2814 | 2940 | _ | _ | _ | _ |
| 8KOH | 252 | 196 | 212 | _ | _ | _ | 240 | 220 | 200 | 200 | _ | _ |
| 11NaOH | 156 | 146 | _ | 130 | _ | _ | 158 | 134 | _ | _ | _ | _ |
| 20HCL | 3700 | 2850 | _ | _ | _ | - | 2850 | _ | _ | _ | _ | _ |
| 22HCL | 2370 | _ | 1890 | _ | _ | 1710 | 2130 | 2010 | _ | _ | _ | _ |
| 25NaOH | 1460 | _ | _ | _ | _ | 1300 | 1520 | _ | _ | _ | _ | _ |
| 26KOH | 840 | _ | _ | _ | _ | _ | _ | _ | _ | _ | _ | _ |
| 28HNO3 | 2100 | 1960 | 1652 | 1708 | _ | _ | 1932 | 1820 | _ | _ | _ | _ |
| 30HCL | 5320 | 3990 | _ | _ | _ | - | _ | _ | _ | _ | _ | _ |
| 32HCL | 2130 |  | 1620 | _ | _ | 1830 | 1620 | _ | _ | _ | 1620 |  |
| 33NaOH | 1540 | 1440 | 1240 | 1220 | _ | 1280 | 1480 | 2680 | _ | _ | _ | _ |
| 34NaOH | 2890 | 2414 | _ | _ | _ | _ | 2720 | 2278 | _ | _ | _ | 1700 |
| 35KOH | 2516 | _ | _ | _ | _ | _ | 1904 | 1904 | _ | _ | _ | _ |