Table S1. Energy characteristics [Lifshitz–van der Waals (ϒLW), electron-donor (ϒ-), and electron-acceptor (ϒ+) parameters (mJ m-2)] of the liquids used

| Liquids | Surface energy parameters (mJ m-2) |  |  |
| --- | --- | --- | --- |
|  | ϒ LW | ϒ+ | ϒ- |
| Water (θw) | 21.8 | 25.5 | 25.5 |
| Formamide (θF) | 38.7 | 2.3 | 39.4 |
| Diiodomethane (θD) | 50.5 | 0.7 | 0 |

Table S2. Variables and levels used in the screening design for factors affecting the biosorption capacity of AR14.

| Test variables | Temperature (ºC) (A) |  | pH (B) | Yeast dosage (g L-1) (C) | Shaking speed (rpm) (D) | Dye (mg L-1) (E) | Time (h) (F) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Low level (-) |  | 25 | 3 | 0.5 | 0 | 50 | 2 |
| High level (+) |  | 37 | 7 | 0.2 | 120 | 200 | 8 |

Table S3. Process variables used in Box-Behnken design, with 3 design factors and one optimization parameters

| Name | Units | Type | -1 | 0 | +1 |
| --- | --- | --- | --- | --- | --- |
| Dye concentration (A) | mg L-1 | Factor | 50 | 125 | 200 |
| Biomass dosage (B) | g L-1 | Factor | 0.5 | 1 | 2 |
| pH (C) | --- | Factor | 3 | 5 | 7 |
| Decolorization (D%) | (%) | Response |  |  |  |