# Optimization and Life-Cycle Assessment of Biochar Production through Microwave–Assisted Pyrolysis of Industrial Hemp Hurd

Nived S Menon1, Rejeti Venkat Srinadh1, Neelancherry Remya1*

1School of Infrastructure, Indian Institute of Technology Bhubaneswar, Argul, Odisha, 752050, India.

*Corresponding author: remya@iitbbs.ac.in

# Figures

Fig.  1 Schematic diagram of MAP setup

# Tables

Table S1. Fit summary of developed model for HB yield and HHV

|  | Linear |  | 2FI |  | Quadratic |  | Cubic |  | Lack of Fit |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | p-value | R2 | p-value | R2 | p-value | R2 | p-value | R2 | F-value | p-value |
| HB yield | 0.0002 | 0.81 | 0.2024 | 0.84 | < 0.0001 | 0.99 | 0.1140 | 0.99 | 3.82 | 0.1140 |
| HHV | 0.0059 | 0.57 | 0.7392 | 0.53 | < 0.0001 | 0.98 | 0.1031 | 0.99 | 4.10 | 0.1031 |

Table S2 Validation of the model for HB yield and HHV

| MW Power (W) | Time (min) | HB yield (%) |  |  | HHV (MJ/kg) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Observed | Predicted | Error | Observed | Predicted | Error (%) |
| 700 | 17.5 | 35.2 | 29.7 | 5.5 | 13.0 | 12.2 | 6.5 |
| 500 | 10 | 88.6 | 93.7 | 5.1 | 14.4 | 14.8 | 2.7 |
| 1000 | 15 | 8.7 | 12.5 | 3.8 | 25.4 | 27.2 | 6.6 |
| Average Error |  |  |  | 4.8 |  |  | 5.2 |

Table S3 Various solutions based on the optimization of biochar yield and HHV

| Number | MP (W) | Residence time (mins) | Yield (%) | HHV (MJ/kg) | Desirability |
| --- | --- | --- | --- | --- | --- |
| 1 | 1000 | 7 | 37.6 | 24.9 | 0.52 |
| 2 | 500 | 12.3 | 75.3 | 15.1 | 0.38 |
| 3 | 500 | 12.8 | 77.9 | 15.1 | 0.38 |
| 4 | 1000 | 30 | 16.8 | 29.5 | 0.31 |

Table S4. Data related to EF estimation

| Feedstock Type | Woody residue |
| --- | --- |
| Carbonization Method | Closed carbonization (MAP) |
| Carbonization Scale | Unspecified |
| Amount of HH (MHH) | 100 t/yr |
| Moisture content of HH (m) | 9.85 % |
| EF (without surplus energy utilization) [Class 6] | 0.10 |
| EF (with surplus energy utilization) [Class 17] | -0.78 |
| HB yield in terms of dry weight of HH | 41.7 % |
| Scenario specific annual HB Production (MHB) | 4.11 t/yr |
| Utilization rate (u) | 100 % |

Table S5. Impact result using ReCiPe Midpoint (H)

| Name | Impact result | Unit |
| --- | --- | --- |
| Fine particulate matter formation | 0.66 | kg PM2.5 eq. |
| Fossil resource scarcity | 28.23 | kg oil eq. |
| Freshwater ecotoxicity | 4.92 | kg 1,4-DCB |
| Freshwater eutrophication | 0.16 | kg P eq. |
| Global warming | 167.35 | kg CO2 eq. |
| Human carcinogenic toxicity | 4.96 | kg 1,4-DCB |
| Human non-carcinogenic toxicity | 3199.92 | kg 1,4-DCB |
| Ionizing radiation | 5.38 | kBq Co-60 eq. |
| Land use | 1437.69 | m2a crop eq. |
| Marine ecotoxicity | 7.39 | kg 1,4-DCB |
| Marine eutrophication | 1.14 | kg N eq. |
| Mineral resource scarcity | 18.94 | kg Cu eq. |
| Ozone formation, Human health | 2.01 | kg NOx eq. |
| Ozone formation, Terrestrial ecosystems | 2.63 | kg NOx eq. |
| Stratospheric ozone depletion | 0.003 | kg CFC11 eq. |
| Terrestrial acidification | 3.99 | kg SO2 eq. |
| Terrestrial ecotoxicity | 2380.14 | kg 1,4-DCB |
| Water consumption | 0.78 | m3 |

Table S6. Environmental impacts by different stages of HB production

| Groups | Global warming potential (kg CO2 eq.) | Ozone depletion (kg CFC-11-eq.) | Photochemical oxidant (kg ethylene-eq.) | Acidification (kg SO2-eq.) | Eutrophication (kg P-eq.) |
| --- | --- | --- | --- | --- | --- |
| Hemp farming | -2.94 | 0 | 1.11*10-3 | 9.13*10-3 | 0 |
| Harvesting | 80.83 | 1.11*10-8 | 0.13 | 4.50 | 3.13*10-2 |
| Transportation | 47.83 | 3.53*10-7 | 0.28 | 0.36 | 1.04*10-3 |
| MAP | 0 | 0 | 1.99 | 0 | 0 |
| Allied | 37.48 | 1.35*10-5 | 5.32*10-2 | 0.18 | 4.29*10-2 |

Table S7. Sensitivity analysis

|  |  | Hemp farming | Harvest | Transportation | Electricity | MAP | Allied |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Global warming potential (kg CO2 Eq) | EDIP | -2.94 | 80.31 | 48.14 | 0.08 | 49.58 | 37.67 |
|  | CML 2001 | -2.94 | 80.83 | 47.96 | 0.08 | 0 | 37.64 |
|  | ReCiPe Midpoint (H) | -2.94 | 80.83 | 47.83 | 0.08 | 0 | 37.48 |
|  | ILCD 2.0 2018 | -2.94 | 80.83 | 47.98 | 0.10 | 0 | 38.62 |
| Ozone depletion (kg CFC-11-Eq) | EDIP | 0 | 1.06*10-8 | 3.24*10-7 | 4.27*10-10 | 0 | 1.21*10-5 |
|  | CML 2001 | 0 | 1.11*10-8 | 3.53*10-7 | 4.88*10-10 | 0 | 1.35*10-5 |
|  | ReCiPe Midpoint (H) | 0 | 1.11*10-8 | 3.53*10-7 | 4.89*10-10 | 0 | 1.35*10-5 |
|  | ILCD 2.0 2018 | 0 | 1.40*10-8 | 4.34*10-7 | 5.69*10-10 | 0 | 1.63*10-5 |
| Photo-chemical oxidant (kg ethylene-Eq) | EDIP | - | - | - | - | - | - |
|  | CML 2001 | 0 | 1.22*10-5 | 3.21*10-3 | 1.16*10-5 | 2.84 | 1.23*10-2 |
|  | ReCiPe Midpoint (H) | 1.11*10-3 | 0.13 | 0.28 | 1.95*10-5 | 1.99 | 5.32*10-2 |
|  | ILCD 2.0 2018 | 1.11*10-3 | 0.13 | 0.28 | 1.95*10-5 | 1.99 | 5.32*10-2 |
| Acidification (kg SO2-Eq) | EDIP | 7.86*10-3 | 3.53 | 0.45 | 3.06*10-5 | 0 | 0.19 |
|  | CML 2001 | 6.32*10-3 | 2.98 | 0.33 | 2.78*10-5 | 0 | 0.20 |
|  | ReCiPe Midpoint (H) | 9.13*10-3 | 4.50 | 0.36 | 2.72*10-5 | 0 | 0.18 |
|  | ILCD 2.0 2018 | 1.13*10-2 | 5.56 | 0.48 | 3.57*10-5 | 0 | 0.24 |
| Eutro-phication ($kg PO4-Eq, &kg P-Eq) | EDIP | - | - | - | - | - | - |
|  | $CML 2001 | 1.50*10-3 | 2.46 | 8.15*10-2 | 1.02*10-5 | 0 | 5.61*10-2 |
|  | &ReCiPe Midpoint (H) | 0 | 3.13*10-2 | 1.04*10-3 | 6.75*10-6 | 0 | 4.29*10-2 |
|  | &ILCD 2.0 2018 | 0 | 3.13*10-2 | 1.03*10-3 | 6.74*10-6 | 0 | 4.28*10-2 |