Table 1. Chemical composition of the alloy used (in weight percent)

| Al | Si | Fe | Mg |
| --- | --- | --- | --- |
| rest | 5.13 | 0.16 | 7.76 |

Table 2. Relationship between Mg2Si particle size in the inner layer of the Al-13.8%Mg₂Si and Al-13.8%Mg2Si-Zr cast cylinders after centrifugal casting

|  | Inner layer (μm) |
| --- | --- |
| Al-13.8%Mg₂Si | 43.59±9.83 |
| Al-13.8%Mg2Si-Zr | 16.23±6.19 |