
Table 1. Chemical composition of the alloy used (in weight percent)
	Al
	Si
	Fe
	Mg

	rest
	5.13
	0.16
	7.76




[bookmark: _Ref235294728]Table 2. Relationship between Mg2Si particle size in the inner layer of the Al-13.8%Mg₂Si and Al-13.8%Mg2Si-Zr cast cylinders after centrifugal casting  
	
	Inner layer (μm)

	Al-13.8%Mg₂Si
	43.59±9.83

	Al-13.8%Mg2Si-Zr
	16.23±6.19




