Table 1: Materials description and Processing details

| SS316L Composition of alloying elements (SUBSTRATE) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ni | P | Cr | Fe |  | Si | C | Mn | S |  | Mo |  | N |
| 13.00 | 0.05 | 18.00 | Balance |  | 1.00 | 0.03 | 2.00 | 0.02 |  | 2.50 |  | 0.10 |
| Ball Milling Process |  |  |  |  |  | Material Combination |  |  |  |  |  |  |
| Milling Time | 40 minutes*3 times interval = 120 Minutes |  |  |  |  | # AL (325 Mesh) Fine | # Mg (36 Mesh) Course |  | # Al2O3 (Nano-Powder) |  | # SiC (Nano-Powder) |  |
| Idle Duration Interval |  |  |  | 01 Hour |  | 94% | 4% |  | 2% |  | - |  |
| Weight Ratio |  |  |  | 1:10 |  | 94% | 4% |  | - |  | 2% |  |
| Perforation of Substrate |  |  |  |  |  | Compaction & Heating |  |  |  |  |  |  |
| Dimension | SS316L(30x30mm2) |  |  |  |  | Initial Compaction (UTM) |  |  | 22.2 MPa |  |  |  |
|  | 0.8mm diameter, 4x4 matrix |  |  |  |  | Thickness between substrate |  |  | 02 mm |  |  |  |
| Technique Used | Fiber laser technique (HSG 1000W G4015C) |  |  |  |  | Material for Slurry | Gelatin Gel |  | Inert Gas Used during Heating |  |  | Argon |
| Polishing & Buffing (Grade) |  | 150 | 320 | 600 |  | Processing Temperature | 1100-1380 ºC (Industrial Muffle Furnace) |  |  |  |  |  |
| Copper Sulphate test methodology for corrosion analysis (CuST) |  |  |  |  |  |  |  |  |  |  |  |  |
| Solution Preparation Constituents |  |  |  | Mixing Time |  | Dilution by Wt. | Continuous Swabbing of the Surface |  | Copper deposits indicate the presence of metallic ions |  |  |  |
| 08 gm CuSO4 + 2ml H2SO4 +500 ml Distilled water |  |  |  | 05 Minutes |  | 1.6% | 06 minutes |  |  |  |  |  |

Table 2: Elemental distribution for the EDX analysis for the clad surfaces after corrosion

| Particular | Elements by wt. % |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Combination↓ | C | O | Al | Si | Cr | Cu | S |
| 2%Al2O3-4%Mg-SS316L | 41.08 | 10.25 | 0.9 | 0.93 | 12.72 | 32.17 | 1.95 |
| 2%SiC-4%Mg-SS316L | 34.03 | 8.01 | 1.61 | 0.8 | 14.06 | 38.3 | 3.2 |

Table 3: XRD evaluation for the 2%Al2O3/SiC-4%Mg-SS316L combinations

| Combination | Phase Identified/Evaluation |
| --- | --- |
| 2%Al2O3-4%Mg-SS316L | Al+α-Al2O3, CrO2, CuO, Al2O3-Mg, Cu-Al2O |
| 2%SiC-4%Mg-SS316L | Al+SiO2, CuO, CrO2 , Cu-Mg2.5O, AlCr2, Si2CMg |