Support Information

Pressure-Stabilized MnSb2 with Complex Incommensurate Magnetic Order

Mingyu Xu1,2,3, Matt Boswell1,4, Qing-Ping Ding2, Peng Cheng1, Aashish Sapkota2,3, Qiang Zhang4, Danielle Yahne4, Sergey. L. Bud’ko2, 3, Yuji Furukawa2,3, Raquel A. Ribeiro2,3, Paul. C. Canfield2,3, Weiwei Xie1*

1Department of Chemistry, Michigan State University, East Lansing, Michigan 48824, USA

2Ames National Laboratory, Iowa State University, Ames, Iowa 50011, USA

3Department of Physics and Astronomy, Iowa State University, Ames, Iowa 50011, USA

4Neutron Scattering Division, Oak Ridge National Laboratory, Oak Ridge, Tennessee 37831, USA

Corresponding Authors: Weiwei Xie (xieweiwe@msu.edu)

Table of Contents

Table S1  The crystal structure and refinement of MnSb2 ……………….….…...........…………..S2

Table S2  Atomic coordinates of MnSb2 ……………….….….….….…...….…...........…………..S2

Table S3  Calculated the total energy of different magnetic models……...………….….….….……..S2

Fig. S1. Powder XRD results from the different batches…………………….…...........…………..S3

Fig. S2. M(H) data of single crystals and polycrystals at 300K………………...........…………….S4

Fig. S3. Heat capacity and entropy analysis and M(T) measurements ………............…………….S5

Fig. S4. PXRD results for the same batches……………………...…………..............…………….S6

Fig. S5. NMR spectrum of polycrystalline samples at 4.2K…...…….………............…………….S7

Fig. S6. Rietveld refinement of the 300 K powder neutron diffraction data for MnSb2…………...S9

Table S4  Refined atomic coordinates of MnSb2 using neutron diffraction at 300 K…………….S10

Table S5  Basis vectors for the space group Pnnm at 300 K…….….….….….............……..……S10

Table S7  Basis vectors for the space group P1 at 200 K……………………….….….…………S11

Fig. S7. The single crystal X-ray diffraction sample picture and synthesis design of MnSb2…....S12

References…………………………………………………………...……………………………S13

Table S1. The crystal structure and refinement of MnSb2 at room temperature. Values in parentheses are estimated standard deviation from refinement.

| Chemical Formula | MnSb2 |
| --- | --- |
| Formula Weight | 298.44 g/mol |
| Space Group | Pnnm |
| lUnit Cell dimensions | a = 6.0227(3) Å b = 6.8893(3) Å c = 3.3240(2) Å |
| Volume | 137.918(12) Å3 |
| Density (calculated) | 7.186 g/cm3 |
| Absorption coefficient | 23.579 mm−1 |
| F (000) | 254 |
| 2θ range | 9.00 to 80.26° |
| Reflections collected | 3540 |
| Independent reflections | 478 [Rint = 0.0561] |
| Refinement method | Full-matrix least-squares on F2 |
| Data/restraints/parameters | 478/0/11 |
| Final R indices | R1 (I>2σ(I)) = 0.0282; wR2 (I > 2 σ(I)) = 0.0795 R1 (all) = 0.0289; wR2 (all) = 0.0799 |
| Largest diff. peak and hole | +2.072 e-/Å3 and -1.637 e-/Å3 |
| R. M. S. deviation from mean | 0.428 e-/Å3 |
| Goodness-of-fit on F2 | 1.229 |

Table S2. Atomic coordinates and equivalent isotropic atomic displacement parameters (Å2) MnSb2. (Ueq is defined as one-third of the trace of the orthogonalized Uij tensor.) Values in parentheses are estimated standard deviations from refinement.

| Atoms | Wyck. | x | y | z | Occ. | Ueq |
| --- | --- | --- | --- | --- | --- | --- |
| Sb | 4g | 0.17921(5) | 0.36252(4) | 0 | 1 | 0.01228(11) |
| Mn | 2a | 0 | 0 | 0 | 1 | 0.01182(17) |

Table S3. Calculated the total energy of different magnetic models.

|  | NM | FM | AFM |
| --- | --- | --- | --- |
| Magnetic Model |  |  |  |
| Total Energy | 0 meV | -69.68 meV | -80.79 meV |

Figure S1, Powder XRD results from the different batches. The sample for XRD is a part of the chunk directly from synthesis without the separation of single crystals.

Figure S1 shows the powder XRD results from the different batches. The sample for XRD is a part of the chunk directly from synthesis without the separation of single crystals. To complete the reaction of Mn, a small excess of Sb (~1 wt%) was added.

Figure S2, M(H) data of single crystals and polycrystals at 300 K. The mole ratio of Mn1.1Sb is estimated by assuming all the ferromagnetic single crystals come from Mn1.1Sb.

Figure S2 shows M (H) data of single crystals and polycrystals at 300 K. The mole ratio of Mn1.1Sb is estimated by assuming all the ferromagnetic single crystals come from MnSb.

Figure S3, Temperature-dependent specific heat was measured in the temperature range from 150 K to 280 K and 2 K to 200 K. The measurement is taken on the N-grease with addenda taken with the same data points as the sample measurements in the temperature range from 150 K to 280 K. There is no clear difference between the field at 0 Oe or 90 kOe. Magnetic entropy is calculated with reference to FeSb2.

Figure S4. Powder XRD results from the same batch. The interval of the time is around six months. The highest intensity peak normalizes the intensity.

To assess the ambient stability of MnSb2 over time, Figure S4 shows the normalized powder X-ray diffraction (XRD) patterns of the same sample batch measured immediately after synthesis (black) and after six months of air exposure at room temperature (red). Despite MnSb2 being a metastable phase at ambient pressure, no discernible changes in the diffraction pattern are observed, indicating that the phase remains structurally stable under ambient conditions for 6 months. This result suggests that MnSb2 is stable at or below room temperature, with no evidence of decomposition or transformation over six months.

Figure S5. (a) NMR spectrum measured at T = 4.2 K by sweeping the magnetic field on polycrystalline powder samples. (b) Zero-field NMR spectrum at T = 4.2 K on polycrystalline powder samples.

We attempted to get information about the magnetic ground state of MnSb2 from 55Mn, 121Sb, and 123Sb NMR measurements at a low temperature of T = 4.2 K using the same sample from neutron diffraction measurements.  Figure S5a shows the NMR spectrum, where a very broad spectrum from the highest magnetic field of our magnet (8.25 T) to zero field was observed.  The relatively sharp lines detected from 5.5 T to 7.5 T (indicated by the red arrows) were assigned to a typical quadrupolar split 121Sb NMR power lines from the impurity of Sb metal1. The intrinsic broad spectrum indicates that the hyperfine fields at the Mn and Sb sites are widely distributed in the magnetically ordered state, consistent with the inhomogeneous magnetic state as determined by the neutron diffraction measurements. Such an inhomogeneous magnetic state is also suggested by the very broad zero-field NMR spectrum shown in Figure S5b. The signals around 250-260 MHz and 200-230 MHz are from 55Mn and 123Sb, respectively, in the impurity of the ferromagnetic Mn1.1Sb2.  Although the broad spectrum is not fully resolved at present, we consider that the signals below 200 MHz are due to 55Mn and 121Sb NMR signals in antiferromagnetically ordered MnSb2. This again suggests the large distributions of hyperfine fields at the Mn and Sb sites, consistent with the NMR spectrum, indicating the inhomogeneous magnetic state.

To investigate the possibility that high-pressure synthesized MnSb2 exhibits magnetic ordering above room temperature (Tn > 300 K), powder neutron diffraction measurements were conducted to detect either additional magnetic Bragg reflections or intensity enhancements of the nuclear Bragg peaks consistent with the Pnmm crystal symmetry. In general, antiferromagnetic (AFM) ordering gives rise to new magnetic reflections, while ferromagnetic ordering manifests as enhanced intensity at the positions of nuclear Bragg peaks. Figure S6a presents the neutron diffraction pattern collected at 300 K, along with the corresponding Rietveld refinement. All observed peaks are consistent with the Pnmm symmetry of MnSb2, and no additional magnetic peaks are detected. The refined lattice parameters from the neutron diffraction data are a = 6.0162(2) Å, b = 6.8824(3) Å, and c = 3.3226(1) Å, which are in good agreement with the values obtained from the X-ray diffraction refinement. Minor impurity phases were identified as MnSb (2.7 wt%), MnO (0.3 wt%), Sb (3.6 wt%), and boron nitride (BN, 0.07 wt%), which account for the weak reflections not indexed to the primary phase. Statistical parameters from the refinement, including all the phases in the model, are Rwp = 6.0% and GOF= 3.2, indicating a reasonable refinement. The site occupancy, atomic coordinates, and isotropic displacement parameters obtained from the refinement are summarized in Table S4.

Figure S6. (a) Rietveld refinement of the 300 K powder neutron diffraction data for MnSb2, yielding a weighted profile R-factor (Rwp) of 6.0% and a goodness of fit (GOF) of 3.2. The blue dots represent the experimental data, while the orange line corresponds to the calculated pattern. The green line indicates the difference between the observed and calculated intensities. Vertical tick marks represent the allowed Bragg reflection positions for the identified phases: MnSb2 (red), Sb (gray), MnSb (black), MnO (cyan), and boron nitride (BN, magenta). (b) Enlarged view of the low-Q region from panel (a), emphasizing the absence of additional magnetic Bragg peaks, indicating no long-range magnetic ordering at room temperature.

Table S4. Refined atomic coordinates and the equivalent isotropic displacement parameters of MnSb2 at 300 K.

| Atoms | Wyck. | x | y | z | Occ. | Ueq |
| --- | --- | --- | --- | --- | --- | --- |
| Sb | 4g | 0.1799(1) | 0.3624(1) | 0 | 1 | 0.0080(2) |
| Mn | 2a | 0 | 0 | 0 | 1 | 0.0060(3) |

Table S5. Basis vectors for the space group Pnnm with k = (0, 0, 0). The decomposition of the magnetic representation for the Mn site (0, 0, 0) is ΓMag=1Γ11+2Γ31+2Γ51+1Γ71. The atoms of the nonprimitive basis are defined according to 1: (0, 0, 0), 2: (1/2, 1/2, 1/2).

| IR BV Atom |  |  | BV components m∥a m∥b m∥c im∥a im∥b im∥c |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Γ1 | ѱ1 | 1 | 0 | 0 | 4 | 0 | 0 | 0 |
|  |  | 2 | 0 | 0 | -4 | 0 | 0 | 0 |
| Γ3 | ѱ2 | 1 | 4 | 0 | 0 | 0 | 0 | 0 |
|  |  | 2 | 4 | 0 | 0 | 0 | 0 | 0 |
|  | ѱ3 | 1 | 0 | 4 | 0 | 0 | 0 | 0 |
|  |  | 2 | 0 | -4 | 0 | 0 | 0 | 0 |
| Γ5 | ѱ4 | 1 | 4 | 0 | 0 | 0 | 0 | 0 |
|  |  | 2 | -4 | 0 | 0 | 0 | 0 | 0 |
|  | ѱ5 | 1 | 0 | 4 | 0 | 0 | 0 | 0 |
|  |  | 2 | 0 | 4 | 0 | 0 | 0 | 0 |
| Γ7 | ѱ6 | 1 | 0 | 0 | 4 | 0 | 0 | 0 |
|  |  | 2 | 0 | 0 | 4 | 0 | 0 | 0 |

Table S6. Symmetry-allowed magnetic basis vectors obtained from representation analysis for the Mn1 and Mn2 sublattices, obtained from Rietveld refinements of the powder neutron diffraction data collected at 200 K. For each sublattice, the basis vectors ѱ1, ѱ2, and ѱ3 correspond to magnetic moment components along the crystallographic a, b, and c axes, respectively.

| Mn1 | a | b | c |
| --- | --- | --- | --- |
| ѱ1 | 1 | 0 | 0 |
| ѱ2 | 0 | 1 | 0 |
| ѱ3 | 0 | 0 | 1 |
| Mn2 |  |  |  |
| ѱ1 | 1 | 0 | 0 |
| ѱ2 | 0 | 1 | 0 |
| ѱ3 | 0 | 0 | 1 |

To further probe potential magnetic contributions in MnSb2, Figure S6b highlights the low-Q region of the neutron diffraction pattern, where magnetic scattering is typically enhanced due to the Q-dependence of the magnetic form factor. The absence of additional Bragg reflections in this region provides compelling evidence against the presence of long-range magnetic ordering at room temperature. In particular, the lack of magnetic peaks strongly suggests that antiferromagnetic (AFM) ordering with a non-zero propagation vector (k ≠ (0, 0, 0)) is absent in this compound. Nonetheless, the possibility of ferromagnetic ordering corresponding to k = (0, 0, 0) cannot be excluded solely based on the absence of additional reflections. In such a case, magnetic ordering would manifest as an enhancement of nuclear Bragg peak intensities. However, our Rietveld refinement shows no observable intensity increase at the nuclear peak positions, and no systematic deviation between observed and calculated intensities was detected. To definitively assess the presence of ferromagnetic ordering and to estimate an upper bound for the ordered Mn moment, magnetic structure refinements were performed using the FullProf suite with magnetic subgroups of the Pnmm space group. Symmetry-allowed magnetic configurations were derived from a group-subgroup analysis of the propagation vector k = (0, 0, 0), implemented via SARAh-Representational Analysis. Four irreducible representations (IRs) and their corresponding basis vectors (BVs) were identified, as listed in Table S5. Among them, IRs Γ3 (with BV ѱ₂) and Γ5 (with BV ѱ₅), which describe ferromagnetic alignment of Mn moments within the ab-plane, produced the best magnetic refinements, with magnetic R-factors (Rmag) below 5. Despite these fits, the refined ordered moment was consistently small, with a total magnetic moment of μtot that should be much smaller than 0.2 μB/Mn, indicating the absence of significant static magnetic ordering in MnSb2 at room temperature.

Figure S7. (a) The sample used to determine the crystallographic direction of MnSb2 is shown. (b) The PXRD data are shown for solid-state reactions at temperatures above 700 °C.  (c) The sample current as a function of temperature is shown for different MnSb2 reactions. (d) The phase diagram is shown. A point is the eutectic point, and the b point is the peritectic point. The red curve indicates the liquidus lines.

Reference

(1) Hewitt, R. R.; Williams, B. F. Nuclear Quadrupole Interaction of Sb121 and Sb123 in Antimony Metal. Phys Rev 1963, 129, 1188. https://doi.org/10.1103/PhysRev.129.1188

(2) Nagarajan, V.; Vijayaraghavan. Nuclear Magnetic Resonance in Ferromagnetic MnSb and CrxMn1-xSb. J Phys Soc Jpn 1972, 33, 88-91. https://doi.org/10.1143/JPSJ.33.88