Supporting Information

Nitrogen-Doped Porous Carbon Derived from Bimetallic Zeolitic Imidazolate Frameworks for Electrochemical Li+/Na+ Storage

Shuai Donga, Jiewu Cuia,b,c,*, Dongbo Yua,b,c,*, Zhongnan Caoa, Cuiping Yua, Yong Zhanga,b,c, Yucheng Wua,b,c

aSchool of Materials Science and Engineering, Hefei University of Technology, Hefei, 230009, P. R. China

bKey Laboratory of Advanced Functional Materials and Devices of Anhui Province，Hefei, 230009, P. R. China

cChina International S&T Cooperation Base for Advanced Energy and Environmental Materials & Anhui Provincial International S&T Cooperation Base for Advanced Energy Materials, Hefei University of Technology, Hefei 230009, China

E-mail: dongboy@hfut.edu.cn, jwcui@hfut.edu.cn

Fig. S1 Optical photograph of ZnCo-ZIF with different Zn/Co molar ratios.

Fig. S2 SEM images of ZnCo-ZIFs with different Zn2+/Co2+ molar ratios: ZIF-8 (a), 80Zn20Co-ZIF(b), 60Zn40Co-ZIF (c), 40Zn-60Co-ZIF (d) and ZIF-67 (e).

Fig. S3 XRD patterns of ZIF-8, ZIF-67, 40Zn60Co-ZIF and 20Zn80Co-ZIF.

Fig. S4 TGA and DTG curves of 40Zn60Co-ZIF from 25 °C to 1000 °C with a rate of 5 °C min-1 in N2 atmosphere.

Fig. S5 SEM images of 40Zn60Co-ZIF calcinated at different temperatures: NPC(40Zn-60Co)-600°C (a), NPC(40Zn-60Co)-700°C (b), NPC(40Zn-60Co)- 800°C (c) and NPC(40Zn-60Co)-900°C (d) with subsequently etched in diluted HNO3 at 80 °C for 24 h.

Fig. S6 SEM images of NPC(100Zn)-600°C (a), NPC(80Zn-20Co)-600°C (b), NPC(60Zn-40Co)-600°C (c) and  NPC(100Co)-600°C (d).

Fig S7  Full XPS spectrum of NPC(40Zn-60Co)-600°C, NPC(40Zn-60Co)-700°C, NPC(40Zn-60Co)-800°C and NPC(40Zn-60Co)-900°C (a), C 1s spectrum of NPC(40Zn-60Co)-600°C (b), NPC(40Zn-60Co)-700°C (c), NPC(40Zn-60Co)-800°C (d) and NPC(40Zn-60Co)-900°C (e).

Fig S8 N 1s XPS spectrum of  NPC(40Zn-60Co)-600°C (a), NPC(40Zn-60Co)-700°C (b), NPC(40Zn-60Co)-800°C (c) and  NPC(40Zn-60Co)-900°C (d), nitrogen content of all 40Zn60Co-ZIF-derived NPC materials (e).

Table S1 Contents and ratios of Pyridinic N, Pyrrolic N and Graphitic N in NPC(40Zn-60Co)-600°C, NPC(40Zn-60Co)-700°C, NPC(40Zn-60Co)-800°C and NPC(40Zn-60Co)-900°C.

| Samples | N content | Pyridinic N | Pyrrolic N | Graphitic N |
| --- | --- | --- | --- | --- |
| NPC(40Zn-60Co)-600°C | 10.74% | 4.92% | 4.29% | 1.53% |
| NPC(40Zn-60Co)-700°C | 9.77% | 1.81% | 5.71% | 2.25% |
| NPC(40Zn-60Co)-800°C | 5.90% | 1.20% | 3.05% | 1.65% |
| NPC(40Zn-60Co)-900°C | 4.90% | 1.11% | 1.46% | 2.33% |

Fig. S9  Full XPS spectrum of all the samples (a), C 1s XPS spectrum of  NPC(100Zn)-600°C (b), NPC(80Zn-20Co)-600°C (c), NPC(60Zn-40Co)-600°C (d), NPC(20Zn-80Co)-600°C (e) and  NPC(100Co)-600°C (f).

Fig. S10 N 1s spectrum of NPC(100Zn)-600°C (a), NPC(80Zn-20Co)-600°C (b), NPC(60Zn-40Co)-600°C (c) and NPC(100Co)-600°C (d).

Table S2 Contents and ratios of Pyridinic N, Pyrrolic N and Graphitic N in NPC(xZn-yCo)-600°C.

| Samples | N content | Pyridinic N | Pyrrolic N |  | Graphitic N |
| --- | --- | --- | --- | --- | --- |
| NPC(100Zn)-600°C | 24.91% | 17.55% |  | 3.62% | 3.74% |
| NPC(80Zn-20Co)-600°C | 22.35% | 12.82% |  | 6.63% | 2.90% |
| NPC(60Zn-40Co)-600°C | 17.44% | 7.82% |  | 8.09% | 1.53% |
| NPC(40Zn-60Co)-600°C | 10.74% | 4.92% |  | 4.29% | 1.53% |
| NPC(20Zn-80Co)-600°C | 9.49% | 4.49% |  | 2.65% | 2.35% |
| NPC(100Co)-600°C | 13.26% | 4.33% |  | 6.33% | 2.60% |

Fig. S11  N2 adsorption/desorption isotherms (a) and pore size distributions (b) of the NPC(40Zn-60Co)-600°C, NPC(40Zn-60Co)-700°C, NPC(40Zn-60Co)-800°C and NPC(40Zn-60Co)-900°C measured at 77 K.

Fig. S12  N2 adsorption/desorption isotherms (a) and pore size distributions (b) of the NPCs-600°C measured at 77 K.

Fig. S13 Li+ storage performance: The first three CV curves of NPC(20Zn-80Co)-600°C at scan rate of 0.1 mV s-1 (a); rate capability of NPC(40Zn-60Co)-T at various current densities ranging from 0.1 to 5 A g-1 (b); cycling performance of NPC(20Zn-80Co)-600°C electrodes at current density of 0.1 A g-1 after 100 cycles (c); Nyquist plots of NPC(xZn-yCo)-600°C (d)

Table S3 Comparison of Li+ storage properties of NPC prepared in this work with other porous carbon materials.

| Samples | Specific capacity | Rate capacity | Cycling stability | Ref. |
| --- | --- | --- | --- | --- |
| # N-doped porous carbon | 570 mAh g-1 at 0.1 A g-1 at first cycle | 370 mAh g-1 at 0.5 A g-1; 215 mAh g-1 at 4 A g-1 | 540 mAh g-1 at 0.1 A g-1 after 100 cycles | [1] |
| COFs-derived porous carbon | 505.7 mAh g-1 at 0.1 A g-1 after 5 cycles | 143 mAh g-1 at 5 A g-1 | 488 mAh g-1 at 0.1 A g-1 after 100 cycles | [2] |
| S/O co-doped porous carbon | 931 mAh g-1 at 0.1 A g-1 at first cycle | 312 mAh g-1 at 1 A g-1 | 504 mAh g-1 at 0.2 A g-1 after 200 cycles | [3] |
| Spheroidal carbon particles | 320 mAh g-1 at 0.1 A g-1 | - | 350 mAh g-1 at 0.1 A g-1 after 200 cycles | [4] |
| B-doped porous carbon | 697 mAh g-1 at 0.1 A g-1 after 10 cycles | 345 mAh g-1 at 2 A g-1 | 496 mAh g-1 at 0.1 A g-1 after 100 cycles | [5] |
| Egg yolk-derived carbon | 739 mAh g-1 at 0.1 A g-1 after 2 cycles | 321 mAh g-1 at 1 A g-1 | 711.6 mAh g-1 at 0.1 A g-1 after 100 cycles | [6] |
| N-doping hard carbon nanoshells | 395 mAh g-1 at 0.1 A g-1 after 15 cycles | 376 mAh g-1 at 0.5 A g-1; 257 mAh g-1 at 1 A g-1 | 245 mAh g-1 at 1.5 A g-1 after 300 cycles | [7] |
| N-doped carbon balls | 990 mAh g-1 at 0.1 A g-1 after 10 cycles | 209 mAh g-1 at 1 A g-1; 57 mAh g-1 at 40 A g-1 | 454 mAh g-1 at 0.5 A g-1 after 100 cycles | [8] |
| N-doped carbon nanosheets | 648 mAh g-1 at 0.5 A g-1 after 2 cycles | 683 mAh g-1 at 0.2 A g-1; 405 mAh g-1 at 1 A g-1 | 513 mAh g-1 at 0.5 A g-1 after 500 cycles | [9] |
| Ultrathin hollow carbon shell | 421 mAh g-1 at 1 A g-1 after 170 cycles | 621 mAh g-1 at 0.2 A g-1; 398 mAh g-1 at 1 A g-1 | 334 mAh g-1 at 1 A g-1 after 1000 cycles | [10] |
| ZIF-derived porous carbon | 876.5 mAh g-1 at 0.1 A g-1 at 2 cycle | 768.9 mAh g-1 at 0.2 A g-1; 480.9 mAh g-1 at 2 A g-1 | 591.5 mAh g-1 at 1 A g-1 after 500 cycles | This work |

Fig. S14 Na+ storage performance of NPC(20Zn-80Co)-600°C: initial three CV curves at scan rate of 0.1 mV s-1 (a); cycling performance at current density of 0.05 A g-1 for 450 cycles (b). Nyquist plots of NPC(20Zn-80Co)-T (c).

Table S4 Comparison of Na+ storage properties of NPC prepared in this work with other porous carbon-based materials.

| Samples | Specific capacity | Rate capacity | Cycling stability | Ref. |
| --- | --- | --- | --- | --- |
| Soft carbon | 222 mAh g-1 at 30 mA g-1 | 135 mAh g-1 at 0.3 A g-1 | 170 mAh g-1 at 0.3 A g-1 after 200 cycles | [11] |
| 3D amorphous carbon | 280 mAh g-1 at 30 mA g-1 | 66 mAh g-1 at 9.6 A g-1 | 188 mAh g-1 at 0.3 A g-1 after 600 cycles | [12] |
| N-rich mesoporous carbon | 434.6 mAh g-1 at 30 mA g-1 | 110 mAh g-1 at 2 A g-1 | 280.8 mAh g-1 at 50 mA g-1 after 300 cycles | [13] |
| N-rich porous carbon | 371.4 mAh g-1 at 30 mA g-1 | 174.2 mAh g-1 at 1 A g-1 | 255.9 mAh g-1 at 0.5 A g-1 after 3000 cycles | [14] |
| P-doped carbon nanofibers | 288 mAh g-1 at 50 mA g-1 | 103 mAh g-1 at 2 A g-1 | 253 mAh g-1 at 50 mA g-1 after 200 cycles | [15] |
| Mesoporous hard carbon | 375 mAh g-1 at 20 mA g-1 | 220 mAh g-1 at 0.2 A g-1 | 300 mAh g-1 at 0.1 A g-1 after 400 cycles | [16] |
| N-doping carbon nanoshells | 325 mAh g-1 at 0.1 A g-1 | 63 mAh g-1 at 5 A g-1 | 174 mAh g-1 at 0.1 A g-1 after 200 cycles | [17] |
| S-doped porous carbon | 313 mAh g-1 at 20 mA g-1 | - | 220 mAh g-1 at 20 mA g-1 after 50 cycles | [18] |
| Porous graphene grids carbon | 160 mAh g-1 at 50 mA g-1 | 109 mAh g-1 at 0.14 A g-1 | 112 mAh g-1 at 1 A g-1 after 1000 cycles | [19] |
| COFs-derived porous carbon | 239.5 mAh g-1 at 50 mA g-1 | 170 mAh g-1 at 1 A g-1 | 237.7 mAh g-1 at 50 mA g-1 after 100 cycles | [2] |
| Defective hard carbon | 308 mAh g-1 at 20 mA g-1 | - | 288 mAh g-1 at 20 mA g-1 after 210 cycles | [20] |
| ZIF-derived porous carbon | 416.1 mAh g-1 at 0.02 A g-1 | 206.6 mAh g-1 at 0.2 A g-1; 113 mAh g-1 at 2 A g-1 | 117.8 mAh g-1 at 1 A g-1 after 1000 cycles | This work |

References

[1] V. Selvamani, R. Ravikumar, V. Suryanarayanan, D. Velayutham, S. Gopukumar, Garlic peel derived high capacity hierarchical N-doped porous carbon anode for sodium/lithium ion cell, Electrochim. Acta 190 (2016) 337-345.

[2] X.J. Zhang, G. Zhu, M. Wang, J.B. Li, T. Lu, L.K. Pan, Covalent-organic-frameworks derived N-doped porous carbon materials as anode for superior long-life cycling lithium and sodium ion batteries, Carbon 116 (2017) 686-694.

[3] P.Y. Zhang, Z.Y. Sui, E.J. Wang, Y.W. Liu, B.H. Han, Preparation of hierarchically porous sulfur- and oxygen-co-doped carbon for gas uptake and lithium-ion battery, Microporous and Mesoporous Materials 264 (2018) 118-124.

[4] K. Kim, R.A. Adams, P.J. Kim, A. Arora, E. Martinez, J.P. Youngblood, V.G. Pol, Li-ion storage in an amorphous, solid, spheroidal carbon anode produced by dry-autoclaving of coffee oil, Carbon 133 (2018) 62-68.

[5] D. Wang, Z. Wang, Y. Li, K. Dong, J. Shao, S. Luo, Y. Liu, X. Qi, In situ double-template fabrication of boron-doped 3D hierarchical porous carbon network as anode materials for Li- and Na-ion batteries, Applied Surface Science 464 (2019) 422-428.

[6] S. Wang, H. Wang, R. Zhang, L. Zhao, X. Wu, H. Xie, J. Zhang, H. Sun, Egg yolk-derived carbon: Achieving excellent fluorescent carbon dots and high performance lithium-ion batteries, Journal of Alloys and Compounds 746 (2018) 567-575.

[7] F. Zhao, X. Zhao, B. Peng, F. Gan, M. Yao, W. Tan, J. Dong, Q. Zhang, Polyimide-derived carbon nanofiber membranes as anodes for high-performance flexible lithium ion batteries, Chinese Chemical Letters 29 (2018) 1692-1697.

[8] A. Agrawal, K. Biswas, S.K. Srivastava, S. Ghosh, Effect of N-doping on hard carbon nano-balls as anode for Li-ion battery: improved hydrothermal synthesis and volume expansion study, Journal of Solid State Electrochemistry 22 (2018) 3443-3455.

[9] A.K. Mondal, K. Kretschmer, Y. Zhao, H. Liu, C. Wang, B. Sun, G. Wang, Nitrogen-Doped Porous Carbon Nanosheets from Eco-Friendly Eucalyptus Leaves as High Performance Electrode Materials for Supercapacitors and Lithium Ion Batteries, Chemistry 23 (2017) 3683-3690.

[10] P. Li, J. Liu, Y. Wang, Y. Liu, X. Wang, K.W. Nam, Y.M. Kang, M. Wu, J. Qiu, Synthesis of ultrathin hollow carbon shell from petroleum asphalt for high-performance anode material in lithium-ion batteries, Chemical Engineering Journal 286 (2016) 632-639.

[11] Y. Li, Y.S. Hu, X. Qi, X. Rong, H. Li, X. Huang, L. Chen, Advanced sodium-ion batteries using superior low cost pyrolyzed anthracite anode: towards practical applications, Energy Storage Materials 5 (2016) 191-197.

[12] P. Lu, Y. Sun, H. Xiang, X. Liang, Y. Yu, 3D Amorphous Carbon with Controlled Porous and Disordered Structures as a High-Rate Anode Material for Sodium-Ion Batteries, Adv. Energy Mater. 8 (2018) 1702434.

[13] H. Liu, M. Jia, S. Yue, B. Cao, Q. Zhu, N. Sun, B. Xu, Creative utilization of natural nanocomposites: nitrogen-rich mesoporous carbon for a high-performance sodium ion battery, Journal of Materials Chemistry A 5 (2017) 9572-9579.

[14] X. Hu, X. Sun, S.J. Yoo, B. Evanko, F. Fan, S. Cai, C. Zheng, W. Hu, G.D. Stucky, Nitrogen-rich hierarchically porous carbon as a high-rate anode material with ultra-stable cyclability and high capacity for capacitive sodium-ion batteries, Nano Energy 56 (2019) 828-839.

[15] F. Wu, R. Dong, Y. Bai, Y. Li, G. Chen, Z. Wang, C. Wu, Phosphorus-Doped Hard Carbon Nanofibers Prepared by Electrospinning as an Anode in Sodium-Ion Batteries, ACS Appl Mater Interfaces 10 (2018) 21335-21342.

[16] H. Zhu, F. Shen, W. Luo, S. Zhu, M. Zhao, B. Natarajan, J. Dai, L. Zhou, X. Ji, R.S. Yassar, T. Li, L. Hu, Low temperature carbonization of cellulose nanocrystals for high performance carbon anode of sodium-ion batteries, Nano Energy 33 (2017) 37-44.

[17] S. Huang, Z. Li, B. Wang, J. Zhang, Z. Peng, R. Qi, J. Wang, Y. Zhao, N-Doping and Defective Nanographitic Domain Coupled Hard Carbon Nanoshells for High Performance Lithium/Sodium Storage, Adv. Funct. Mater. 28 (2018) 1706294.

[18] S. Zhang, F. Yao, L. Yang, F. Zhang, S. Xu, Sulfur-doped mesoporous carbon from surfactant-intercalated layered double hydroxide precursor as high-performance anode nanomaterials for both Li-ion and Na-ion batteries, Carbon 93 (2015) 143-150.

[19] H. Zhang, H. Guo, A. Li, X. Chang, S. Liu, D. Liu, Y. Wang, F. Zhang, H. Yuan, High specific surface area porous graphene grids carbon as anode materials for sodium ion batteries, Journal of Energy Chemistry 31 (2019) 159-166.

[20] Z. Li, Y. Chen, Z. Jian, H. Jiang, J.J. Razink, W.F. Stickle, J.C. Neuefeind, X. Ji, Defective Hard Carbon Anode for Na-Ion Batteries, Chemistry of Materials 30 (2018) 4536-4542.