Supporting information

Self-aligned double injection-function contact mitigating short channel effects in sub-micron channels of solution processed indium gallium zinc oxide

Gil Sheleg and Nir Tessler*

Sara and Moshe Zisapel Nano-Electronic Center, Department of Electrical Engineering, Technion - Israel Institute of Technology, Haifa 32000, Israel.

Double dope function TFT

In the main text, Figure 7 and Figure 8, we demonstrated the effect of creating a source electrode that is made of two self-aligned metals having two different injection barriers. Another method to produce differential injection such that only the part facing the drain is injection-limited is through lithography patterned doping. In this method the metal contact is of Schottky type and the channel material is highly doped under the source electrode but not close to the channel (see Figure 1Sa). The mechanisms by which doping turns a Schottky contact into an effectively ohmic is known and is reproduced in Figure 1Sb.1

Figure 1S. a) Schematic description of the double doped function source electrode. b) Schematic description of Schottky (top) and ohmic-tunneling (bottom) contacts.

In Figure 2S we reproduce the data of Figure 8 and add simulation results for a structure having double doped function (DDF) source electrode. As Figure 2Sc shows, this method is also a viable one and seems to be as good as the double work function (DWF) architecture.

Figure 2S. Output characteristics of (a), (d) single work function (SWF);  (b), (e) double work function (DWF); and (c), (f) double dope function (DDF) TFTs. The Schottky barrier height used is 0.75eV (a), (b), (c) and 1.05eV (d), (e), (f). The full, dash-dotted, and dashed lines represent TFTs having channel length of 1000nm, 500nm, and 200nm, respectively. The current is normalized to the channel’s width.

First attempts at making the DWF structure

A transistor with a combination of Platinum on Molybdenum source metal was fabricated in the proposed configuration (Figure 11 in main text) with the same IGZO solution thickness and atom ratio. Figure 3S shows the characteristics of the device.

Figure 3S (a) transfer and (b) output characteristics of the Mo/Pt source contact. The IGZO layer is made from a 15 nm 70:15:15 atom in the sol-gel solution.

Figure 3Sa shows some (not much) improvement in the subthreshold slope, while Figure 3Sb shows a very pronounced Schottky effect as if the platinum electrode completely blocks the injection from the ohmic contact. However, despite the pronounced Schottky effect, the maximum currents are higher than those of the ohmic contact transistor (see Figure 12a and b in the main text). After detailed analysis using experiments and simulations, we concluded that when we deposit on the IGZO 4 different materials (molybdenum, platinum, alumina, and silver), we lose our ability to control the oxygen vacancies concentration in the IGZO film. As the entire approach of double work function source electrode relies on controlling the depletion under the electrode, not controlling the vacancies (doping) makes it hopeless. Hence we adapted the double layer approach for the IGZO (see main text).

References:

1.	Sze, S. M., Physics of Semiconductor Devices. Wiley: New York, 1981.