Table 1. Information of experimental materials.

| Name | Relevant Parameters | Image |
| --- | --- | --- |
| Cylindrical ternary lithium-ion battery | Nominal capacity:41.90Ah; Nominal voltage:3.68V Dimensions: 46mm in diameter and 120mm in height |  |
| Battery shelf | Layer height: 750 mm; height of a single shelf: 375 mm |  |
| Fire sprinkler | Fast-response upright type K-ZSTZ-161-68℃ flow rate 322 L/min |  |
|  | Fast-response sidewall type K-ZSTBS-80-68℃ flow rate 160 L/min |  |

Table 2. Information of experimental equipment.

| Name | Model/ Specifications Parameters | Manufacturer | Image |
| --- | --- | --- | --- |
| Camera | FDR-AX60, with approximately 8.29 million pixels | Sony Corporation |  |
| DC Regulated Power Supply | LW-22010KD/220V 10A | Longwei Instrument Co., Ltd |  |
| Data Acquisition System | LR8431-30 | Hioki (Japan) |  |
| Thermocouple | Armored Type K, accuracy ±0.1℃, temperature measurement range 0~1000℃ | / |  |
| Heating Device | PI heating film, thickness 0.15±0.05mm, resistance 161.3Ω±5%, rated voltage 220V, rated power 300W | Custom-made |  |

Table 3. Working Cases

| Case | Heating Position | Sprinkler Arrangement | Shelf Layout | Schematic Diagram |
| --- | --- | --- | --- | --- |
| A | Inner edge of lower tray | Top-spray sprinkler, flow rate: 322L/min | Double-layer |  |
| B | Center of lower tray |  |  |  |
| C | Edge of upper tray |  |  |  |
| D | Inner edge of lower tray | Side-spray sprinklers, flow rate: 160L/min | Double-layer |  |
| F | Center of lower tray |  |  |  |
| G | Inner edge | Top-spray sprinkler, flow rate: 322L/min | Single-layer |  |