Table-2 :  HFMs fabrication parameters

| Parameters | Conditions |
| --- | --- |
| Spinneret ID/OD (mm) | 0.55/1.1 |
| Dope solution composition | ZIF-8@NH2-MIL125(Ti)/(PVP/PES/NMP |
| Spinneret temperature (oC) | 27 |
| Dope extrusion rate (mL/min) | 3 |
| Bore fluid composition | H2O |
| Bore extrusion rate (mL/min) | 2.5 |
| Air gap (cm) | 5 |
| Coagulation and rinsing bath | H2O |
| Coagulation bath temperature (oC) | 27 |
| Humidity (%) | 50 - 70 |
| Take up speed (rpm) | 15 - 18 |