# Table 1. Collagen cross-linkers used in this study

| Cross-linker | Chemical structure | Manufacturer and details |
| --- | --- | --- |
| Proanthocyanidin (PA) |  | CAS: 4852-22-6 (generic) Molecular weight: variable (oligomeric mixture) Sigma-Aldrich, St. Louis, MO, USA |
| Theaflavin (TF) |  | CAS: 4670-05-7 Molecular weight: 564.49 g/mol Sigma-Aldrich, St. Louis, MO, USA |

## Table 2. Comparison of immediate and 6-month microtensile bond strength values within each group

| Group | Time | Mean ± SD (MPa) | Median (min–max) | p |
| --- | --- | --- | --- | --- |
| U | Immediate | 32,7 ± 13,63 | 31,5 (8,1 - 65) | 0,048 |
|  | 6 months | 27,61 ± 9,65 | 26,15 (11 - 49,1) |  |
| E+U | Immediate | 41,32 ± 15,67 | 40,9 (5,6 - 83) | <0,001 |
|  | 6 months | 28,94 ± 9,35 | 27,9 (12,3 - 50,3) |  |
| E+PA+U | Immediate | 34,84 ± 13,45 | 32,6 (15,4 - 69,3) | <0,001 |
|  | 6 months | 25,49 ± 9,53 | 23,3 (11,3 - 58,2) |  |
| E+PAU | Immediate | 25,48 ± 9,98 | 22,5 (9,2 - 51,8) | 0,025 |
|  | 6 months | 21,38 ± 7,17 | 18,9 (12,1 - 38,5) |  |
| PAFL | Immediate | 24,18 ± 9,76 | 21,85 (9,2 - 48,9) | 0,004 |
|  | 6 months | 19,47 ± 6,27 | 18,75 (7,7 - 33,5) |  |
| PA+U | Immediate | 11,85 ± 4,46 | 11,35 (5,2 - 24,3) | 0,001 |
|  | 6 months | 15,03 ± 4,87 | 13,3 (9,2 - 33) |  |
| PAU | Immediate | 11,3 ± 4,68 | 10,9 (5,2 - 23,2) | 0,253 |
|  | 6 months | 12,22 ± 3,03 | 12,35 (6,5 - 19,4) |  |
| E+TF+U | Immediate | 21,01 ± 10,14 | 19,6 (5,6 - 42,2) | 0,597 |
|  | 6 months | 20,62 ± 9,67 | 18,3 (6,5 - 60,4) |  |
| E+TFU | Immediate | 24,48 ± 9,66 | 20,5 (12,4 - 45,6) | 0,003 |
|  | 6 months | 19,07 ± 6,97 | 18,6 (8,3 - 41,2) |  |
| TF+U | Immediate | 12,58 ± 3,98 | 12 (5,3 - 21,9) | 0,961 |
|  | 6 months | 12,54 ± 4,09 | 12,4 (4,3 - 22,4) |  |
| TFU | Immediate | 12,78 ± 6,74 | 12,1 (5,2 - 31,2) | 0,561 |
|  | 6 months | 11,63 ± 4,5 | 11,2 (6,3 - 26,3) |  |

# Table 3. SEM evaluation of resin–dentin interface at different magnifications

| Group | SEM Imaging (X1,000) | SEM Imaging (X5,000) | SEM Imaging (X10,000) |
| --- | --- | --- | --- |
| U |  |  |  |
| E+U |  |  |  |
| E+PA+U |  |  |  |
| E+PAU |  |  |  |
| PA+U |  |  |  |
| PAU |  |  |  |
| E+TF+U |  |  |  |
| E+TFU |  |  |  |
| TF+U |  |  |  |
| TFU |  |  |  |
| Group | SEM Imaging (X1,000) | SEM Imaging (X5,000) | SEM Imaging (X10,000) |
| U |  |  |  |
| E+U |  |  |  |
| E+PA+U |  |  |  |
| E+PAU |  |  |  |
| PA+U |  |  |  |
| PAU |  |  |  |
| E+TF+U |  |  |  |
| E+TFU |  |  |  |
| TF+U |  |  |  |
| TFU |  |  |  |

Table 4. Fingerprint region of FTIR spectra of dentin specimens treated with proanthocyanidin (PA) and theaflavin (TF) at different stages of the adhesive protocol