🧪 STANDARD OPERATING PROCEDURE #7

Magnetic Susceptibility Hysteresis in Spin-Crossover Complexes

Testing λ-Framework via Light-Induced Entropy Weighting

Version: 1.0
Date: March 14, 2026
Laboratory: IIT Chemistry / Materials Science / Low-Temperature Physics Lab
Correspondence: [Principal Investigator]

📋 EXECUTIVE SUMMARY

This SOP provides a complete, reproducible protocol for measuring magnetic susceptibility hysteresis in spin-crossover (SCO) complexes as a function of light irradiation. The experiment directly tests the λ-framework prediction:

A(λ)=∫∣χTheat(T)-χTcool(T)∣ dT∝λ

where λ is controlled by photoexcitation via the LIESST effect (Light-Induced Excited Spin State Trapping).

🔬 1. SCIENTIFIC BACKGROUND

1.1 Why Spin-Crossover Complexes?

Spin-crossover complexes (e.g., Fe(Htrz)₂(trz)) exhibit:

- Bistable spin states: Low-spin (LS, S=0) ↔ High-spin (HS, S=2)

- Thermal hysteresis tunable by chemical design

- Photo-switchable via LIESST effect (green light)

- Established synthesis at multiple IITs

- Direct magnetic readout via SQUID or VSM

1.2 The λ-Connection

In your framework:

- λ = entropy weighting parameter

- In SCO complexes: λ ∝ fraction of photoinduced HS molecules

- Light creates metastable HS states → weighted ensemble

- LIESST effect: Green light (532 nm) traps HS at low T

1.3 Predicted Signature

| Measurement | λ = 0 (dark) | λ > 0 (irradiated) |
| --- | --- | --- |
| χT(T) heating = cooling | ✓ (thermal hysteresis only) | ✗ (enhanced hysteresis) |
| Loop area A | A₀ (intrinsic) | A₀ + ΔA ∝ λ |
| T₁/₂ (transition temp) | Fixed | Shifted |
| Relaxation kinetics | Single exponential | Stretched (λ-dependent) |

🧪 2. MATERIALS AND SAMPLE PREPARATION

2.1 Target Complexes

| Complex | T₁/₂ (K) | ΔT_hysteresis (K) | λ Sensitivity | Availability |
| --- | --- | --- | --- | --- |
| Fe(Htrz)₂(trz) | 350-380 | 30-40 K | High | IIT Bombay |
| [Fe(phen)₂(NCS)₂] | 176 | 0 K (gradual) | Medium (control) | IIT Madras |
| [Fe(PM-PEA)₂(NCS)₂] | 170-200 | 0 K (abrupt) | Medium | IIT Kanpur |
| [Fe(PM-BiA)₂(NCS)₂] | 150-180 | 10-20 K | High | IIT Kharagpur |
| [Fe(PM-AzA)₂(NCS)₂] | 120-150 | 20-30 K | Very High | IIT Delhi |

2.2 Synthesis Protocol (Example: Fe(Htrz)₂(trz))

Materials:

- Fe(BF₄)₂·6H₂O (99%, Sigma-Aldrich)

- 1H-1,2,4-triazole (Htrz, 99%, Sigma-Aldrich)

- Ethanol (absolute)

- Deionized water

Procedure:

python

"""

synthesis_protocol.py

Standard synthesis for iron-triazole spin-crossover complex

"""

def synthesize_SCO(batch_size_g=1.0):

"""

batch_size_g: target mass in grams

Returns: yield, characterization data

"""

# Molar masses

M_Fe = 391.89  # Fe(BF₄)₂·6H₂O

M_Htrz = 69.07  # Htrz

M_product = 475.5  # Approximate for [Fe(Htrz)₂(trz)](BF₄)

# Stoichiometry: Fe : Htrz = 1 : 3

n_product = batch_size_g / M_product

m_Fe = n_product * M_Fe * 1.05  # 5% excess

m_Htrz = n_product * 3 * M_Htrz

print(f"Synthesizing {batch_size_g}g of [Fe(Htrz)₂(trz)](BF₄)")

print(f"Weigh {m_Fe:.3f}g Fe(BF₄)₂·6H₂O")

print(f"Weigh {m_Htrz:.3f}g Htrz")

print("\nProcedure:")

print("1. Dissolve Fe salt in 10 mL deionized water")

print("2. Dissolve Htrz in 20 mL ethanol")

print("3. Add Htrz solution dropwise to Fe solution with stirring")

print("4. Stir at 60°C for 2 hours")

print("5. Cool to room temperature")

print("6. Filter precipitate, wash with ethanol")

print("7. Dry under vacuum at 60°C for 12 hours")

return {

'theoretical_yield_g': batch_size_g,

'expected_T1/2_K': 360,

'expected_hysteresis_K': 35

}

2.3 Sample Preparation for Magnetic Measurements

Powder Sample:

- Mass: 10-20 mg

- Pack in gelatin capsule or PTFE tape

- Ensure uniform packing

Thin Film (optional):

- Spin-coat on 5×5 mm Si substrate

- Thickness: 100-500 nm

- Anneal at 80°C for 1 hour

Photoexcitation Preparation:

- Mount optical fiber in cryostat

- Calibrate power at sample position

- Green laser: 532 nm, 1-50 mW

2.4 Light Irradiation Parameters

| λ Level | Laser Power | Irradiation Time | HS Fraction | Application |
| --- | --- | --- | --- | --- |
| 0.0 | 0 mW | 0 min | 0% | Dark reference |
| 0.1 | 1 mW | 5 min | ~10% | Low λ |
| 0.2 | 2 mW | 10 min | ~20% | Medium λ |
| 0.4 | 5 mW | 20 min | ~40% | High λ |
| 0.6 | 10 mW | 30 min | ~60% | Very High |
| 0.8 | 20 mW | 60 min | ~80% | Saturation |

🔧 3. INSTRUMENTATION SPECIFICATIONS

3.1 Core Instruments

| Instrument | Model (example) | Purpose | IIT Availability |
| --- | --- | --- | --- |
| SQUID Magnetometer | MPMS-XL or MPMS3 | High-sensitivity χ(T) | IITB/IITK/IITM |
| VSM | PPMS-VSM | Faster measurements | IITKGP/IITR/IITD |
| Cryostat | 2-400 K range | Temperature control | All IITs |
| Laser | 532 nm DPSS | Photoexcitation | All IITs |
| Optical fiber | Multimode, 400 μm | Light delivery | All IITs |
| Power meter | Thorlabs PM100D | Calibrate laser power | All IITs |

3.2 Required Configuration

Magnetic Measurement:

- DC susceptibility mode

- Field: 1000 Oe (or 0.1 T)

- Temperature range: 5-400 K

- Ramp rate: 2 K/min (standard)

- Data points: every 1 K (near transition), every 5 K (elsewhere)

Photoexcitation Setup:

text

┌─────────────────┐

│    Laser        │

│    532 nm       │

└────────┬────────┘

│

┌────────┴────────┐

│   Power meter   │

│   (calibration) │

└────────┬────────┘

│

┌────────┴────────┐

│   Optical fiber │

└────────┬────────┘

│

┌────────┴────────┐

│   Cryostat      │

│   with sample   │

└─────────────────┘

3.3 Complete Parts List

| Item | Specification | Quantity | Source |
| --- | --- | --- | --- |
| Gelatin capsules | Size 4 | 100 | Any pharmacy |
| PTFE tape | 1/2 inch width | 1 roll | Local hardware |
| Quartz rod | 3 mm diameter | 10 cm | Local supplier |
| Optical fiber | 400 μm, SMA connectors | 2 m | Thorlabs |
| Laser safety goggles | 532 nm OD6 | 2 pairs | Thorlabs |
| Blackout fabric | Light-tight | 1 m² | Local |

📏 4. PRE-MEASUREMENT CALIBRATION

4.1 SQUID Calibration

python

"""

squid_calibration.py

Calibrate SQUID response with standard

"""

def calibrate_squid():

"""

Use Pd standard (known susceptibility)

Expected: χ = 5.3×10⁻⁶ emu/g at 300K

"""

# Measure Pd standard at 300K

mass_Pd = 10.0  # mg

measured_moment = 5.3e-5  # emu (example)

calibration_factor = (5.3e-6 * mass_Pd/1000) / measured_moment

return {

'calibration_factor': calibration_factor,

'date': datetime.now().isoformat()

}

4.2 Laser Power Calibration

python

"""

laser_calibration.py

Calibrate laser power at sample position

"""

def calibrate_laser_power(laser, power_meter, fiber):

"""

Measure actual power at sample position

"""

results = []

for set_power in [0, 1, 2, 5, 10, 20, 50]:  # mW

laser.set_power(set_power)

time.sleep(2)  # stabilize

# Measure through fiber

actual_power = power_meter.measure()

results.append({

'set_power_mW': set_power,

'actual_power_mW': actual_power,

'transmission': actual_power / set_power if set_power > 0 else 0

})

return pd.DataFrame(results)

4.3 Temperature Calibration

| Step | Action | Acceptance |
| --- | --- | --- |
| 1 | Mount calibrated Cernox thermometer | Traceable standard |
| 2 | Measure at 4.2 K (liquid He) | Within 0.1 K |
| 3 | Measure at 77 K (liquid N₂) | Within 0.5 K |
| 4 | Measure at 273 K (ice water) | Within 0.5 K |
| 5 | Measure at 373 K (boiling water) | Within 1 K |

4.4 Sample Mass Measurement

| Step | Action | Acceptance |
| --- | --- | --- |
| 1 | Weigh empty capsule | 0.1 μg precision |
| 2 | Load sample | 10-20 mg |
| 3 | Weigh capsule + sample | Record mass |
| 4 | Subtract for sample mass | ±0.01 mg |

4.5 Dark Reference Measurement

Measure full thermal cycle without irradiation:

- Cool from 400 K → 5 K

- Heat from 5 K → 400 K

- Record χT(T) for both cycles

- This gives baseline hysteresis A₀

📊 5. MEASUREMENT PROTOCOL

5.1 Experimental Sequence

For each λ level (0.0, 0.1, 0.2, 0.4, 0.6, 0.8):

python

"""

measurement_protocol.py

Automated measurement sequence for SCO hysteresis

"""

import time

import numpy as np

import pandas as pd

from datetime import datetime

class SCOMeasurement:

def __init__(self, sample_id, laser_power, irradiation_time,

magnetometer, laser, temp_controller):

self.sample_id = sample_id

self.laser_power = laser_power

self.irradiation_time = irradiation_time

self.lambda_val = self.calculate_lambda(laser_power)

self.magnetometer = magnetometer

self.laser = laser

self.temp_controller = temp_controller

def calculate_lambda(self, power):

"""λ ∝ power (calibrate so that max power gives λ=1)"""

max_power = 20  # mW (saturation)

return min(power / max_power, 1.0)

def irradiate_sample(self, T_irradiate=10):

"""

Irradiate sample at low temperature to trap HS state

"""

print(f"Irradiating at {T_irradiate} K for {self.irradiation_time} s")

# Cool to irradiation temperature

self.temp_controller.ramp_to(T_irradiate, 5)

time.sleep(300)  # stabilize

# Turn on laser

self.laser.set_power(self.laser_power)

self.laser.shutter_open()

# Irradiate

time.sleep(self.irradiation_time)

# Turn off laser

self.laser.shutter_close()

self.laser.set_power(0)

print("Irradiation complete")

def measure_susceptibility_at_T(self, T, field=1000):

"""

Measure χ at fixed temperature

"""

# Stabilize

self.temp_controller.set_T(T)

time.sleep(60)  # 1 min stabilization

# Measure

moment = self.magnetometer.measure_moment(field)

# Convert to χT (emu·K/mol)

χT = moment * T / self.mass_g * self.molar_mass

return {

'T': T,

'moment_emu': moment,

'χT': χT,

'field_Oe': field

}

def run_temperature_ramp(self, T_start, T_end, step=2,

rate=2, cycle='heat', field=1000):

"""

Run temperature ramp with measurements

"""

results = []

if T_start < T_end:  # heating

T_range = np.arange(T_start, T_end+step, step)

else:  # cooling

T_range = np.arange(T_start, T_end-step, -step)

for T in T_range:

print(f"  Measuring at T = {T} K")

self.temp_controller.ramp_to(T, rate)

data = self.measure_susceptibility_at_T(T, field)

data['cycle'] = cycle

results.append(data)

return pd.DataFrame(results)

def run_full_experiment(self):

"""

Complete protocol for one λ value

"""

print(f"\n{'='*50}")

print(f"Sample: {self.sample_id}")

print(f"Laser power: {self.laser_power} mW")

print(f"λ = {self.lambda_val:.2f}")

print(f"{'='*50}")

# Step 1: Anneal at high T (erase history)

print("Annealing at 400 K...")

self.temp_controller.ramp_to(400, 10)

time.sleep(600)  # 10 min anneal

# Step 2: Cool to irradiation temperature

print("Cooling to irradiation temperature...")

self.temp_controller.ramp_to(10, 5)

time.sleep(300)

# Step 3: Irradiate (if λ > 0)

if self.lambda_val > 0:

self.irradiate_sample(T_irradiate=10)

else:

print("Dark reference - no irradiation")

# Step 4: Measure heating cycle (5 K → 400 K)

print("Heating cycle...")

heat_data = self.run_temperature_ramp(

T_start=5, T_end=400, step=2, rate=2, cycle='heat'

)

# Step 5: Measure cooling cycle (400 K → 5 K)

print("Cooling cycle...")

cool_data = self.run_temperature_ramp(

T_start=400, T_end=5, step=2, rate=2, cycle='cool'

)

# Combine

full_data = pd.concat([heat_data, cool_data], ignore_index=True)

full_data['sample_id'] = self.sample_id

full_data['laser_power_mW'] = self.laser_power

full_data['lambda'] = self.lambda_val

full_data['timestamp'] = datetime.now().isoformat()

return full_data

5.2 Data Recording Format

python

"""

data_recording.py

Save SCO measurement data

"""

def save_sco_data(data_df, filename):

"""

Required columns:

- timestamp: ISO format

- sample_id: e.g., 'Fe-Htrz-01'

- laser_power_mW: irradiation power

- lambda: λ = power/power_max

- cycle: 'heat' or 'cool'

- T: temperature (K)

- moment_emu: measured magnetic moment

- field_Oe: applied field

- χT: χ·T (emu·K/mol)

"""

data_df.to_csv(filename, index=False)

print(f"Data saved to {filename}")

# Metadata

metadata = {

'date': data_df['timestamp'].iloc[0],

'sample': data_df['sample_id'].iloc[0],

'lambda_values': data_df['lambda'].unique().tolist(),

'T_range': [data_df['T'].min(), data_df['T'].max()]

}

import json

with open(filename.replace('.csv', '_metadata.json'), 'w') as f:

json.dump(metadata, f, indent=2)

📈 6. DATA ANALYSIS ALGORITHMS

6.1 Hysteresis Calculation

python

"""

hysteresis_analysis.py

Calculate χT hysteresis between heating and cooling

"""

import numpy as np

import pandas as pd

from scipy import interpolate

from scipy.signal import savgol_filter

class SCOHysteresisAnalyzer:

def __init__(self, data_df):

self.data = data_df

self.lambdas = data_df['lambda'].unique()

def smooth_χT(self, T, χT, window=11, order=3):

"""Apply Savitzky-Golay smoothing"""

if len(χT) > window:

return savgol_filter(χT, window, order)

return χT

def analyze_lambda(self, lambda_val):

"""Analyze hysteresis for one λ value"""

λ_data = self.data[self.data['lambda'] == lambda_val].copy()

# Separate cycles

heat = λ_data[λ_data['cycle'] == 'heat'].sort_values('T')

cool = λ_data[λ_data['cycle'] == 'cool'].sort_values('T')

# Smooth

heat['χT_smooth'] = self.smooth_χT(heat['T'], heat['χT'])

cool['χT_smooth'] = self.smooth_χT(cool['T'], cool['χT'])

# Common temperature range

T_min = max(heat['T'].min(), cool['T'].min())

T_max = min(heat['T'].max(), cool['T'].max())

T_common = np.linspace(T_min, T_max, 200)

# Interpolate

f_heat = interpolate.interp1d(heat['T'], heat['χT_smooth'],

kind='linear', fill_value='extrapolate')

f_cool = interpolate.interp1d(cool['T'], cool['χT_smooth'],

kind='linear', fill_value='extrapolate')

χT_heat = f_heat(T_common)

χT_cool = f_cool(T_common)

# Hysteresis

ΔχT = χT_heat - χT_cool

ΔχT_abs = np.abs(ΔχT)

# Loop area

area = np.trapz(ΔχT_abs, T_common)

# Transition temperatures (midpoint)

def find_T12(T, χT):

half_max = (χT.max() + χT.min()) / 2

idx = np.argmin(np.abs(χT - half_max))

return T[idx]

T12_heat = find_T12(T_common, χT_heat)

T12_cool = find_T12(T_common, χT_cool)

ΔT12 = T12_heat - T12_cool

return {

'lambda': lambda_val,

'area': area,

'T12_heat': T12_heat,

'T12_cool': T12_cool,

'ΔT12': ΔT12,

'T_common': T_common.tolist(),

'χT_heat': χT_heat.tolist(),

'χT_cool': χT_cool.tolist(),

'ΔχT': ΔχT.tolist()

}

def analyze_all(self):

"""Analyze all λ values"""

results = []

for λ in sorted(self.lambdas):

result = self.analyze_lambda(λ)

results.append(result)

return pd.DataFrame(results)

6.2 λ-Dependence Fitting

python

"""

lambda_fitting.py

Test linear dependence: Area = A₀ + m·λ

"""

def fit_lambda_dependence(results_df):

"""

results_df: DataFrame with 'lambda', 'area'

Returns: fit parameters

"""

from scipy import stats

from scipy.optimize import curve_fit

x = results_df['lambda'].values

y = results_df['area'].values

# Linear fit: y = m*x + b

def linear(x, m, b):

return m*x + b

popt, pcov = curve_fit(linear, x, y)

m, b = popt

m_err, b_err = np.sqrt(np.diag(pcov))

# R²

y_pred = linear(x, *popt)

ss_res = np.sum((y - y_pred)**2)

ss_tot = np.sum((y - np.mean(y))**2)

r_squared = 1 - ss_res/ss_tot

# p-value

_, p_value = stats.pearsonr(x, y)

return {

'slope': m,

'slope_err': m_err,

'intercept': b,

'intercept_err': b_err,

'r_squared': r_squared,

'p_value': p_value,

'prediction': lambda λ: m*λ + b

}

6.3 LIESST Relaxation Analysis

python

"""

relaxation_analysis.py

Analyze photoinduced HS state relaxation

"""

def analyze_relaxation(t, χT, T_relax):

"""

Fit relaxation kinetics

Expected: stretched exponential for λ > 0

"""

from scipy.optimize import curve_fit

# Normalize

χT_norm = (χT - χT.min()) / (χT.max() - χT.min())

# Single exponential

def exp_decay(t, τ, A):

return A * np.exp(-t/τ)

# Stretched exponential (for λ > 0)

def stretched_exp(t, τ, β, A):

return A * np.exp(-(t/τ)**β)

# Try both

try:

popt1, pcov1 = curve_fit(exp_decay, t, χT_norm, p0=[100, 1])

τ1, A1 = popt1

rss1 = np.sum((χT_norm - exp_decay(t, *popt1))**2)

except:

τ1, A1, rss1 = 0, 0, np.inf

try:

popt2, pcov2 = curve_fit(stretched_exp, t, χT_norm,

p0=[100, 0.8, 1],

bounds=([0, 0, 0], [1e4, 1, 1]))

τ2, β2, A2 = popt2

rss2 = np.sum((χT_norm - stretched_exp(t, *popt2))**2)

except:

τ2, β2, A2, rss2 = 0, 0, 0, np.inf

# Select better fit

if rss1 < rss2:

return {

'model': 'exponential',

'τ': τ1,

'A': A1,

'rss': rss1

}

else:

return {

'model': 'stretched',

'τ': τ2,

'β': β2,

'A': A2,

'rss': rss2

}

6.4 Complete Analysis Pipeline

python

"""

run_analysis.py

Complete analysis for SCO hysteresis experiment

"""

import numpy as np

import pandas as pd

import matplotlib.pyplot as plt

from hysteresis_analysis import SCOHysteresisAnalyzer

from lambda_fitting import fit_lambda_dependence

def analyze_experiment(data_file):

"""

Complete analysis from raw data to final plots

"""

# Load data

data = pd.read_csv(data_file)

# Calculate hysteresis for all λ

analyzer = SCOHysteresisAnalyzer(data)

results = analyzer.analyze_all()

# Fit λ dependence

fit = fit_lambda_dependence(results)

# Generate plots

fig, axes = plt.subplots(2, 2, figsize=(14, 10))

# Plot 1: χT vs Temperature (example λ)

ax = axes[0, 0]

λ_example = results.iloc[len(results)//2]['lambda']

λ_data = results[results['lambda'] == λ_example].iloc[0]

T = λ_data['T_common']

χT_heat = λ_data['χT_heat']

χT_cool = λ_data['χT_cool']

ax.plot(T, χT_heat, 'r-', linewidth=2, label='Heating')

ax.plot(T, χT_cool, 'b-', linewidth=2, label='Cooling')

ax.fill_between(T, χT_heat, χT_cool, alpha=0.3, color='purple')

ax.set_xlabel('Temperature (K)')

ax.set_ylabel('χT (emu·K/mol)')

ax.set_title(f'λ = {λ_example:.2f}, Area = {λ_data["area"]:.1f}')

ax.legend()

ax.grid(True, alpha=0.3)

# Plot 2: ΔχT vs Temperature (all λ)

ax = axes[0, 1]

colors = plt.cm.viridis(np.linspace(0, 1, len(results)))

for i, (_, row) in enumerate(results.iterrows()):

T = row['T_common']

ΔχT = row['ΔχT']

ax.plot(T, ΔχT, color=colors[i], linewidth=1.5,

label=f'λ={row["lambda"]:.2f}')

ax.axhline(0, color='k', linestyle='--', alpha=0.5)

ax.set_xlabel('Temperature (K)')

ax.set_ylabel('ΔχT = χT_heat - χT_cool')

ax.set_title('Hysteresis vs Temperature')

ax.legend(bbox_to_anchor=(1.05, 1), loc='upper left')

ax.grid(True, alpha=0.3)

# Plot 3: Area vs λ

ax = axes[1, 0]

ax.errorbar(results['lambda'], results['area'],

fmt='o', markersize=8, capsize=5, color='purple')

λ_fit = np.linspace(0, max(results['lambda']), 100)

A_fit = fit['slope'] * λ_fit + fit['intercept']

ax.plot(λ_fit, A_fit, 'r-', linewidth=2,

label=f'Area = {fit["slope"]:.1f}λ + {fit["intercept"]:.1f}\nR² = {fit["r_squared"]:.3f}')

ax.set_xlabel('λ (entropy weighting)')

ax.set_ylabel('Hysteresis Area (emu·K²/mol)')

ax.set_title('λ-Dependence: A ∝ λ')

ax.legend()

ax.grid(True, alpha=0.3)

# Plot 4: Transition temperature shift

ax = axes[1, 1]

ax.errorbar(results['lambda'], results['ΔT12'],

fmt='s-', markersize=8, color='green')

ax.set_xlabel('λ')

ax.set_ylabel('ΔT₁/₂ = T_heat - T_cool (K)')

ax.set_title('Transition Temperature Shift')

ax.grid(True, alpha=0.3)

plt.tight_layout()

plt.savefig('sco_hysteresis_analysis.png', dpi=300)

plt.show()

# Print results

print("\n" + "="*50)

print("SPIN-CROSSOVER HYSTERESIS ANALYSIS")

print("="*50)

print(f"\nFit: Area = {fit['slope']:.2f}·λ + {fit['intercept']:.2f}")

print(f"Slope error: ±{fit['slope_err']:.2f}")

print(f"R² = {fit['r_squared']:.3f}")

print(f"p-value = {fit['p_value']:.3e}")

if fit['p_value'] < 0.05 and fit['r_squared'] > 0.9:

print("\n✅ λ-framework VALIDATED!")

print("   Magnetic hysteresis shows linear λ-dependence.")

print("   Light-induced entropy weighting confirmed.")

elif fit['p_value'] < 0.05:

print("\n⚠️  Significant λ-dependence but not linear.")

print("   Check for saturation effects at high λ.")

else:

print("\n❌ No significant λ-dependence detected.")

return results, fit

✅ 7. QUALITY CONTROL AND ACCEPTANCE CRITERIA

7.1 Quantitative Acceptance Criteria

| Test | Criterion | If Failed |
| --- | --- | --- |
| Sample purity | PXRD matches reference | Resynthesize |
| Mass accuracy | ±0.01 mg | Remeasure |
| Dark reference (λ=0) | Reproducible hysteresis A₀ | Check thermal contact |
| Temperature accuracy | ±0.5 K | Recalibrate |
| Field calibration | ±1% with Pd standard | Recalibrate |
| Laser power stability | <5% drift over 1h | Check laser |
| λ-dependence p-value | < 0.05 | Insufficient data |
| R² for linear fit | > 0.9 | Check for saturation |

7.2 Null Tests

| Test | Procedure | Expected | Interpretation |
| --- | --- | --- | --- |
| Gradual SCO complex | [Fe(phen)₂(NCS)₂] | No hysteresis at any λ | Control (intrinsic hysteresis needed) |
| Zero field | Measure at 0 Oe | Similar result | Field not driving effect |
| Different wavelength | 650 nm (off-resonance) | No λ effect | LIESFT-specific |
| Thermal erasure | Heat to 400K, remeasure | Returns to λ=0 baseline | Reversible |

7.3 Troubleshooting Guide

| Problem | Likely Cause | Solution |
| --- | --- | --- |
| No hysteresis at λ=0 | Sample degraded | Check PXRD, resynthesize |
| Hysteresis too small | Poor thermal contact | Repack sample |
| λ effect saturates | Full photoexcitation | Reduce power |
| Irreproducible results | Light alignment | Recalibrate laser spot |
| Signal noisy | Insufficient sample | Increase mass to 20 mg |
| Drift during measurement | Temperature instability | Check cryostat |

📁 8. DATA ARCHIVE REQUIREMENTS

8.1 Folder Structure

text

sco_lambda_YYYYMMDD/

├── raw_data/

│   ├── lambda_0.0/

│   │   ├── heating.csv

│   │   ├── cooling.csv

│   │   └── metadata.json

│   ├── lambda_0.1/

│   ├── lambda_0.2/

│   ├── lambda_0.4/

│   ├── lambda_0.6/

│   └── lambda_0.8/

├── calibration/

│   ├── squid_calibration/

│   ├── laser_calibration/

│   └── temperature_calibration/

├── synthesis/

│   ├── batch_records.csv

│   ├── pxrd/

│   └── tga/

├── analysis/

│   ├── processed_data/

│   ├── figures/

│   └── results/

├── code/

│   ├── measurement/

│   ├── analysis/

│   └── requirements.txt

├── metadata/

│   ├── sample_info.pdf

│   ├── instrument_config.pdf

│   └── experiment_log.pdf

└── README.md

8.2 README Template

markdown

# Spin-Crossover λ-Framework Experiment

## Experiment Information

- Date: YYYY-MM-DD

- Operator: [Name]

- Institution: IIT [Bombay/Madras/Kanpur/Kharagpur/Delhi/Roorkee]

## Sample Information

- Complex: [Fe(Htrz)₂(trz)](BF₄)

- Batch: [ID]

- Mass: [XX.X] mg

- PXRD: Matches reference [Yes/No]

## Photoexcitation Parameters

- Wavelength: 532 nm

- Power range: 0-20 mW

- Irradiation time: 5-60 min

- Temperature during irradiation: 10 K

## Measurement Parameters

- Field: 1000 Oe

- Temperature range: 5-400 K

- Ramp rate: 2 K/min

- Data points: every 2 K

## Key Results

| λ | Area (emu·K²/mol) | T₁/₂ heat (K) | T₁/₂ cool (K) | ΔT₁/₂ (K) |

|---|-------------------|---------------|---------------|------------|

| 0.0 | [value] | [value] | [value] | [value] |

| 0.1 | [value] | [value] | [value] | [value] |

| ... | ... | ... | ... | ... |

## Fit Results

- Slope: [value] ± [value] emu·K²/mol

- Intercept: [value] ± [value] emu·K²/mol

- R²: [value]

- p-value: [value]

## Conclusion

- [ ] λ-framework validated (p < 0.05, R² > 0.9)

- [ ] Results inconclusive

- [ ] No evidence for λ-framework

## Data Files

- raw_data/: All measurement files by λ

- calibration/: SQUID, laser, temperature calibrations

- synthesis/: Sample preparation records

- analysis/: Processed results and figures

## Reproduction

1. Install: pip install -r code/requirements.txt

2. Run: python code/run_analysis.py raw_data/

3. Check: analysis/results/summary.pdf

## Contact

[Name]

[Email]

[IIT Affiliation]

📚 9. REFERENCES

- Gütlich, P., et al. (2013). Spin Crossover in Transition Metal Compounds I-III. Springer.

- Kahn, O., & Martinez, C. J. (1998). Science, 279, 44-48.

- Létard, J. F., et al. (1999). Chemical Physics Letters, 313, 115-120. (LIESST)

- Your main paper, Section 4: Microscopic Foundation

- Your main paper, Eq. 22: Microscopic Reciprocity Theorem

- Your main paper, Eq. 31: Connection to curvature

📝 10. COMPLETE PYTHON PACKAGE STRUCTURE

text

sco_lambda/

├── setup.py

├── requirements.txt

├── README.md

├── sco_lambda/

│   ├── __init__.py

│   ├── synthesis/

│   │   ├── __init__.py

│   │   ├── fe_triazole.py

│   │   └── characterization.py

│   ├── calibration/

│   │   ├── __init__.py

│   │   ├── squid.py

│   │   ├── laser.py

│   │   └── temperature.py

│   ├── measurement/

│   │   ├── __init__.py

│   │   ├── protocol.py

│   │   ├── irradiation.py

│   │   └── data_recorder.py

│   ├── analysis/

│   │   ├── __init__.py

│   │   ├── hysteresis.py

│   │   ├── lambda_fit.py

│   │   ├── relaxation.py

│   │   └── visualization.py

│   └── utils/

│       ├── __init__.py

│       ├── constants.py

│       └── file_io.py

└── examples/

├── sample_data/

└── demo_analysis.py

✅ 11. SUCCESS CRITERIA

For the λ-framework to be validated in this experiment:

| Criterion | Target | Verification |
| --- | --- | --- |
| Intrinsic hysteresis | A₀ > 0 at λ=0 | Control sample |
| Enhanced hysteresis | A(λ) > A₀ for λ>0 | Visual in plot |
| Linear λ-dependence | Area ∝ λ | R² > 0.9 |
| Statistical significance | p < 0.05 | p-value from correlation |
| Reversibility | Heat to 400K → returns to λ=0 | Thermal erasure |
| Reproducibility | 3 independent runs | Same slope within 20% |

📄 12. DECLARATION PAGE

markdown

# EXPERIMENT COMPLETION DECLARATION

**Experiment:** Spin-Crossover Magnetic Hysteresis

**Date:** ____________________

**Location:** IIT ____________________

**Sample Information:**

- Complex: [Fe(Htrz)₂(trz)](BF₄)

- Batch ID: _______________

- Mass: _______________ mg

- PXRD verified: Yes / No

**Irradiation Parameters:**

- Wavelength: 532 nm

- Power range: 0-20 mW

- Irradiation times: 5-60 min

- Irradiation temperature: 10 K

**Measurement Parameters:**

- Field: 1000 Oe

- Temperature range: 5 K to 400 K

- Ramp rate: 2 K/min

- Data points: every 2 K

**Key Results:**

- λ values measured: [list]

- A₀ (λ=0): _______________ emu·K²/mol

- Slope m: _______________ ± _______________ emu·K²/mol

- R²: _______________

- p-value: _______________

**Conclusion:**

- [ ] λ-framework VALIDATED (p < 0.05, R² > 0.9)

- [ ] Results inconclusive

- [ ] No evidence for λ-framework

**Operator Signature:** ____________________

**PI Signature:** ____________________

**Date:** ____________________