# Supplementary Information

# Additional Raman Analysis Supporting Thermal Hysteresis

# This Supplementary Information provides additional analysis of the Raman spectra used to quantify thermal hysteresis in the main manuscript. The analysis includes peak fitting, uncertainty estimation, hysteresis loop quantification, and linewidth evolution for two spatial locations on the sample.

# Supplementary Methods

# Raman Spectroscopy

# Raman spectra were collected using a 532 nm excitation laser and a 50× objective. Spectra were acquired in the spectral range 1200–3200 cm⁻¹, covering both the G (~1580 cm⁻¹) and 2D (~2680 cm⁻¹) Raman modes.

# Experimental parameters were:

| # Parameter | # Value |
| --- | --- |
| # Laser wavelength | # 532 nm |
| # Spectral resolution | # ~1.9 cm⁻¹ |
| # Acquisition time | # 30 s |
| # Accumulations | # 1 |
| # Objective | # 50× |

# Temperature-dependent measurements were performed during controlled heating and cooling cycles at:

# 300 K, 350 K, 400 K, 450 K, and 500 K.

# Spectra were recorded at two spatial positions on the sample, referred to as Spot 1 and Spot 2.

# At each temperature, one spectrum was collected during heating and one during cooling.

# Raman Peak Extraction

# The G and 2D Raman modes were extracted using Lorentzian peak fitting with a linear background.

# The fitting model was:

# I(ω)=A(Γ/2)2ω-ω0)2+(Γ/2)2+mω+b

# where

# ω0is the peak center

# Γis the full width at half maximum (FWHM)

# Ais the peak amplitude

# mω+brepresents the linear baseline.

# Peak fitting was performed using nonlinear least-squares optimization.

# Uncertainties were obtained from the covariance matrix of the fit parameters.

# Measurement Uncertainty

# The uncertainty in peak position corresponds to the 1σ confidence interval obtained from the Lorentzian fit covariance matrix.

# Typical uncertainties across the dataset were:

| # Quantity | # Typical uncertainty |
| --- | --- |
| # G peak center | # 0.1–0.5 cm⁻¹ |
| # 2D peak center | # 0.1–0.7 cm⁻¹ |
| # FWHM | # 0.3–1 cm⁻¹ |

# These uncertainties are represented as vertical error bars in the supplementary figures.

# Because a single spectrum was collected at each temperature point, uncertainties arise from peak fitting precision rather than repeated measurements.

# Quantification of Raman Hysteresis

# Thermal hysteresis was quantified by calculating the temperature-integrated separation between the heating and cooling trajectories.

# The loop area was defined as

# A=∫∣ωcool(T)-ωheat(T)∣ dT

# where

# ωheat(T)is the Raman peak position measured during heating

# ωcool(T)is the Raman peak position measured during cooling.

# Numerical integration was performed using the trapezoidal rule.

# Uncertainty Propagation

# The uncertainty in loop area was propagated from the uncertainties in the extracted peak positions:

# σA2=iwi2(σheat,i2+σcool,i2)

# where wirepresents the trapezoidal integration weights and σheat,iand σcool,iare the uncertainties in the heating and cooling peak positions at temperature Ti.

# Supplementary Table S1

# Loop Area and Statistical Significance

| # Spot | # Mode | # Loop area (cm⁻¹·K) | # Uncertainty | # Significance |
| --- | --- | --- | --- | --- |
| # Spot 1 | # G | # 749.7 | # ±24.9 | # 30 σ |
| # Spot 1 | # 2D | # 711.1 | # ±34.2 | # 21 σ |
| # Spot 2 | # G | # 189.0 | # ±31.5 | # 6 σ |
| # Spot 2 | # 2D | # 295.1 | # ±55.7 | # 5 σ |

# All hysteresis loops exceed 3σ statistical significance, confirming that the separation between heating and cooling trajectories is well above measurement uncertainty.

# Supplementary Figures

# Figure S1

# G peak position as a function of temperature for Spot 1.
Error bars represent 1σ uncertainties obtained from Lorentzian peak fitting.

# Figure S2

# G peak position as a function of temperature for Spot 2.

# Figure S3

# 2D peak position as a function of temperature for Spot 1.

# Figure S4

# 2D peak position as a function of temperature for Spot 2.

# Figure S5

# Temperature dependence of the G-mode linewidth (FWHM) for Spot 1.

# Figure S6

# Temperature dependence of the G-mode linewidth (FWHM) for Spot 2.

# Figure S7

# Temperature dependence of the 2D-mode linewidth (FWHM) for Spot 1.

# Figure S8

# Temperature dependence of the 2D-mode linewidth (FWHM) for Spot 2.

# Statistical Significance of the Hysteresis

# The maximum separation between heating and cooling curves reaches approximately 2–4 cm⁻¹, while the measurement uncertainty is typically ≈0.3 cm⁻¹.

# Thus the signal-to-noise ratio is

# Δωσ≈7–13

# which significantly exceeds the 3σ threshold, confirming that the observed Raman hysteresis is statistically robust.

# Data Availability

# The Raman spectra used for this analysis are provided in the accompanying dataset.