STANDARD OPERATING PROCEDURE: Spin-Crossover Magnetic Hysteresis

Entropy-Weighted Magnetic Memory via λ-Framework

SOP-SCO-λ Version 1.0
Date: March 14, 2026
Purpose: To provide a complete, reproducible protocol for measuring magnetic hysteresis in spin-crossover materials as a validation of entropy-weighted thermodynamic geometry.

📋 Table of Contents

- Purpose and Scientific Background

- Theoretical Foundation (λ-Framework Applied to SCO)

- Materials and Sample Preparation

- Instrumentation Specifications

- Pre-Measurement Calibration

- Measurement Protocol

  - 6.1 DC Magnetization (SQUID)

  - 6.2 AC Susceptibility (Frequency-Dependent)

  - 6.3 Thermal Cycling Hysteresis

  - 6.4 Light-Induced Excited Spin State Trapping (LIESST)

- Data Analysis Algorithms

- Complete Python Analysis Code

- Quality Control and Acceptance Criteria

- Expected Results and Interpretation

- Troubleshooting Guide

- Data Archive Requirements

- References

1. Purpose and Scientific Background

1.1 Objective

To experimentally measure the hysteresis in spin-crossover (SCO) materials and demonstrate that:

- The hysteresis width $ΔT_{1/2}$ scales with the entropy-weighting parameter $λ$

- The loop area $A = \oint M(T) dT$ follows $A \propto (C_p - C_v)$

- The asymmetry between heating and cooling branches is a direct manifestation of thermodynamic curvature $Ω = dω$

1.2 Scientific Hypothesis

The entropy-weighted framework predicts:

Ω=dω=∂λv∂p∂λp∂vdp∧dv≠0

For magnetic systems, this curvature manifests as hysteresis in the magnetization vs. temperature curve:

∮M(T)dT=∬Ω=loop area∝(Cp-Cv)

1.3 Why Spin-Crossover Materials?

Spin-crossover compounds (e.g., Fe(Htrz)₂(trz)) are ideal because:

| Property | Advantage |
| --- | --- |
| Large entropy change | ΔS ~ 50-80 J/mol·K between LS and HS states |
| Sharp transition | Cooperative effects give narrow hysteresis |
| Tunable λ | Chemical substitution controls entropy weighting |
| Optical access | LIESST effect allows isothermal switching |
| Room temperature | Many SCO materials operate near 300 K |

2. Theoretical Foundation (λ-Framework Applied to SCO)

2.1 The Spin-Crossover System

A spin-crossover material exists in two states:

| State | Spin | Volume | Entropy | Magnetic Moment |
| --- | --- | --- | --- | --- |
| Low-Spin (LS) | S=0 | Small | Low | Diamagnetic |
| High-Spin (HS) | S=2 | Large | High | Paramagnetic |

The high-spin fraction $γ_{HS}(T)$ follows:

γHS(T)=11+exp⁡ΔH-TΔSRT

2.2 λ-Weighted Formulation

In the entropy-weighted framework, the effective free energy becomes:

Geff(T,γ)=γΔH-TγΔS+RT[γln⁡γ+(1-γ)ln⁡(1-γ)]+λ⋅γ(1-γ)

Where:

- $λ$ = entropy weighting parameter (interaction strength)

- The $γ(1-γ)$ term represents cooperative interactions (regular solution model)

2.3 Key Predictions

1. Hysteresis width scales with λ:

ΔT1/2=2λΔS

2. Loop area scales with heat capacity difference:

A=∮γHS(T)dT∝(Cp-Cv)

3. Frequency-dependent AC susceptibility shows antisymmetric component:

χ''(ω)∝ωτ1+(ωτ)2⋅(1+α⋅λ)

4. LIESST relaxation rate depends on λ:

kLIESST(T)=k0exp⁡Ea+βλRT

3. Materials and Sample Preparation

3.1 Recommended SCO Materials

| Compound | $T_{1/2}$ (K) | ΔH (kJ/mol) | ΔS (J/mol·K) | λ tunability |
| --- | --- | --- | --- | --- |
| Fe(Htrz)₂(trz) | 350-380 | 15-20 | 50-60 | High (anion substitution) |
| [Fe(PM-Bia)₂(NCS)₂] | 170-220 | 8-12 | 40-50 | Medium (ligand modification) |
| [Fe(pic)₃]Cl₂·EtOH | 120-150 | 6-10 | 35-45 | Low (solvent loss) |
| [Fe(PM-PEA)₂(NCS)₂] | 200-250 | 10-15 | 45-55 | Medium |

3.2 Synthesis Protocol (Example: Fe(Htrz)₂(trz))

Materials:

- Fe(BF₄)₂·6H₂O (99%, Sigma-Aldrich)

- Htrz (1H-1,2,4-triazole, 99%, Alfa Aesar)

- Ascorbic acid (antioxidant)

- Ethanol (absolute)

Procedure:

text

Step 1: Solution A

- Dissolve 1.0 mmol Fe(BF₄)₂·6H₂O in 5 mL ethanol

- Add 10 mg ascorbic acid (prevents Fe³⁺ formation)

Step 2: Solution B

- Dissolve 4.0 mmol Htrz in 5 mL ethanol

- Heat to 60°C with stirring

Step 3: Reaction

- Add Solution B dropwise to Solution A at 60°C

- Stir for 30 minutes

- White precipitate forms immediately

Step 4: Aging

- Continue stirring at 60°C for 2 hours

- Cool to room temperature

Step 5: Recovery

- Centrifuge (5000 rpm, 10 min)

- Wash with ethanol (3×)

- Dry under vacuum at 60°C for 12 hours

3.3 λ Tuning via Chemical Substitution

| Anion | λ (relative) | $T_{1/2}$ (K) | ΔT (hysteresis) |
| --- | --- | --- | --- |
| BF₄⁻ | 1.0 (reference) | 350 | 40 K |
| ClO₄⁻ | 1.2 | 345 | 48 K |
| PF₆⁻ | 0.8 | 360 | 32 K |
| CF₃SO₃⁻ | 1.5 | 335 | 60 K |

3.4 Sample Mounting for SQUID

Powder samples:

- Grind sample (agate mortar, 5 min)

- Pack into gelatin capsule (size 4)

- Insert into plastic straw

- Fix with Kapton tape

Thin films:

- Spin-coat on 5×5 mm Si substrate

- Mount in straw with GE varnish

Single crystals:

- Align crystal axes (optional)

- Mount with GE varnish on quartz holder

3.5 Sample Storage

- Store in desiccator (silica gel)

- Protect from light (SCO materials photosensitive)

- Temperature: 25°C

- Maximum storage time: 1 month

4. Instrumentation Specifications

4.1 Core Instruments

| Instrument | Model (example) | Purpose |
| --- | --- | --- |
| SQUID magnetometer | Quantum Design MPMS3 | DC magnetization, AC susceptibility |
| Cryostat | 4-400 K range | Temperature control |
| Magnet | ±7 T | Field-dependent measurements |
| Light source | 532 nm laser (100 mW) | LIESST experiments |
| Optical fiber | Multi-mode, 1 mm core | In-situ illumination |
| Temperature controller | Lakeshore 336 | Independent heater control |

4.2 Required Specifications

| Parameter | Requirement |
| --- | --- |
| Temperature range | 2-400 K |
| Temperature stability | ±0.1 K |
| Temperature sweep rate | 0.1-10 K/min |
| Magnetic field | ±5 T |
| Moment sensitivity | < 10⁻⁷ emu |
| AC frequency range | 0.1 Hz - 1 kHz |
| AC amplitude | 1-10 Oe |

4.3 Sample Environment

text

SQUID Chamber

│

├── Sample Holder (straw)

│       │

│       ├── Gelatin capsule with powder

│       └── GE varnish

│

├── Temperature Sensor (Cernox)

│

├── Heater

│

└── Optical Fiber (for LIESST)

│

└── 532 nm Laser (external)

5. Pre-Measurement Calibration

5.1 Temperature Calibration

Procedure:

- Insert paramagnetic standard (Pd or Dy₂O₃)

- Measure magnetization at 100 Oe from 2-400 K

- Fit Curie law: $χ = C/T + χ_0$

- Compare measured vs. expected temperature

Acceptance: |T_measured - T_set| < 0.5 K over entire range

5.2 Moment Calibration

Procedure:

- Measure standard (Pd, 1 mg)

- Expected moment at 300 K, 1 T: $M = χ·H·mass$

- Calculate calibration factor

Acceptance: Calibration factor within 2% of factory value

5.3 Background Subtraction

Procedure:

- Measure empty sample holder (same capsule + straw)

- Measure sample

- Subtract background: $M_{sample} = M_{total} - M_{holder}$

Acceptance: Background < 10% of sample signal at all temperatures

5.4 Remanent Field Check

Procedure:

- Quench magnet

- Measure standard at zero field

- Fit offset

Acceptance: Remanent field < 5 Oe

5.5 AC Susceptibility Phase Calibration

Procedure:

- Measure paramagnetic standard (Gd₂O₃)

- χ' should be frequency-independent

- χ'' should be zero (no dissipation)

- Adjust phase until χ'' ≈ 0

Acceptance: χ''/χ' < 0.01 at all frequencies

6. Measurement Protocol

6.1 DC Magnetization (SQUID)

Purpose: Determine $T_{1/2}$ and hysteresis width.

For each sample:

| Parameter | Setting |
| --- | --- |
| Field | 1000 Oe |
| Temperature range | 2-400 K (or appropriate) |
| Sweep rate | 2 K/min |
| Stabilization | 60 s at each temperature |
| Measurement mode | DC scan (4 cm, 3 s) |
| Points | Every 2 K (far from transition) |
|  | Every 0.5 K (near transition, ±50 K) |

Protocol:

text

1. Zero-field cool (ZFC) to 2 K

2. Apply field H = 1000 Oe

3. Measure M(T) heating: 2 K → 400 K

4. Measure M(T) cooling: 400 K → 2 K

5. Repeat for field H = 100, 500, 5000 Oe

Expected output: $M(T)$ curves for heating and cooling branches.

6.2 AC Susceptibility (Frequency-Dependent)

Purpose: Measure dynamic response and frequency-dependent asymmetry.

| Parameter | Setting |
| --- | --- |
| AC field amplitude | 5 Oe |
| Frequencies | 0.1, 1, 10, 100, 1000 Hz |
| Temperature range | Through transition ±50 K |
| Temperature steps | 1 K |
| Stabilization | 120 s at each T |

Protocol:

text

For each temperature T in range:

For each frequency f in [0.1, 1, 10, 100, 1000] Hz:

Measure χ'(T,f) and χ''(T,f)

End

End

Expected output: Frequency-dependent in-phase (χ') and out-of-phase (χ'') susceptibility.

6.3 Thermal Cycling Hysteresis

Purpose: Measure hysteresis loop area and its dependence on sweep rate.

| Parameter | Setting |
| --- | --- |
| Field | 1000 Oe |
| Sweep rates | 0.5, 1, 2, 5, 10 K/min |
| Cycles | 3 per rate |
| Temperature range | $T_{1/2} ± 50$ K |

Protocol:

text

For each sweep rate r in [0.5, 1, 2, 5, 10] K/min:

For cycle = 1 to 3:

Heat: T_min → T_max at rate r

Cool: T_max → T_min at rate r

Measure M(T) continuously

End

End

Expected output: Hysteresis loops at different sweep rates.

6.4 Light-Induced Excited Spin State Trapping (LIESST)

Purpose: Measure isothermal relaxation from photo-induced HS state.

| Parameter | Setting |
| --- | --- |
| Temperature | 10 K (base) |
| Illumination | 532 nm, 100 mW, 60 min |
| Relaxation temperatures | 10-100 K (5 K steps) |
| Measurement | M(t) for 2 hours at each T |

Protocol:

text

1. Cool to 10 K in dark

2. Measure baseline M (LS state)

3. Illuminate with 532 nm for 60 min

4. Measure M_HS (fully converted)

5. Turn off light

6. Measure M(t) for 2 hours at T = 10 K

7. Repeat at T = 15, 20, 25, ... 100 K (fresh illumination each time)

Expected output: Relaxation curves $γ_{HS}(t)$ at multiple temperatures.

7. Data Analysis Algorithms

7.1 Extracting $T_{1/2}$ and Hysteresis Width

python

def extract_transition_temperature(T, M_heating, M_cooling):

"""

Find T_{1/2} from sigmoid fit

Parameters:

T: temperature array (K)

M_heating: magnetization on heating (emu)

M_cooling: magnetization on cooling

Returns:

T_heat, T_cool, delta_T

"""

from scipy.optimize import curve_fit

def sigmoid(T, T0, A, B, C):

return A / (1 + np.exp((T0 - T)/B)) + C

# Normalize to high-spin fraction

gamma_heat = (M_heating - np.min(M_heating)) / (np.max(M_heating) - np.min(M_heating))

gamma_cool = (M_cooling - np.min(M_cooling)) / (np.max(M_cooling) - np.min(M_cooling))

# Fit heating

popt_h, _ = curve_fit(sigmoid, T, gamma_heat,

p0=[300, 1, 5, 0], maxfev=5000)

T_half_heat = popt_h[0]

# Fit cooling

popt_c, _ = curve_fit(sigmoid, T, gamma_cool,

p0=[300, 1, 5, 0], maxfev=5000)

T_half_cool = popt_c[0]

delta_T = T_half_heat - T_half_cool

return T_half_heat, T_half_cool, delta_T

7.2 Calculating Loop Area

python

def hysteresis_loop_area(T_heat, gamma_heat, T_cool, gamma_cool):

"""

Calculate hysteresis loop area A = ∮ γ dT

Parameters:

T_heat, gamma_heat: heating branch

T_cool, gamma_cool: cooling branch

Returns:

area: loop area (K)

"""

from scipy.interpolate import interp1d

# Find common temperature range

T_min = max(min(T_heat), min(T_cool))

T_max = min(max(T_heat), max(T_cool))

# Interpolate to common grid

T_common = np.linspace(T_min, T_max, 1000)

f_heat = interp1d(T_heat, gamma_heat, kind='cubic',

bounds_error=False, fill_value='extrapolate')

f_cool = interp1d(T_cool, gamma_cool, kind='cubic',

bounds_error=False, fill_value='extrapolate')

gamma_heat_interp = f_heat(T_common)

gamma_cool_interp = f_cool(T_common)

# Area = integral of difference (absolute value)

area = np.trapz(np.abs(gamma_heat_interp - gamma_cool_interp), T_common)

return area

7.3 Extracting λ from Hysteresis Width

python

def lambda_from_hysteresis(delta_T, delta_S):

"""

Calculate λ from hysteresis width

λ = ΔT₁/₂ * ΔS / 2

Parameters:

delta_T: hysteresis width (K)

delta_S: entropy change (J/mol·K)

Returns:

lambda_val: entropy weighting parameter (J/mol)

"""

lambda_val = delta_T * delta_S / 2

return lambda_val

7.4 AC Susceptibility Analysis

python

def analyze_ac_susceptibility(f, chi_prime, chi_double_prime):

"""

Extract relaxation time and asymmetry

Parameters:

f: frequency array (Hz)

chi_prime: in-phase susceptibility

chi_double_prime: out-of-phase susceptibility

Returns:

tau: relaxation time (s)

alpha: asymmetry parameter

"""

from scipy.optimize import curve_fit

def debye(f, chi0, chi_inf, tau, alpha):

"""Cole-Cole function"""

omega = 2 * np.pi * f

chi = chi_inf + (chi0 - chi_inf) / (1 + (1j * omega * tau)**(1-alpha))

return chi.real, chi.imag

# Fit simultaneously

popt, _ = curve_fit(lambda f: np.concatenate(debye(f, *popt)),

f, np.concatenate([chi_prime, chi_double_prime]),

p0=[1, 0, 1/f[10], 0.1])

chi0, chi_inf, tau, alpha = popt

return tau, alpha

7.5 LIESST Relaxation Analysis

python

def fit_liesst_relaxation(t, gamma):

"""

Fit LIESST relaxation to stretched exponential

γ(t) = γ₀ exp(-(t/τ)^β)

Parameters:

t: time array (s)

gamma: high-spin fraction

Returns:

tau: relaxation time (s)

beta: stretching exponent

"""

from scipy.optimize import curve_fit

def stretched_exp(t, gamma0, tau, beta):

return gamma0 * np.exp(-(t/tau)**beta)

popt, _ = curve_fit(stretched_exp, t, gamma,

p0=[gamma[0], 1000, 0.5],

bounds=([0, 0, 0], [1, 1e6, 1]))

gamma0, tau, beta = popt

return tau, beta

7.6 Complete Analysis Pipeline

python

class SCOLambdaAnalyzer:

"""

Complete analyzer for spin-crossover λ-framework experiments

"""

def __init__(self):

self.data = {}

self.results = {}

def load_squid_data(self, filename):

"""Load SQUID .dat file"""

data = np.loadtxt(filename, skiprows=1)

return {

'T': data[:, 0],

'M': data[:, 1],

'field': data[0, 2] if data.shape[1] > 2 else 1000

}

def analyze_sample(self, sample_id, heating_file, cooling_file,

delta_S, sample_mass_mg):

"""

Complete analysis for one sample

Parameters:

sample_id: sample identifier

heating_file: heating branch data file

cooling_file: cooling branch data file

delta_S: entropy change (J/mol·K)

sample_mass_mg: sample mass (mg)

"""

# Load data

heat = self.load_squid_data(heating_file)

cool = self.load_squid_data(cooling_file)

# Convert to molar susceptibility

mass_g = sample_mass_mg / 1000

mol_mass = 500  # g/mol (typical for SCO)

mol = mass_g / mol_mass

M_heat_molar = heat['M'] / mol

M_cool_molar = cool['M'] / mol

# Normalize to high-spin fraction

M_min = min(np.min(M_heat_molar), np.min(M_cool_molar))

M_max = max(np.max(M_heat_molar), np.max(M_cool_molar))

gamma_heat = (M_heat_molar - M_min) / (M_max - M_min)

gamma_cool = (M_cool_molar - M_min) / (M_max - M_min)

# Extract transition temperatures

T_half_heat, T_half_cool, delta_T = extract_transition_temperature(

heat['T'], gamma_heat, gamma_cool

)

# Calculate loop area

area = hysteresis_loop_area(

heat['T'], gamma_heat,

cool['T'], gamma_cool

)

# Calculate λ

lambda_val = lambda_from_hysteresis(delta_T, delta_S)

# Store results

self.results[sample_id] = {

'T_half_heat': T_half_heat,

'T_half_cool': T_half_cool,

'delta_T': delta_T,

'area': area,

'lambda': lambda_val,

'gamma_heat': gamma_heat.tolist(),

'gamma_cool': gamma_cool.tolist(),

'T_heat': heat['T'].tolist(),

'T_cool': cool['T'].tolist()

}

return self.results[sample_id]

def plot_hysteresis(self, sample_id, save_path=None):

"""Plot hysteresis loop"""

res = self.results[sample_id]

fig, ax = plt.subplots(figsize=(8, 6))

ax.plot(res['T_heat'], res['gamma_heat'], 'r-',

linewidth=2, label='Heating')

ax.plot(res['T_cool'], res['gamma_cool'], 'b-',

linewidth=2, label='Cooling')

ax.fill_between(res['T_heat'], res['gamma_heat'],

np.interp(res['T_heat'], res['T_cool'], res['gamma_cool']),

alpha=0.3, color='purple')

ax.axvline(res['T_half_heat'], color='r', linestyle='--', alpha=0.5)

ax.axvline(res['T_half_cool'], color='b', linestyle='--', alpha=0.5)

ax.set_xlabel('Temperature (K)')

ax.set_ylabel('High-Spin Fraction γ')

ax.set_title(f'Sample {sample_id}: ΔT = {res["delta_T"]:.1f} K, A = {res["area"]:.1f} K')

ax.legend()

ax.grid(True, alpha=0.3)

if save_path:

plt.savefig(save_path, dpi=300, bbox_inches='tight')

plt.show()

return fig

def lambda_scaling_plot(self, results_df, save_path=None):

"""Plot area vs λ"""

fig, ax = plt.subplots(figsize=(10, 6))

ax.errorbar(results_df['lambda'], results_df['area'],

yerr=results_df['area_err'] if 'area_err' in results_df.columns else None,

fmt='o', markersize=8, capsize=5)

# Linear fit

fit = np.polyfit(results_df['lambda'], results_df['area'], 1)

x_fit = np.linspace(0, max(results_df['lambda']), 100)

y_fit = fit[0] * x_fit + fit[1]

ax.plot(x_fit, y_fit, 'r-', label=f'A = {fit[0]:.1f}λ + {fit[1]:.1f}')

ax.set_xlabel('λ (entropy weighting parameter)')

ax.set_ylabel('Hysteresis Loop Area (K)')

ax.set_title('SCO Hysteresis Area vs λ')

ax.legend()

ax.grid(True, alpha=0.3)

if save_path:

plt.savefig(save_path, dpi=300, bbox_inches='tight')

plt.show()

return fig

8. Complete Python Analysis Code

Directory Structure

text

sco_lambda_analysis/

├── __init__.py

├── config/

│   └── experiment_config.yaml

├── data/

│   ├── raw/

│   │   ├── sample_A_heating.dat

│   │   ├── sample_A_cooling.dat

│   │   ├── sample_B_heating.dat

│   │   └── ...

│   └── calibration/

│       ├── background.dat

│       └── standard.dat

├── src/

│   ├── loader.py

│   ├── fitting.py

│   ├── hysteresis.py

│   ├── lambda_calc.py

│   └── plotting.py

├── notebooks/

│   └── analysis_pipeline.ipynb

├── results/

│   ├── figures/

│   └── data/

├── requirements.txt

├── environment.yml

└── run_analysis.py

requirements.txt

text

numpy>=1.21

scipy>=1.7

pandas>=1.3

matplotlib>=3.4

lmfit>=1.0

pyyaml>=5.4

jupyter>=1.0

run_analysis.py

python

#!/usr/bin/env python3

"""

Complete analysis pipeline for SCO λ-framework experiments

"""

import numpy as np

import pandas as pd

import matplotlib.pyplot as plt

import yaml

from pathlib import Path

from src.loader import SCODataLoader

from src.hysteresis import HysteresisAnalyzer

from src.lambda_calc import LambdaCalculator

from src.plotting import SCOPlotter

def main():

# Load configuration

with open('config/experiment_config.yaml', 'r') as f:

config = yaml.safe_load(f)

# Initialize modules

loader = SCODataLoader(config)

hysteresis = HysteresisAnalyzer()

lambda_calc = LambdaCalculator()

plotter = SCOPlotter()

# Load all samples

samples = loader.load_all_samples('data/raw/')

# Analyze each sample

results = []

for sample_id, data in samples.items():

print(f"\nAnalyzing {sample_id}...")

# Extract hysteresis parameters

hyst = hysteresis.analyze(

data['heating']['T'], data['heating']['M'],

data['cooling']['T'], data['cooling']['M']

)

# Calculate λ

lambda_val = lambda_calc.from_hysteresis(

hyst['delta_T'],

config['materials'][sample_id]['delta_S']

)

# Store results

results.append({

'sample': sample_id,

'T_half_heat': hyst['T_half_heat'],

'T_half_cool': hyst['T_half_cool'],

'delta_T': hyst['delta_T'],

'area': hyst['area'],

'lambda': lambda_val,

'composition': config['materials'][sample_id]['composition']

})

# Generate plot

plotter.hysteresis(

data['heating']['T'], hyst['gamma_heat'],

data['cooling']['T'], hyst['gamma_cool'],

title=f"{sample_id}: ΔT = {hyst['delta_T']:.1f} K",

save_path=f"results/figures/{sample_id}_hysteresis.png"

)

# Create results dataframe

results_df = pd.DataFrame(results)

results_df.to_csv('results/data/summary.csv', index=False)

# Plot λ scaling

plotter.lambda_scaling(

results_df['lambda'], results_df['area'],

save_path='results/figures/lambda_scaling.png'

)

print("\n=== Analysis Complete ===")

print(results_df)

return results_df

if __name__ == "__main__":

main()

9. Quality Control and Acceptance Criteria

9.1 Quantitative Acceptance Criteria

| Test | Criterion | If Failed |
| --- | --- | --- |
| Temperature calibration | < 0.5 K error | Recalibrate |
| Moment calibration | < 2% error | Recalibrate |
| Background subtraction | Background < 10% signal | Remeasure background |
| Remanent field | < 5 Oe | Quench magnet |
| AC phase | χ''/χ' < 0.01 | Readjust phase |
| Transition sharpness | dγ/dT > 0.1 K⁻¹ | Sample quality issue |
| Hysteresis reproducibility | ±1 K between cycles | Check sample stability |
| λ scaling | R² > 0.9 | Check material series |

9.2 Null Tests

| Test | Procedure | Expected | Interpretation |
| --- | --- | --- | --- |
| Zero field | Measure at H=0 | No signal | System noise floor |
| Reference compound | Measure Pd | Curie law | Instrument OK |
| Empty holder | Measure empty | Flat baseline | Background OK |
| Repeated cycles | 3× heating/cooling | Identical | Sample stable |
| Different sweep rates | 0.5-10 K/min | Rate-independent | Equilibrium achieved |

10. Expected Results and Interpretation

10.1 Typical Values

| Parameter | Fe(Htrz)₂(trz) | [Fe(PM-Bia)₂(NCS)₂] |
| --- | --- | --- |
| $T_{1/2}$ (K) | 350-380 | 170-220 |
| ΔT (hysteresis) | 30-60 K | 5-15 K |
| Loop area (K) | 500-1000 | 50-150 |
| ΔS (J/mol·K) | 50-60 | 40-50 |
| λ (kJ/mol) | 8-15 | 1-3 |
| dγ/dT (K⁻¹) | 0.2-0.5 | 0.1-0.3 |

10.2 Predicted Signatures

| Observable | Prediction | Figure |
| --- | --- | --- |
| M(T) heating/cooling | Hysteresis loop | Fig 1 |
| Loop area vs λ | Linear scaling | Fig 2 |
| ΔT vs λ | Linear scaling | Fig 3 |
| χ''(ω) | Frequency-dependent peak | Fig 4 |
| LIESST relaxation | Stretched exponential | Fig 5 |

10.3 Interpretation Guidelines

| Observation | Interpretation |
| --- | --- |
| Clear hysteresis loop | Memory via entropy gating |
| Area ∝ λ | Entropy-weighting confirmed |
| ΔT ∝ λ | Interaction strength scales with λ |
| χ'' peak shifts with λ | Dynamic asymmetry |
| LIESST relaxation slower for high λ | Entropy barrier |

10.4 Connection to λ-Framework

| Theoretical Prediction | Experimental Observation |
| --- | --- |
| $Ω = dω ≠ 0$ | Hysteresis loop area > 0 |
| $A ∝ (C_p - C_v)$ | Loop area scales with material properties |
| $ΔT_{1/2} = 2λ/ΔS$ | Hysteresis width ∝ λ |
| Frequency-dependent asymmetry | AC susceptibility shows λ dependence |

11. Troubleshooting Guide

| Problem | Likely Cause | Solution |
| --- | --- | --- |
| No hysteresis | Sample degraded | Check storage, resynthesize |
| Hysteresis too small | Low cooperativity | Try different anion |
| Hysteresis too large | Overly cooperative | Dilute with inert matrix |
| Transition too broad | Poor crystallinity | Anneal sample |
| Drifting baseline | SQUID drift | Remeasure background |
| No LIESST effect | Light not reaching sample | Check fiber alignment |
| Relaxation too fast | Temperature too high | Lower measurement T |
| AC χ'' too small | AC field too low | Increase amplitude |
| Frequency-independent | Relaxation outside window | Change temperature |
| Poor λ scaling | Incomplete anion series | Synthesize more samples |

12. Data Archive Requirements

12.1 Folder Structure

text

experiment_YYYYMMDD_SCO_lambda/

├── raw_data/

│   ├── sample_A/

│   │   ├── heating.dat

│   │   ├── cooling.dat

│   │   └── ac_susceptibility.dat

│   ├── sample_B/

│   └── ...

├── calibration/

│   ├── temperature_calib.dat

│   ├── moment_calib.dat

│   └── background.dat

├── analysis/

│   ├── processed_data/

│   ├── figures/

│   └── results.csv

├── code/

│   ├── sco_analysis/

│   ├── notebooks/

│   └── requirements.txt

├── metadata/

│   ├── synthesis_protocol.pdf

│   ├── sample_characterization.pdf

│   ├── instrument_config.pdf

│   └── experiment_log.pdf

├── photos/

│   ├── sample_mounting.jpg

│   └── setup.jpg

└── README.md

12.2 README Template

markdown

# Spin-Crossover λ-Framework Experiment

## Experiment Information

- Date: YYYY-MM-DD

- Operator: [Name]

- Samples: [list of sample IDs]

- Material system: [e.g., [Fe(Htrz)₂(trz)](BF₄)]

## Sample Preparation

- Synthesis date: YYYY-MM-DD

- Method: [description]

- Anion substitution: [details]

- Mass: [value] mg

- Form: [powder/film/crystal]

## Instrument Configuration

- SQUID: [model]

- Temperature range: [min-max] K

- Field: [value] Oe

- Sweep rate: [value] K/min

- AC frequencies: [list] Hz

## Key Results

- T₁/₂ (heating): [value] K

- T₁/₂ (cooling): [value] K

- Hysteresis width: [value] K

- Loop area: [value] K

- λ (calculated): [value] J/mol

## File Guide

- raw_data/: Raw SQUID data files

- calibration/: Calibration measurements

- analysis/: Processed results and figures

- code/: Analysis scripts

## Reproduction

1. Install dependencies: pip install -r code/requirements.txt

2. Run analysis: python code/run_analysis.py

3. Check results: analysis/results.csv

## Contact

[Name]

[Email]

12.3 Figshare Upload Structure

text

Figshare record: "Spin-Crossover Magnetic Hysteresis - λ-Framework Validation"

Files:

1. SOP_SCO_lambda_v1.0.pdf (this document)

2. raw_data.zip (all raw SQUID files)

3. analysis_code.zip (complete Python package)

4. processed_data.csv (extracted parameters)

5. figures.zip (publication-ready plots)

6. synthesis_protocols.pdf (detailed synthesis)

7. README.md (reproduction guide)

8. environment.yml (conda environment)