🧪 STANDARD OPERATING PROCEDURE #6

Thermoelectric Voltage Hysteresis in Correlated Oxides

Testing λ-Framework via Oxygen Stoichiometry Control

Version: 1.0
Date: March 14, 2026
Laboratory: IIT Materials Science / Low-Temperature Physics Lab
Correspondence: [Principal Investigator]

📋 EXECUTIVE SUMMARY

This SOP provides a complete, reproducible protocol for measuring thermoelectric voltage hysteresis in rare-earth nickelate thin films (RNiO₃, R = Nd, Sm, Eu) as a function of oxygen stoichiometry. The experiment directly tests the λ-framework prediction:

A(λ)=∫∣Vthermheat(T)-Vthermcool(T)∣ dT∝λ

where λ is controlled by oxygen vacancy concentration δ in RNiO₃₋δ.

🔬 1. SCIENTIFIC BACKGROUND

1.1 Why Nickelates?

Rare-earth nickelates (RNiO₃) exhibit:

- Metal-insulator transition tunable by oxygen content

- Strong electron-lattice coupling → large thermopower

- Oxygen stoichiometry easily controlled by annealing

- Established synthesis at multiple IITs

1.2 The λ-Connection

In your framework:

- λ = entropy weighting parameter

- In nickelates: λ ∝ oxygen vacancy concentration ∝ δ

- Vacancies create local entropy fluctuations → weighted ensemble

1.3 Predicted Signature

| Measurement | λ = 0 (stoichiometric) | λ > 0 (oxygen-deficient) |
| --- | --- | --- |
| Thermopower S(T) heating = cooling | ✓ | ✗ (hysteresis) |
| V_therm(T) area | 0 | ∝ δ |
| Transition temperature T_MI | Sharp | Broadened |

🧪 2. MATERIALS AND SAMPLE PREPARATION

2.1 Target Materials

| Material | T_MI (K) | λ Sensitivity | Availability |
| --- | --- | --- | --- |
| NdNiO₃ | 200 K | Medium | IIT Bombay |
| SmNiO₃ | 400 K | High | IIT Madras |
| EuNiO₃ | 480 K | Very High | IIT Kanpur |
| LaNiO₃ | No MI | Control (metallic) | All IITs |

2.2 Thin Film Deposition (Pulsed Laser Deposition)

Substrate:

- LaAlO₃ (001) or SrTiO₃ (001)

- Size: 5×5 mm² to 10×10 mm²

Deposition Parameters:

| Parameter | Value |
| --- | --- |
| Laser fluence | 1.5–2.0 J/cm² |
| Repetition rate | 5 Hz |
| Substrate temperature | 650–750 °C |
| Oxygen pressure | 100–200 mTorr |
| Thickness | 30–50 nm |
| Deposition time | 15–30 min |

Post-annealing for stoichiometry control:

| Sample ID | Annealing Condition | δ (approx) | λ (calculated) |
| --- | --- | --- | --- |
| NNO-00 | 500°C, 760 Torr O₂, 2h | 0.00 | 0.00 |
| NNO-01 | 400°C, 100 mTorr O₂, 1h | 0.05 | 0.10 |
| NNO-02 | 400°C, 10 mTorr O₂, 1h | 0.10 | 0.20 |
| NNO-03 | 400°C, 1 mTorr O₂, 1h | 0.15 | 0.30 |
| NNO-04 | 400°C, vacuum, 1h | 0.20 | 0.40 |

2.3 Electrode Fabrication

Contact Geometry:

text

┌─────────────────────┐

│                     │

│   ┌───V₁───┐        │

│   │        │        │

───┴───┤        ├───┬────┴───

I_in   │        │   I_out

───┬───┤        ├───┴────┬───

│   │        │        │

│   └───V₂───┘        │

│                     │

└─────────────────────┘

Heater (Pt)    Thermometer (Pt)

Electrode Deposition:

- Photolithography for Hall bar pattern

- E-beam evaporation: Ti(5 nm)/Au(50 nm) for contacts

- Lift-off in acetone (12 hours)

- Anneal at 300°C in N₂ (30 min) for Ohmic contacts

Heater/Thermometer:

- Pt (50 nm) deposited on opposite ends

- 4-probe configuration for each

🔧 3. INSTRUMENTATION SPECIFICATIONS

3.1 Core Instruments

| Instrument | Model (example) | Purpose | IIT Availability |
| --- | --- | --- | --- |
| Cryostat | Closed-cycle refrigerator (4–500 K) | Temperature control | All IITs |
| Temperature controller | Lakeshore 336 | Heating/cooling ramps | All IITs |
| Nanovoltmeter | Keithley 2182A | Thermopower measurement | All IITs |
| Current source | Keithley 6221 | Heater current | All IITs |
| Switch matrix | Keithley 7001 | Multiplexing | IITB/IITM/IITK |
| Data acquisition | National Instruments PXI | Automated logging | All IITs |

3.2 Required Configuration

Thermopower Measurement:

- Static DC method (ΔT method)

- Two thermometers (Pt resistors or type E thermocouples)

- Two voltage probes

- Heater power: 1–10 mW (ΔT = 0.5–2 K)

Temperature Ramp Control:

- Rate: 2 K/min (standard), 5 K/min (fast), 1 K/min (slow)

- Stabilization: 2 min at each measurement point

- Step size: 5 K (broad), 2 K (near transition)

3.3 Complete Parts List

| Item | Specification | Quantity | Source |
| --- | --- | --- | --- |
| Pt wire | 25 μm diameter | 2 m | Alfa Aesar |
| Silver paste | High conductivity | 5 g | Ted Pella |
| Gold wire | 25 μm diameter | 1 m | Alfa Aesar |
| Kapton tape | High temperature | 1 roll | DuPont |
| Copper tape | Conductive | 1 roll | 3M |
| Cryogenic grease | Apiezon N | 10 g | M&I Materials |
| Heater resistor | 100 Ω, chip | 5 | Vishay |
| Thermometer | Cernox (optional) | 2 | Lake Shore |

📏 4. PRE-MEASUREMENT CALIBRATION

4.1 Thermometer Calibration

python

"""

thermometer_calibration.py

Calibrate Pt resistance thermometers against known standard

"""

import numpy as np

import pandas as pd

from scipy.optimize import curve_fit

import matplotlib.pyplot as plt

def calibrate_thermometer(T_std, R_measured):

"""

Fit R(T) = R0 + αT + βT²

"""

def RT(T, R0, alpha, beta):

return R0 + alpha*T + beta*T**2

popt, pcov = curve_fit(RT, T_std, R_measured)

R0, alpha, beta = popt

# Calculate residuals

R_fit = RT(T_std, *popt)

residuals = R_measured - R_fit

rms = np.sqrt(np.mean(residuals**2))

return {

'R0': R0, 'alpha': alpha, 'beta': beta,

'rms': rms, 'fitted': R_fit,

'calibration_func': lambda T: RT(T, *popt)

}

# Example usage

T_std = np.array([4, 10, 20, 50, 100, 200, 300, 400, 500])

R_data = np.array([0.5, 1.2, 2.5, 6.8, 15.2, 35.6, 62.1, 95.3, 135.8])  # Example

cal = calibrate_thermometer(T_std, R_data)

print(f"R0 = {cal['R0']:.2f}, α = {cal['alpha']:.4f}, β = {cal['beta']:.6f}")

print(f"RMS residual = {cal['rms']:.3f} Ω")

4.2 Heater Calibration

python

"""

heater_calibration.py

Determine thermal resistance R_th = ΔT / P

"""

def calibrate_heater(I_values, V_values, T_hot, T_cold):

"""

I_values: heater currents (A)

V_values: heater voltages (V)

T_hot: thermometer near heater (K)

T_cold: thermometer far from heater (K)

"""

P_heater = I_values * V_values

ΔT = T_hot - T_cold

# Linear fit: ΔT = R_th * P

slope, intercept = np.polyfit(P_heater, ΔT, 1)

R_th = slope

# Quality check

ΔT_fit = R_th * P_heater

residuals = ΔT - ΔT_fit

r_squared = 1 - np.var(residuals) / np.var(ΔT)

return {

'R_th': R_th,  # K/W

'intercept': intercept,

'r_squared': r_squared

}

4.3 Contact Resistance Check

| Step | Action | Acceptance |
| --- | --- | --- |
| 1 | 2-probe resistance at 300K | < 1 kΩ |
| 2 | 4-probe resistance at 300K | < 100 Ω |
| 3 | I-V linearity (-100 μA to +100 μA) | R² > 0.999 |
| 4 | Symmetry (I+ vs I-) | Difference < 1% |
| 5 | Cool to 4K, repeat 2-probe | < 2× increase |

4.4 Thermopower Reference Measurement

Measure known standard (Constantan vs Pt) at 300K:

- Expected: S ≈ -35 μV/K

- Acceptance: ± 2 μV/K

📊 5. MEASUREMENT PROTOCOL

5.1 Experimental Sequence

For each sample (5 stoichiometries):

python

"""

measurement_protocol.py

Automated measurement sequence

"""

import time

import numpy as np

import pandas as pd

from datetime import datetime

class ThermopowerMeasurement:

def __init__(self, sample_id, delta, cryostat,

temp_controller, nanovoltmeter, current_source):

self.sample_id = sample_id

self.delta = delta

self.lambda_val = 2.0 * delta  # λ ∝ 2δ

self.cryostat = cryostat

self.temp_controller = temp_controller

self.nanovoltmeter = nanovoltmeter

self.current_source = current_source

def measure_thermopower_at_T(self, T_set, I_heater=1e-3):

"""

Measure thermopower at fixed temperature

"""

# Stabilize temperature

self.temp_controller.set_T(T_set)

time.sleep(120)  # 2 min stabilization

# Measure with heater ON

self.current_source.set_current(I_heater)

time.sleep(30)  # thermal equilibration

T_hot = self.temp_controller.read_T('hot')

T_cold = self.temp_controller.read_T('cold')

V_hot = self.nanovoltmeter.read_V('hot_cold')

# Measure with heater OFF

self.current_source.set_current(0)

time.sleep(30)

T_hot_off = self.temp_controller.read_T('hot')

T_cold_off = self.temp_controller.read_T('cold')

V_off = self.nanovoltmeter.read_V('hot_cold')

# Calculate ΔT and ΔV

ΔT_on = T_hot - T_cold

ΔT_off = T_hot_off - T_cold_off

ΔV = V_hot - V_off

# Thermopower

S = ΔV / (ΔT_on - ΔT_off)

return {

'T_set': T_set,

'T_hot': T_hot,

'T_cold': T_cold,

'ΔT': ΔT_on - ΔT_off,

'ΔV': ΔV,

'S': S

}

def run_temperature_cycle(self, T_min=100, T_max=500,

step=5, rate=2, cycle='heat'):

"""

Run heating or cooling cycle

"""

results = []

if cycle == 'heat':

T_range = np.arange(T_min, T_max+step, step)

else:

T_range = np.arange(T_max, T_min-step, -step)

for T in T_range:

print(f"  Measuring at T = {T} K")

self.temp_controller.ramp_to(T, rate)

data = self.measure_thermopower_at_T(T)

data['cycle'] = cycle

results.append(data)

return pd.DataFrame(results)

def run_full_experiment(self):

"""

Complete heating-cooling cycle

"""

print(f"\n{'='*50}")

print(f"Sample: {self.sample_id}, δ = {self.delta}, λ = {self.lambda_val:.2f}")

print(f"{'='*50}")

# Initial cooldown to base

print("Cooling to T_min...")

self.temp_controller.ramp_to(100, 5)

time.sleep(300)

# Heating cycle

print("Heating cycle...")

heat_data = self.run_temperature_cycle(

T_min=100, T_max=500, step=5, rate=2, cycle='heat'

)

# Hold at T_max

print("Holding at T_max...")

time.sleep(600)

# Cooling cycle

print("Cooling cycle...")

cool_data = self.run_temperature_cycle(

T_min=100, T_max=500, step=5, rate=2, cycle='cool'

)

# Combine

full_data = pd.concat([heat_data, cool_data], ignore_index=True)

full_data['sample_id'] = self.sample_id

full_data['delta'] = self.delta

full_data['lambda'] = self.lambda_val

full_data['timestamp'] = datetime.now().isoformat()

return full_data

5.2 Data Recording Format

python

"""

data_recording.py

Save data in standardized format

"""

def save_measurement(data_df, filename):

"""

Save with required columns:

- timestamp: ISO format

- sample_id: e.g., 'NNO-02'

- delta: oxygen deficiency

- lambda: λ = 2*delta

- cycle: 'heat' or 'cool'

- T_set: set temperature (K)

- T_hot: hot thermometer (K)

- T_cold: cold thermometer (K)

- delta_T: temperature difference (K)

- delta_V: thermovoltage (V)

- S: thermopower (V/K)

"""

data_df.to_csv(filename, index=False)

print(f"Data saved to {filename}")

# Also save metadata

metadata = {

'date': data_df['timestamp'].iloc[0],

'samples': data_df['sample_id'].unique().tolist(),

'temperature_range': [data_df['T_set'].min(), data_df['T_set'].max()],

'cycles': data_df['cycle'].unique().tolist()

}

import json

with open(filename.replace('.csv', '_metadata.json'), 'w') as f:

json.dump(metadata, f, indent=2)

📈 6. DATA ANALYSIS ALGORITHMS

6.1 Hysteresis Calculation

python

"""

hysteresis_analysis.py

Calculate thermopower hysteresis between heating and cooling

"""

import numpy as np

import pandas as pd

from scipy import interpolate

class HysteresisAnalyzer:

def __init__(self, data_df):

self.data = data_df

self.samples = data_df['sample_id'].unique()

def analyze_sample(self, sample_id):

"""Calculate hysteresis for one sample"""

sample_data = self.data[self.data['sample_id'] == sample_id]

# Separate cycles

heat = sample_data[sample_data['cycle'] == 'heat'].sort_values('T_set')

cool = sample_data[sample_data['cycle'] == 'cool'].sort_values('T_set')

# Common temperature range

T_min = max(heat['T_set'].min(), cool['T_set'].min())

T_max = min(heat['T_set'].max(), cool['T_set'].max())

T_common = np.linspace(T_min, T_max, 100)

# Interpolate

f_heat = interpolate.interp1d(heat['T_set'], heat['S'],

kind='linear', fill_value='extrapolate')

f_cool = interpolate.interp1d(cool['T_set'], cool['S'],

kind='linear', fill_value='extrapolate')

S_heat = f_heat(T_common)

S_cool = f_cool(T_common)

# Hysteresis

delta_S = S_heat - S_cool

delta_S_abs = np.abs(delta_S)

# Loop area

area = np.trapz(delta_S_abs, T_common)

return {

'sample_id': sample_id,

'lambda': sample_data['lambda'].iloc[0],

'delta': sample_data['delta'].iloc[0],

'T_min': T_min,

'T_max': T_max,

'area': area,

'T_common': T_common.tolist(),

'S_heat': S_heat.tolist(),

'S_cool': S_cool.tolist(),

'delta_S': delta_S.tolist()

}

def analyze_all(self):

"""Analyze all samples"""

results = []

for sample in self.samples:

result = self.analyze_sample(sample)

results.append(result)

return pd.DataFrame(results)

6.2 λ-Dependence Fitting

python

"""

lambda_fitting.py

Test linear dependence: Area = m·λ + b

"""

def fit_lambda_dependence(results_df):

"""

results_df: DataFrame with columns 'lambda', 'area'

Returns: fit parameters and statistics

"""

from scipy import stats

x = results_df['lambda'].values

y = results_df['area'].values

y_err = results_df.get('area_err', np.ones_like(y)*0.1*np.mean(y))

# Weighted linear fit

weights = 1.0 / y_err**2

# Calculate weighted statistics

w = weights / np.sum(weights)

x_mean = np.sum(w * x)

y_mean = np.sum(w * y)

slope = np.sum(w * (x - x_mean) * (y - y_mean)) / np.sum(w * (x - x_mean)**2)

intercept = y_mean - slope * x_mean

# R²

y_pred = slope * x + intercept

ss_res = np.sum(weights * (y - y_pred)**2)

ss_tot = np.sum(weights * (y - y_mean)**2)

r_squared = 1 - ss_res / ss_tot

# p-value (significance)

_, p_value = stats.pearsonr(x, y)

return {

'slope': slope,

'intercept': intercept,

'r_squared': r_squared,

'p_value': p_value,

'prediction': lambda λ: slope * λ + intercept

}

6.3 Complete Analysis Pipeline

python

"""

run_analysis.py

Complete analysis pipeline for all samples

"""

import numpy as np

import pandas as pd

import matplotlib.pyplot as plt

from hysteresis_analysis import HysteresisAnalyzer

from lambda_fitting import fit_lambda_dependence

def analyze_experiment(data_file):

"""

Complete analysis from raw data to final plots

"""

# Load data

data = pd.read_csv(data_file)

# Calculate hysteresis for all samples

analyzer = HysteresisAnalyzer(data)

results = analyzer.analyze_all()

# Fit λ dependence

fit = fit_lambda_dependence(results)

# Generate plots

fig, axes = plt.subplots(2, 2, figsize=(14, 10))

# Plot 1: Thermopower vs Temperature (example sample)

ax = axes[0, 0]

sample = results.iloc[0]['sample_id']

sample_data = data[data['sample_id'] == sample]

heat = sample_data[sample_data['cycle'] == 'heat'].sort_values('T_set')

cool = sample_data[sample_data['cycle'] == 'cool'].sort_values('T_set')

ax.plot(heat['T_set'], heat['S']*1e6, 'r-', linewidth=2, label='Heating')

ax.plot(cool['T_set'], cool['S']*1e6, 'b-', linewidth=2, label='Cooling')

ax.set_xlabel('Temperature (K)')

ax.set_ylabel('Thermopower (μV/K)')

ax.set_title(f'Sample {sample}, λ={results.iloc[0]["lambda"]:.2f}')

ax.legend()

ax.grid(True, alpha=0.3)

# Plot 2: Hysteresis ΔS vs T (example sample)

ax = axes[0, 1]

T = results.iloc[0]['T_common']

delta = results.iloc[0]['delta_S']

ax.plot(T, np.array(delta)*1e6, 'k-', linewidth=2)

ax.fill_between(T, 0, np.array(delta)*1e6, alpha=0.3,

where=np.array(delta)>0, color='red', label='ΔS>0')

ax.fill_between(T, 0, np.array(delta)*1e6, alpha=0.3,

where=np.array(delta)<0, color='blue', label='ΔS<0')

ax.axhline(0, color='k', linestyle='--', alpha=0.5)

ax.set_xlabel('Temperature (K)')

ax.set_ylabel('ΔS = S_heat - S_cool (μV/K)')

ax.set_title(f'Hysteresis, Area = {results.iloc[0]["area"]:.2f}')

ax.legend()

ax.grid(True, alpha=0.3)

# Plot 3: Area vs λ (all samples)

ax = axes[1, 0]

ax.errorbar(results['lambda'], results['area'],

fmt='o', markersize=8, capsize=5, color='purple')

# Fit line

λ_fit = np.linspace(0, max(results['lambda']), 100)

A_fit = fit['slope'] * λ_fit + fit['intercept']

ax.plot(λ_fit, A_fit, 'r-', linewidth=2,

label=f'Slope = {fit["slope"]:.1f}, R² = {fit["r_squared"]:.3f}')

ax.set_xlabel('λ (entropy weighting)')

ax.set_ylabel('Hysteresis Area (μV·K)')

ax.set_title('λ-Dependence: A ∝ λ')

ax.legend()

ax.grid(True, alpha=0.3)

# Plot 4: Comparison with theory

ax = axes[1, 1]

ax.scatter(results['lambda'], results['area'] / results['area'].max(),

s=100, label='Experiment')

ax.plot(λ_fit, λ_fit / λ_fit[-1], 'k--', linewidth=2, label='Theory: A ∝ λ')

ax.set_xlabel('λ (normalized)')

ax.set_ylabel('Area (normalized)')

ax.set_title('Theory vs Experiment')

ax.legend()

ax.grid(True, alpha=0.3)

plt.tight_layout()

plt.savefig('thermoelectric_hysteresis_analysis.png', dpi=300)

plt.show()

# Print results

print("\n" + "="*50)

print("THERMOELECTRIC HYSTERESIS ANALYSIS")

print("="*50)

print(f"\nFit: Area = {fit['slope']:.2f}·λ + {fit['intercept']:.2f}")

print(f"R² = {fit['r_squared']:.3f}")

print(f"p-value = {fit['p_value']:.3e}")

if fit['p_value'] < 0.05:

print("\n✅ Statistically significant λ-dependence confirmed!")

print("   Onsager reciprocity violated in thermoelectric response.")

else:

print("\n⚠️  No significant λ-dependence detected.")

return results, fit

✅ 7. QUALITY CONTROL AND ACCEPTANCE CRITERIA

7.1 Quantitative Acceptance Criteria

| Test | Criterion | If Failed |
| --- | --- | --- |
| Contact resistance | < 100 Ω (4-probe) | Redeposit contacts |
| I-V linearity | R² > 0.999 | Check Schottky barriers |
| Thermometer calibration | RMS < 0.5 K | Recalibrate |
| Heater calibration | R² > 0.99 | Check thermal contact |
| Reference thermopower | Within ±2 μV/K of standard | Check wiring |
| Heating/cooling symmetry at λ=0 |  | ΔS | < 0.5 μV/K | Sample OK (control) |
| λ-dependence p-value | < 0.05 | Insufficient data/signal |  |  |

7.2 Null Tests

| Test | Procedure | Expected | Interpretation |
| --- | --- | --- | --- |
| Control sample (LaNiO₃) | Measure full cycle | No hysteresis | Metallic, no MI transition |
| Zero heater power | Repeat with I=0 | S ≈ 0 | Thermopower measured correctly |
| Same parity check | Reverse voltage leads | S → -S | Thermopolarity correct |
| Isothermal hold | Hold at T for 1h | S stable < 0.1% drift | Thermal equilibrium |

📁 8. DATA ARCHIVE REQUIREMENTS

8.1 Folder Structure

text

thermoelectric_lambda_YYYYMMDD/

├── raw_data/

│   ├── sample_NNO-00/

│   │   ├── heating.csv

│   │   ├── cooling.csv

│   │   └── metadata.json

│   ├── sample_NNO-01/

│   └── ...

├── calibration/

│   ├── thermometers/

│   ├── heater/

│   └── reference/

├── analysis/

│   ├── processed_data/

│   ├── figures/

│   └── results/

├── code/

│   ├── measurement/

│   ├── analysis/

│   └── requirements.txt

├── metadata/

│   ├── sample_preparation.pdf

│   ├── instrument_config.pdf

│   └── experiment_log.pdf

└── README.md

8.2 README Template

markdown

# Thermoelectric Hysteresis Experiment - λ-Framework Validation

## Experiment Information

- Date: YYYY-MM-DD

- Operator: [Name]

- Institution: IIT [Bombay/Madras/Kanpur/Delhi/Kharagpur/Roorkee]

## Samples

| ID | Material | δ (oxygen deficiency) | λ |

|----|----------|----------------------|---|

| NNO-00 | NdNiO₃ | 0.00 | 0.00 |

| NNO-01 | NdNiO₃ | 0.05 | 0.10 |

| NNO-02 | NdNiO₃ | 0.10 | 0.20 |

| NNO-03 | NdNiO₃ | 0.15 | 0.30 |

| NNO-04 | NdNiO₃ | 0.20 | 0.40 |

## Measurement Parameters

- Temperature range: 100 K - 500 K

- Step size: 5 K

- Ramp rate: 2 K/min

- Heater power: 1-10 mW (ΔT ≈ 0.5-2 K)

- Stabilization time: 2 min per point

## Key Results

- Hysteresis detected: [Yes/No]

- λ-dependence slope: [value] μV·K

- R²: [value]

- p-value: [value]

- Conclusion: [λ-framework validated / not validated]

## Data Files

- raw_data/: All raw measurement files

- calibration/: Thermometer and heater calibrations

- analysis/: Processed results and figures

- code/: Python analysis scripts

## Reproduction

1. Install: pip install -r code/requirements.txt

2. Run: python code/run_analysis.py raw_data/

3. Check: analysis/results/summary.pdf

10. COMPLETE PYTHON PACKAGE STRUCTURE

text

thermoelectric_lambda/

├── setup.py

├── requirements.txt

├── README.md

├── thermoelectric_lambda/

│   ├── __init__.py

│   ├── calibration/

│   │   ├── __init__.py

│   │   ├── thermometer.py

│   │   └── heater.py

│   ├── measurement/

│   │   ├── __init__.py

│   │   ├── protocol.py

│   │   └── data_recorder.py

│   ├── analysis/

│   │   ├── __init__.py

│   │   ├── hysteresis.py

│   │   ├── lambda_fit.py

│   │   └── visualization.py

│   └── utils/

│       ├── __init__.py

│       ├── constants.py

│       └── file_io.py

└── examples/

├── sample_data/

└── demo_analysis.py

✅ 11. SUCCESS CRITERIA

For the λ-framework to be validated in this experiment:

| Criterion | Target | Verification |
| --- | --- | --- |
| Hysteresis in thermopower | ΔS(T) ≠ 0 for λ > 0 | Visual in plot |
| Zero hysteresis at λ=0 | ΔS(T) ≈ 0 for δ=0 sample | Within 3σ of noise |
| Linear λ-dependence | Area ∝ λ | R² > 0.9 |
| Statistical significance | p < 0.05 | p-value from correlation |
| Reproducibility | 3 independent runs | Same slope within 20% |

📄 12. DECLARATION PAGE

markdown

# EXPERIMENT COMPLETION DECLARATION

**Experiment:** Thermoelectric Hysteresis in Nickelates

**Date:** ____________________

**Location:** IIT ____________________

**Sample Information:**

- Samples measured: [list IDs]

- Oxygen stoichiometry verified by: [XRD/XPS/Annealing history]

- Contact resistances: ________ Ω (avg)

**Measurement Parameters:**

- Temperature range: ______ K to ______ K

- Ramp rate: ______ K/min

- Number of cycles: ______

**Key Results:**

- Hysteresis detected: Yes / No

- λ-dependence slope: ________ μV·K

- R²: ________

- p-value: ________

**Conclusion:**

- [ ] λ-framework validated (p < 0.05, R² > 0.9, hysteresis at λ>0)

- [ ] Results inconclusive

- [ ] No evidence for λ-framework

**Operator Signature:** ____________________

**PI Signature:** ____________________

**Date:** ____________________