Table 1. Pseudo first order rate constant of Crystal violet for photocatalytic degradation

| Irradiations | Amount of LDS nanoparticles (mg) | Concentration of dye (mg/ml) | Rate constant (k) min1 | Liner equation |
| --- | --- | --- | --- | --- |
| With UV | 500 | 10 | 0.0205 | 0.9962 |
| Without UV | 500 | 10 | 0.01092 | 0.9942 |

Table 2. Compare the Catalytic parameters result of Absorbed HRP in LDS and Free HRP.

| Enzyme | Km (mol) | Vmax (mol) | [E0] (mol) | Kcat S-1 |
| --- | --- | --- | --- | --- |
| Absorbed HRP in LDS | 2.1 103 | 4103 | 2 108 | 2 105 |
| Free HRP | 2.0 103 | 4.4 103 | 2 108 | 2.20 105 |