Supplementary Information for:

Comparative Acid Hydrolysis and Physicochemical Characterization of Agro-Food Processing Residues for Glucose-Rich Extract Production

Tuna Karataş1, Deniz Saltık1, İdil Ceylin Toğan2, Berna Oruc3, Duygu Ekinci3, Sahar Porrang4*, Nur Mustafaoglu4, 5, 6*

1 Molecular Biology, Genetics and Bioengineering Program, Faculty of Engineering and Natural Sciences, Sabanci University, Tuzla 34596, Istanbul, Turkiye

2 Materials Science and Nanoengineering Program, Faculty of Engineering and Natural Sciences, Sabanci University, Tuzla 34596, Istanbul, Turkiye

3 KORDSA Research and Development Center, Izmit 41310, Kocaeli, Turkiye

4 Faculty of Engineering and Natural Sciences, Sabanci University, Tuzla 34596, Istanbul, Turkiye

5 Nanotechnology Research and Application Center (SUNUM), Sabanci University, Tuzla 34596, Istanbul, Turkiye

6 Center of Excellence for Functional Surfaces and Interfaces for Nano Diagnostics (EFSUN), Sabanci University, Tuzla 34956, Istanbul, Turkiye

* Corresponding authors: nur.mustafaoglu@sabanciuniv.edu and sahar.porrang@sabanciuniv.edu

Table 1: Table of the Comparative Analysis for Raw Wheat Husk FTIR Spectra

| This Study | Wang et al. (2022) | Buazar et al. (2019) | Assignment |
| --- | --- | --- | --- |
| 3319.76 cm-1 | 3348 cm-1 | 3320 cm-1 | O-H group stretching vibrations of cellulose |
| 2918.80 cm-1 | 2923 cm-1 | 2915 cm-1 | C-H stretching of methyl groups of cellulose |
| 1728.27 cm-1 |  | 1738 cm-1 | C=O stretching of hemicellulose |
| 1631.15 cm-1 | 1650 cm-1 |  | C=O stretching vibration of lignin |
|  | 1519 cm-1 |  | Aromatic skeletal stretching of lignin |
|  |  | 1412 cm-1 | C=O stretching vibration of free carboxyl groups of lignin |
| 1370.75 cm-1 |  |  | C-H bonding of cellulose and hemicellulose |
|  | 1242 cm-1 | 1130 cm-1 | C-O stretching of acetyl group of lignin |
|  |  | 1052 cm-1 | Siloxane (O-Si-O) functional group |
| 1030.96 cm-1 | 1041 cm-1 | 1012 cm-1 | C-O-C stretching typical of glucan and xylan |
| 790.98 cm-1 |  | 785 cm-1 | Stretching vibration of the silanol (Si–OH) group |

Table 2: Table of the Comparative Analysis for Raw Sweet Lime Peel FTIR Spectra

| This Study | Malakar et al. (2020) | John et al. (2019) | Assignment |
| --- | --- | --- | --- |
| 3303.29 cm-1 100% | 3308.01 cm-1 | 3334 cm-1 | O-H group stretching vibrations of cellulose |
| 2919.86 cm-1 87.4% | 2920.50 cm-1 | 2901 cm-1 | Asymmetrical C-H stretching of methyl and methylene groups of cellulose |
| 1743.69 cm-1 97.0% | 1733.97 cm-1 | 1745 cm-1 | C=O stretching vibration of lignin / hemicellulose |
| 1608.59 cm-1 80.7% | 1603.72 cm-1 | 1606 cm-1 | C=O stretching vibration of lignin |
| 1435.53 cm-1 83.1% | 1434.98 cm-1 |  | Peak related to cellulose |
| 1375.49 cm-1 83.6% | 1369.20 cm-1 |  | Peak related to hemicellulose |
| 1233.98 cm-1 86.1% |  |  |  |
| 1013.90 cm-1 56.9% | 1014.39 cm-1 | 1016 cm-1 | C-O, C-C, C-OH stretching vibrations of cellulose, hemicellulose, lignin |
| 913.90 cm-1 77.4% |  |  | C1–H deformation of cellulose |
| 886.10 cm-1 66.8% |  |  | C1–H deformation of cellulose |
|  | 419.73 cm-1 |  | C-CO-C- bend in ketones |

Table 3: Table of the Comparative Analysis for Carrot Pomace FTIR Spectra

| This Study | Mousavi et al. (2023) | Jafari et al. (2017) | Assignment |
| --- | --- | --- | --- |
| 3286.80 cm-1 86.4% | 3330 cm-1 | 3382.98 cm-1 | O-H group stretching vibrations of cellulose |
| 2933.07 cm-1 93.5% | 2920 cm-1 | 2932.48 cm-1 | -C-H stretching vibrations of methyl groups in cellulose, hemicellulose, lignin |
| 2884.86 cm-1 93.5% |  |  |  |
| 2285.19 cm-1 100% |  |  |  |
| 1729.66 cm-1 95.3% | 1733 cm-1 | 1742.97 cm-1 | C=O stretching vibration of carboxylic acid methyl ester of hemicellulose, lignin |
| 1604.56 cm-1 88.4% | 1607 cm-1 | 1656.70 cm-1 | C=O stretching vibration of free carboxyl groups of hemicellulose |
|  |  | 1427.89 cm−1 | C=O stretching vibration of free carboxyl groups of lignin |
| 1323.48 cm-1 88.4% | 1367 cm-1 |  | cellulose band |
| 1237.28 cm-1 | 1234 cm-1 |  | C–O stretching of lignin |
|  | 1114 cm-1 | 1171.07 cm−1 1138.02 cm-1 | C-O-C ring stretching vibration of cellulose |
| 1011.78 cm-1 63.5% |  | 934.38 cm−1 | Characteristic of the amorphous component of cellulose |

Table 4: Table of the Comparative Analysis for Wheat Husk FTIR Spectra After Acid Hydrolysis

| This Study | Wang et al. (2022) | Bano et al. (2018) | Assignment |
| --- | --- | --- | --- |
| 2916.17 cm-1 | 2923 cm-1 | 2905 cm-1 | C-H stretching vibrations of methyl groups in cellulose, hemicellulose, lignin |
| 2848.46 cm-1 | 2850 cm-1 |  | C-H stretching vibrations of methyl and methylene groups in cellulose, hemicellulose, lignin |
| 1691.68 cm-1 |  |  | C=O Stretching vibration of carboxylic acid methyl ester of hemicellulose and lignin |
| 1462.36 cm-1 |  |  | C=O stretching vibration of free carboxyl groups of lignin |
| 1101.57 cm-1 | 1107 cm-1 | 1109 cm-1 | Bands of glucose |
| 1017.08 cm-1 | 1033 cm-1 | 1045 cm-1 | Bands of glucose |
| 870.29 cm-1 |  |  | Variations of the monosaccharide sugars fructose and glucose |

Table 5: Table of the Comparative Analysis for Sweet Lime Peel FTIR Spectra After Acid Hydrolysis

| This Study | Malakar et al. (2020) | Adina et al. (2010) | Assignment |
| --- | --- | --- | --- |
| 3357.08 cm-1 98.6% | 3338.81 cm-1 |  | O-H group stretching vibrations of cellulose |
| 3107.85 cm-1 89.5% | 2919.87 cm-1 |  | -C-H stretching vibrations of methyl groups in cellulose, hemicellulose, lignin |
| 2872.28 cm-1 92.8% |  |  |  |
| 2547.03 cm-1 100% |  |  |  |
| 2453.24 cm-1 98.3% |  |  |  |
| 1707.07 cm-1 81.3% | 1634.69 cm-1 |  | C=O stretching vibration of carboxylic acid methyl ester of lignin |
| 1537.08 cm-1 93.5% | 1515.89 cm-1 |  | C=C stretching of the aromatic benzene rings of lignin |
| 1436.11 cm-1 84.1% | 1434.98 cm-1 |  | Cellulose band |
|  | 1369.20 cm-1 |  | Hemicellulose band |
|  | 1262.60 cm-1 |  | C-O stretching in lignin |
| 1143.71 cm-1 34.9% | 1159.38 cm-1 | 1149 cm-1 | C-O-C ring stretching vibration of cellulose |
|  | 1103.57 cm-1 | 1107 cm-1 | C-O-C ring vibrational stretching of cellulose |
|  |  | 1078 cm-1 |  |
| 1013.96 cm-1 23.2% | 1032.23 cm-1 | 1033 cm-1 | C-O, C-C and C-OH stretching vibrations of the cellulose, hemicelluloses and lignin |
| 868.07 cm-1 34.1% |  | 991 cm-1 | Variations of the monosaccharide sugars fructose and glucose |

Table 6: Table of the Comparative Analysis for Carrot Pomace FTIR Spectra After Acid Hydrolysis

| This Study | Adina et al. (2010) | Duarte et al. (2002) | Assignment |
| --- | --- | --- | --- |
| 3286.24 cm-1 91.1% |  |  | O-H group stretching vibrations of cellulose |
| 2918.65 cm-1 88.5% |  |  | -C-H stretching vibrations of methyl groups in cellulose, hemicellulose, lignin |
| 2250.84 cm-1 100% |  |  |  |
| 1707.50 cm-1 78.1% |  |  | C=O stretching vibration of carboxylic acid methyl ester of hemicellulose, lignin |
| 1506 cm-1 88% |  |  | C=O stretching vibration of free carboxyl groups of lignin |
| 1422.11 cm-1 84.8% |  |  |  |
| 1144.13 cm-1 51.9% | 1149 cm-1 | 1134 cm-1 | Bands of glucose |
| 1098.11 cm-1 50.6% | 1107 cm-1 | 1109 cm-1 | Bands of glucose |
| 1012.94 cm-1 37.5% | 1078 cm-1 |  | Bands of glucose |
| 871.96 cm-1 47.3% | 1033 cm-1 | 1045 cm-1 | Variations of the monosaccharide sugars fructose and glucose |
| 1144.13 cm-1 51.9% | 991 cm-1 | 987 and 920 cm-1 | Variations of the monosaccharide sugars fructose and glucose |

Table 7: Table of the Comparative Analysis for Acid Hydrolysis Supernatant FTIR Spectra

| Wheat Supernatant | Lime Supernatant | Carrot Supernatant | Koyama et al. (2020) | Song et al. (2018) |
| --- | --- | --- | --- | --- |
|  | 3356.23 cm-1 | 3319.80 cm-1 |  | 3379 cm-1 |
| 2916.17 cm-1 |  |  |  |  |
| 2848.46 cm-1 |  |  |  |  |
|  |  | 2359.46 cm-1 |  | 2360 cm-1 |
|  |  | 2341.36 cm-1 |  |  |
|  | 2129.48 cm-1 | 2125.32 cm-1 |  |  |
| 1691.68 cm-1 | 1635.32 cm-1 | 1634.32 cm-1 |  | 1653 cm-1 |
| 1462.36 cm-1 | 1345.06 cm-1 |  |  |  |
| 1101.57 cm-1 | 1190.24 cm-1 | 1192.03 cm-1 | 1155 cm-1 |  |
| 1017.08 cm-1 | 1079.05 cm-1 |  | 1090 and 1110 cm-1 |  |
| 870.29 cm-1 | 1053.20 cm-1 | 1050.14 cm-1 |  | 1066 cm-1 |
|  |  | 587.11 cm-1 |  |  |