Figure 1. UV–Visible absorption spectra of silver nanoparticles synthesized using seed and pod extracts of A. aromaticum.

Distinct surface plasmon resonance (SPR) peaks appear at 432 nm (Seed-AgNPs) and 445 nm (Pod-AgNPs), confirming nanoparticle formation and indicating smaller particle size for seed-derived samples.

Figure 2. FTIR spectra of seed and pod extracts and their corresponding AgNPs.

Major absorption bands at 3420 cm⁻¹ (O–H stretch), 1634 cm⁻¹ (C=O stretch), and 1385 cm⁻¹ (C–N vibration) denote flavonoid and phenolic participation in reduction and capping.

Figure 3. X-ray diffraction (XRD) patterns of Seed-AgNPs and Pod-AgNPs.

Characteristic Bragg reflections at (111), (200), (220), and (311) correspond to face-centered cubic (FCC) silver (JCPDS No. 04-0783). Sharper peaks for Seed-AgNPs indicate smaller crystallite size (~18 nm).

Figure 4. Transmission electron microscopy (TEM) images and particle size histograms.

Seed-AgNPs: well-dispersed, spherical particles (15–20 nm).
Pod-AgNPs: semi-spherical, slightly aggregated particles (25–30 nm).

Figure 5. Dynamic light scattering (DLS) analysis of Seed- and Pod-AgNPs.

Hydrodynamic diameter distribution shows mean sizes of 22.5 nm (Seed) and 31.8 nm (Pod) with polydispersity indices of 0.28 and 0.32, respectively, confirming narrow distribution and stability.

Figure 6. Energy-dispersive X-ray (EDX) spectrum of AgNPs.

Strong Ag peak at ~3 keV verifies elemental silver; minor carbon (0.28 keV) and oxygen (0.52 keV) peaks arise from organic capping residues.

Figure 7. Zeta potential distribution curves of biosynthesized AgNPs.

Seed-AgNPs show −25.4 mV and Pod-AgNPs −18.1 mV, indicating stable colloidal suspensions with higher electrostatic repulsion for seed-derived particles.

Figure 8. Antibacterial assay plates showing inhibition zones of Seed- and Pod-AgNPs against S. aureus and E. coli.
Clear inhibition zones demonstrate effective antibacterial action, with larger zones observed for Seed-AgNPs compared to Pod-AgNPs.

Figure 9. Antibacterial activity of Seed- and Pod-AgNPs against S. aureus and E. coli.

Zone of inhibition (mm) values confirm stronger antibacterial efficacy of smaller Seed-AgNPs; bars represent mean ± SD (n = 3).

Figure 10. Wound-healing assay (scratch test) on human fibroblast monolayers.

Images at 0 h and 24 h show ~78 % closure for Pod-AgNPs versus ~55 % for Seed-AgNPs, indicating higher regenerative efficiency of phenolic-capped nanoparticles.

Table 1. Physicochemical characteristics of Seed- and Pod-derived AgNPs

| Parameter | Seed-AgNPs | Pod-AgNPs |
| --- | --- | --- |
| UV–Vis λmax (nm) | 432 ± 2 | 445 ± 3 |
| TEM size (nm) | 15–20 | 25–30 |
| DLS mean (nm) | 22.5 ± 1.6 | 31.8 ± 2.1 |
| PDI | 0.28 | 0.32 |
| Zeta potential (mV) | −25.4 ± 1.2 | −18.1 ± 0.9 |
| Crystallite size (XRD, nm) | 18.3 | 27.4 |
| Dominant capping group | Flavonoids/amide | Phenolics/tannins |
| Morphology | Spherical | Semi-spherical |

Table 2. Elemental composition of AgNPs by EDX

| Element | Seed-AgNPs (wt %) | Pod-AgNPs (wt %) |
| --- | --- | --- |
| Ag | 85.6 | 82.4 |
| O | 7.9 | 9.8 |
| C | 6.5 | 7.8 |

Table 3. Biological activities of Seed- and Pod-AgNPs

| Assay | Unit | Seed-AgNPs | Pod-AgNPs |
| --- | --- | --- | --- |
| DPPH scavenging | % | 67 ± 2.4 | 81 ± 2.1 |
| S. aureus ZOI | mm | 18.2 ± 1.3 | 14.1 ± 0.9 |
| E. coli ZOI | mm | 16.7 ± 1.1 | 12.9 ± 1.0 |
| Cell viability (100 µg/mL) | % | 82 ± 3 | 85 ± 4 |
| Wound closure (24 h) | % | 55 ± 2.8 | 78 ± 3.1 |
| Biofilm inhibition | % | 49 ± 2.2 | 51 ± 2.5 |