Supplementary Materials for

Atomically Dispersed CoN3C1-TeN1C3 Diatomic Sites Anchored in N-doped Carbon as Efficient Bifunctional Catalyst for Synergistic Electrocatalytic Hydrogen Evolution and Oxygen Reduction

Minmin Wang1,+, Xiuhui Zheng1,+, Min Li1, Kaian Sun2, Chuhao Liu2, Weng-Chon Cheong2, Zhi Liu1, Yanju Chen1, Shoujie Liu2, Bin Wang3, Yanpeng Li1, Yunqi Liu1*, Chenguang Liu1, Xiang Feng1*, Chaohe Yang1, Yuan Pan1*, Chen Chen2*
1State Key Laboratory of Heavy Oil Processing, China University of Petroleum (East China), Qingdao 266580 (China)

2Department of Chemistry, Tsinghua University, Beijing 100084, China

3School of Chemistry and Chemical Engineering, Shaanxi Normal University, Xi’an 710119 (China)

#These authors contributed equally.

*Correspondence to: liuyq@upc.edu.cn (Y. Liu); xiangfeng@upc.edu.cn (X Feng); panyuan@upc.edu.cn (Y. Pan); cchen@mail.tsinghua.edu.cn (C. Chen)

Fig. S1 Schematic illustration of the synthesis process of Co SASs/N-C.

Fig. S2 Schematic illustration of the synthesis process of Te SASs/N-C.

Fig. S3 XRD pattern of Co-Te DASs/N-C, Co SASs/N-C, Te SASs/N-C, CN.

Fig. S4 Raman spectrum of Co-Te DASs/N-C, Co SASs/N-C, Te SASs/N-C, CN.

a

b

c

Fig. S5 (a) N2 adsorption-desorption isotherms, (b) micropore size distribution, and (c) mesoporous size distribution curves of Co SASs/N-C.

Fig. S6 (a) N2 adsorption-desorption isotherms, (b) micropore size distribution, and (c) mesoporous size distribution curves of Te SASs/N-C.

Fig. S7 SEM images of (a) Te SASs/N-C, (b) Co SASs/N-C.

Fig. S8 TEM images of Co SASs/N-C.

Fig. S9 (a) TEM, (b, c) HAADF-STEM, (d) AC-HAADF-STEM, (e) Atom detecct image of Te SASs/N-C.

Fig. S10 XPS spectrum of Co SASs/N-C (a) Co 2p, (b) Te 3d, (c) N 1s, (d) C 1s.

Fig. S11 (a) Co 2p XPS spectrum of Co SASs/N-C, (b) Te 3d XPS spectrum of Te SASs/N-C.

Fig. S12 EXAFS fitting in (a) q space, (b) R space, and (c) k space of Co SASs/N-C.

Fig. S13 EXAFS fitting in k space of Co-Te DASs/N-C.

Fig. S14 EXAFS in k space of Co-Te DASs/N-C, Co SASs/N-C, Co3O4, CoO and Co foil.

Fig. S15 EXAFS fitting (a) q space, (b) R space, and (c) k space of Te SASs/N-C.

Fig. S16 EXAFS fitting in k spaces of Co-Te DASs/N-C.

Fig. S17 EXAFS in k space of Co-Te DASs/N-C, Te SASs/N-C, TeO2 and Te foil.

Fig. S18 C K-edge spectrum of Co-Te DASs/N-C.

Fig. S19 C K-edge spectrum of Co SASs/N-C.

Fig. S20 LSV curves of Co-Te DASs/N-C with different Co/Te ratios in 0.5 M H2SO4.

Fig. S21 LSV curves of Co-Te DASs/N-C with different Co/Te ratios in 1 M KOH.

a

b

Fig. S22 (a) Tafel slope curves in 0.5 M H2SO4, (b) Tafel slope curves in 1 M KOH.

b

a

Fig. S23 (a) EIS curves (0.5 V vs. Ag/AgCl) in 0.5 M H2SO4, (b) EIS curves (1.6 V vs. SCE) in 1 M KOH.

a

b

Fig. S24 (a) TOF curves in 0.5 M H2SO4, (b) TOF curves in 1 M KOH.

a

b

Fig. S25 (a) Cdl curves of Co-Te DASs/N-C, Co SASs/N-C, Te SASs/N-C and CN in 0.5 M H2SO4, (b) Cdl curves of Co-Te DASs/N-C, Co SASs/N-C, Te SASs/N-C and CN in 1 M KOH.

Fig. S26 LSV curves of Co-Te DASs/N-C, Co SASs/N-C, Te SASs/N-C, CN and Pt/C in PBS.

Fig. S27 i-t curves of Co-Te DASs/N-C in PBS.

Fig. S28 CV curves of Co-Te DASs/N-C, Co SASs/N-C, Te SASs/N-C and CN in PBS.

a

b

Fig. S29 LSV curves of Co SASs/N-C and Te SASs/N-C at different rotation speeds (insets shows the corresponding K-L plots).

Fig. S30 CV curves of Co-Te DASs/N-C, Co SASs/N-C and Te SASs/N-C.

Fig. S31 Tafel slope curve for ORR.

Fig. S32 The optimized configurations of different catalyst models: (a) CN, (b) Te SASs/N-C, (c) Co SASs/N-C, (d) Co-Te SASs/N-C. The adsorption intermediate configurations of HER (H is marked in red circles) and ORR of each structure: (e) CN, (f) Te-SACs/N-C, (g) Co SASs/N-C, (h) Co-Te DASs/N-C.

Fig. S33 The projected density of states (PDOS) of individual Co 3d orbitals of CoN3C1TeN1C3 (Co-Te DASs/NC) before and after H adsorption and the local density of states (LDOS) of H after adsorption: (a) 3dxy,3dxy (b) 3dyz3dyz, (c) 3dxz3dxz, (d) 3dz23dz2, (e) 3dx23dx2, (f) H atom state.

After H adsorption on Co-Te DASs/NC, there are broadenings with different levels in the individual Co 3d orbitals from 3dxy3dxy to 3dx23dx2. Among them, the broadenings of 3dyz3dyz, 3dxz3dxz, and 3dz2 3dz2orbitals are more obvious, indicating that there are strong hybridizations between these orbitals and H atom state, which further cause the delocalization of the H atom state, the negative shift of the bonding orbital, and the positive shift of the anti-bonding orbital. In contrast, according to the study by Hossain et al., only 3dz23dz2 orbitals of Co atom effectively participate in orbital hybridization in CoN4 (Co SASs/N-C). Therefore, CoN3C1TeN1C3 has more active surface states involved in orbital hybridization, thus enhancing H atom adsorption.

Fig. S34 The LDOS of adsorbed H2O molecule in (a) CN, (b) Te SASs/N-C, (c) Co SASs/N-C, and (d) Co-Te DASs/N-C.

a

b

Fig. S35 (a) Discharge/charge cycling curves of two-electrode rechargeable Zn-air batteries at a current density of 2 mA·cm-2, (b) specific capacities of the batteries at a current density of 20 mA cm-2.

Table S1 Single-atom(s) adsorption energy and Bader charge population of different catalysts

|  | aEb(eV) | bCharge density(¦e¦) |  |
| --- | --- | --- | --- |
|  |  | Co | Te |
| Te SASs/N-C | 3.77 | - | 1.220 |
| Co SASs/N-C | 7.64 | 0.834 | - |
| Co-Te DASs/N-C | 9.24 | 0.819 | 1.335 |

The cohesion energies per atom are 4.39 eV (Co) and 2.19 eV (Te) with the sum of them being equal to 6.58 eV, which are smaller than the corresponding binding energies Eb, indicating the stability of these three single-atom or dual-atom catalysts (Table S1). Co atom in Co-Te DASs/N-C has a lower positive charge than that in Co SASs/N-C, while Te atom in Co-Te DASs/N-C has a higher positive charge than that in Te SASs/N-C. This is consistent with the XAS results, as shown in Fig. 2o.

Table S2. ICP results

| Sample | Test element | Element content (wt%) |
| --- | --- | --- |
| Co-Te DASs/N-C | Co | 0.37 |
| Co SASs/N-C | Co | 0.23 |

Table S3. Structural parameters extracted from the EXAFS fitting. (S02=0.85)

| Sample | Scattering pair | CN | R(Å) | σ2(10-3Å2) | ΔE0(eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Co SASs/N-C | Co-N | 4.0 | 1.92 | 4.3 | -3.7 | 0.02 |
| Co-Te DASs/N-C | Co-C | 1.0 | 1.92 | 4.8 | -3.7 |  |
|  | Co-N | 2.9 | 1.93 | 4.9 |  |  |
| Te SASs/N-C | Te-C | 4.1 | 1.92 | 4.4 | -3.5 | 0.02 |
| Co-Te DASs/N-C | Te-C | 3.0 | 1.92 | 4.8 | -3.5 |  |
|  | Te-N | 1.1 | 1.93 | 4.9 |  |  |

S02 is the amplitude reduction factor; CN is the coordination number; R is interatomic distance (the bond length between Fu central atoms and surrounding coordination atoms); σ2 is Debye-Waller factor (a measure of thermal and static disorder in absorber-scatterer distances); ΔE0 is edge-energy shift (the difference between the zero kinetic energy value of the sample and that of the theoretical model). R factor is used to value the goodness of the fitting.