Planar ultrasonic transducer based on a metasurface piezoelectric ring array for subwavelength acoustic focusing in water

Shin Hur 1,4*, Hyunggyu Choi3, Gil Ho Yoon3, Nam Woon Kim1, Duck-Gyu Lee1 and Yong Tae Kim2,4

1 Korea Institute of Machinery and Materials, Department of Nature-Inspired System and Application, 156 Gajeongbuk-Ro, 34103, Daejeon, Republic of Korea

2 Korea Research Institute of Standards and Science (KRISS), Acoustics, Ultrasound and Vibration Group, 267 Gajeong-ro, Yuseong-gu, Daejeon, 34113, Republic of Korea

3 Hanyang University, School of Mechanical Engineering, 222, Wangsimni-ro, Seongdong-gu, Seoul, Republic of Korea

4 University of Science and Technology, 217, Gajeong-ro, Yuseong-gu, Daejeon, 34113, Republic of Korea

*Corresponding Email: shur@kimm.re.kr, ytkim@kriss.re.kr

Table s-1 shows the physical properties of the piezoelectric material of the metasurface piezoelectric ring array used for the multiphysical finite element analysis. Table s-2 is the material properties information of the matching layer and backing layer of the planar ultrasonic transducer used for multiphysics finite element analysis. Table S-1. Physical properties of piezoelectric materials. Density(Kg/m3); 7600; Piezoelectric constant(pm/v), d33; 411. Poisson’s ratio; 0.3; Piezoelectric constant(pm/v), d31; -202. Dielectric constant@1 kHz(ℇ/ℇ0); 1900; Piezoelectric constant(pm/v), d15; 498. Table S-2 Physical properties of matching and backing layer Matching layer (stycast 2057); Backing layer (low-density epoxy). Density(Kg/m3); 1580; Density(Kg/m3); 618.55. Poisson’s ratio; 0.45; Poisson’s ratio; 0.45. Young’s modulus(GPa); 1.7; Sound of speed(m/s); 2020.03. According to Equation (4), a graph showing the change of the correction factor with respect to frequency is shown. Figure S-1. Correction value measurement result according to frequency.