Supplementary Information

To the actual accuracy of structural parameters in single-crystal diffraction studies

and possible origins of their systematic errors

Y.L. Slovokhotov1,2*, I.F. Shishkov3, E.P. Altova3, Yu.V. Novakovskaya3**

1Trapeznikov Institute of Control Science, Russian Acad. Sci., Moscow

2Department of Material Sciences, Lomonosov Moscow State University, Moscow

3Department of Chemistry, Lomonosov Moscow State University, Moscow

E-mails: yurislovo@yandex.ru, jvnovakovskaya@gmail.com

1

5

3

A1

A6

6

2

D3

A5

A4

A2

A3

D1

D6

D5

D4

D2

4

Figure S1. Geometric parameters of naphthalene molecule,1 special position in a crystal (vide infra)

Atom numbering and geometric parameters in Table S1

Bond distances

D1 = DIST1, D2 = DIST2, D3 = DIST3, D4 = DIDST4, D5 = DIST5, D6 = DIST6/

Deviations of atoms from the least-square plane of the molecule

Atom 1: DIST7, atom 2: DIST8, atom 3: DIST9, atom 4: DIST10, atom 5: DIST11, atom 6: DIST12

Bond angles

A1 = ANG1, A2 = ANG2, A3 = ANG3, A4 = ANG4, A5 = ANG5, A6 = ANG6

Table S1

Parameters of naphthalene C10H8 molecules according to high-precision single crystal diffraction studies retrieved from CSD

|  | Refcode |  |  | ANG1 |  | ANG2 |  | ANG3 |  | ANG4 |  | ANG5 |  | ANG6 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | NAPHTA04 |  |  | 119,041 |  | 119,294 |  | 120,255 |  | 120,414 |  | 120,731 |  | 120,264 |  |
| 2 | NAPHTA06 |  |  | 118,931 |  | 119,338 |  | 120,436 |  | 120,407 |  | 120,522 |  | 120,363 |  |
| 3 | NAPHTA07 |  |  | 118,907 |  | 119,338 |  | 120,475 |  | 120,413 |  | 120,554 |  | 120,31 |  |
| 4 | NAPHTA08 |  |  | 118,933 |  | 119,258 |  | 120,363 |  | 120,513 |  | 120,696 |  | 120,234 |  |
| 5 | NAPHTA09 |  |  | 118,802 |  | 119,382 |  | 120,439 |  | 120,382 |  | 120,75 |  | 120,242 |  |
| 6 | NAPHTA10 |  |  | 118,915 |  | 119,265 |  | 120,262 |  | 120,362 |  | 120,853 |  | 120,339 |  |
| 7 | NAPHTA15 |  |  | 119,039 |  | 119,278 |  | 120,571 |  | 120,512 |  | 120,388 |  | 120,21 |  |
| 8 | NAPHTA16 |  |  | 119,026 |  | 119,216 |  | 120,65 |  | 120,586 |  | 120,309 |  | 120,211 |  |
| 9 | NAPHTA17 |  |  | 119,042 |  | 119,218 |  | 120,627 |  | 120,582 |  | 120,311 |  | 120,219 |  |
| 10 | NAPHTA18 |  |  | 119,079 |  | 119,178 |  | 120,617 |  | 120,619 |  | 120,283 |  | 120,223 |  |
| 11 | NAPHTA23 |  |  | 118,952 |  | 119,298 |  | 120,623 |  | 120,554 |  | 120,393 |  | 120,177 |  |
| 12 | NAPHTA24 |  |  | 118,967 |  | 119,24 |  | 120,657 |  | 120,604 |  | 120,372 |  | 120,157 |  |
| 13 | NAPHTA25 |  |  | 118,97 |  | 119,254 |  | 120,633 |  | 120,57 |  | 120,394 |  | 120,178 |  |
| 14 | NAPHTA26 |  |  | 118,971 |  | 119,139 |  | 120,725 |  | 120,648 |  | 120,32 |  | 120,195 |  |
| 15 | NAPHTA27 |  |  | 118,987 |  | 119,069 |  | 120,767 |  | 120,707 |  | 120,263 |  | 120,205 |  |
| 16 | NAPHTA28 |  |  | 118,961 |  | 119,04 |  | 120,778 |  | 120,712 |  | 120,297 |  | 120,21 |  |
| 17 | NAPHTA29 |  |  | 119,01 |  | 118,978 |  | 120,754 |  | 120,722 |  | 120,332 |  | 120,203 |  |
| 18 | NAPHTA30 |  |  | 118,987 |  | 118,897 |  | 120,77 |  | 120,774 |  | 120,354 |  | 120,217 |  |
| 19 | NAPHTA31 |  |  | 118,93 |  | 119,358 |  | 120,607 |  | 120,528 |  | 120,396 |  | 120,179 |  |
| 20 | NAPHTA32 |  |  | 118,944 |  | 119,235 |  | 120,693 |  | 120,655 |  | 120,32 |  | 120,151 |  |
| 21 | NAPHTA33 |  |  | 119,196 |  | 118,902 |  | 120,924 |  | 120,683 |  | 120,078 |  | 120,213 |  |
| 22 | NAPHTA34 |  |  | 119,233 |  | 119,153 |  | 120,443 |  | 120,528 |  | 120,445 |  | 120,196 |  |
| 23 | NAPHTA35 |  |  | 119,15 |  | 119,093 |  | 120,486 |  | 120,495 |  | 120,358 |  | 120,417 |  |
| 24 | NAPHTA36 |  |  | 119,18 |  | 118,973 |  | 120,77 |  | 120,564 |  | 119,917 |  | 120,595 |  |
| Refcode |  | DIST1 (D) | DIST10 (X) |  | DIST11 (X) |  | DIST12 (X) |  | DIST2 (D) |  | DIST3 (D) |  | DIST4 (D) |  | DIST5 (D) |  | DIST6 (D) | DIST7 (X) | DIST8 (X) | DIST9 (X) | R-factor (R) | Study Temp. (I) |
| NAPHTA04 |  | 1,422 | 0,003 |  | 0 |  | 0,002 |  | 1,423 |  | 1,423 |  | 1,378 |  | 1,376 |  | 1,412 | 0,001 | 0,001 | 0,002 | 4,7 | 123 |
| NAPHTA06 |  | 1,422 | 0,002 |  | 0,001 |  | 0,001 |  | 1,422 |  | 1,425 |  | 1,376 |  | 1,375 |  | 1,415 | 0,003 | 0 | 0,003 | 3,8 | 92 |
| NAPHTA07 |  | 1,422 | 0,002 |  | 0,001 |  | 0,001 |  | 1,423 |  | 1,424 |  | 1,376 |  | 1,376 |  | 1,414 | 0,003 | 0,001 | 0,003 | 4 | 109 |
| NAPHTA08 |  | 1,423 | 0,002 |  | 0,002 |  | 0,001 |  | 1,421 |  | 1,424 |  | 1,375 |  | 1,375 |  | 1,412 | 0,002 | 0,001 | 0,003 | 3,8 | 143 |
| NAPHTA09 |  | 1,423 | 0,002 |  | 0,002 |  | 0,001 |  | 1,418 |  | 1,423 |  | 1,372 |  | 1,377 |  | 1,409 | 0,002 | 0 | 0,003 | 3,8 | 184 |
| NAPHTA10 |  | 1,42 | 0,003 |  | 0,003 |  | 0,001 |  | 1,419 |  | 1,424 |  | 1,368 |  | 1,373 |  | 1,407 | 0,002 | 0,001 | 0,004 | 3,5 | 239 |
| NAPHTA15 |  | 1,422 | 0,003 |  | 0,001 |  | 0,002 |  | 1,417 |  | 1,417 |  | 1,373 |  | 1,374 |  | 1,416 | 0,002 | 0,001 | 0,002 | 1,77 | 100 |
| NAPHTA16 |  | 1,421 | 0,003 |  | 0,001 |  | 0,002 |  | 1,418 |  | 1,418 |  | 1,374 |  | 1,375 |  | 1,416 | 0,002 | 0,001 | 0,002 | 2,03 | 135 |
| NAPHTA17 |  | 1,418 | 0,002 |  | 0,001 |  | 0,002 |  | 1,416 |  | 1,416 |  | 1,372 |  | 1,373 |  | 1,413 | 0,001 | 0,001 | 0,002 | 2,87 | 170 |
| NAPHTA18 |  | 1,418 | 0,002 |  | 0,001 |  | 0,001 |  | 1,416 |  | 1,417 |  | 1,373 |  | 1,374 |  | 1,414 | 0,001 | 0,001 | 0,002 | 3,64 | 205 |
| NAPHTA23 |  | 1,426 | 0,003 |  | 0,001 |  | 0,002 |  | 1,422 |  | 1,42 |  | 1,377 |  | 1,376 |  | 1,42 | 0,001 | 0,001 | 0,002 | 4 | 10 |
| NAPHTA24 |  | 1,426 | 0,003 |  | 0,001 |  | 0,002 |  | 1,421 |  | 1,42 |  | 1,377 |  | 1,376 |  | 1,42 | 0,002 | 0,001 | 0,003 | 3,37 | 30 |
| NAPHTA25 |  | 1,425 | 0,003 |  | 0,001 |  | 0,002 |  | 1,42 |  | 1,419 |  | 1,375 |  | 1,375 |  | 1,419 | 0,001 | 0,001 | 0,002 | 3,73 | 60 |
| NAPHTA26 |  | 1,424 | 0,003 |  | 0,001 |  | 0,002 |  | 1,422 |  | 1,419 |  | 1,376 |  | 1,375 |  | 1,418 | 0,001 | 0,001 | 0,003 | 3,5 | 90 |
| NAPHTA27 |  | 1,424 | 0,003 |  | 0,001 |  | 0,002 |  | 1,422 |  | 1,419 |  | 1,376 |  | 1,374 |  | 1,418 | 0,002 | 0,001 | 0,002 | 4,01 | 120 |
| NAPHTA28 |  | 1,423 | 0,003 |  | 0,001 |  | 0,002 |  | 1,421 |  | 1,418 |  | 1,374 |  | 1,373 |  | 1,416 | 0,002 | 0,001 | 0,002 | 3,66 | 150 |
| NAPHTA29 |  | 1,422 | 0,002 |  | 0,001 |  | 0,002 |  | 1,421 |  | 1,417 |  | 1,373 |  | 1,372 |  | 1,414 | 0,001 | 0,001 | 0,002 | 4,05 | 180 |
| NAPHTA30 |  | 1,422 | 0,003 |  | 0,001 |  | 0,002 |  | 1,419 |  | 1,415 |  | 1,371 |  | 1,37 |  | 1,411 | 0,001 | 0,001 | 0,002 | 5,13 | 220 |
| NAPHTA31 |  | 1,423 | 0,002 |  | 0,001 |  | 0,002 |  | 1,421 |  | 1,422 |  | 1,377 |  | 1,378 |  | 1,419 | 0,002 | 0 | 0,003 | 2,34 | 5 |
| NAPHTA32 |  | 1,424 | 0,002 |  | 0,001 |  | 0,001 |  | 1,42 |  | 1,421 |  | 1,376 |  | 1,375 |  | 1,42 | 0,002 | 0,001 | 0,003 | 1,74 | 30 |
| NAPHTA33 |  | 1,422 | 0,004 |  | 0,001 |  | 0,004 |  | 1,424 |  | 1,417 |  | 1,371 |  | 1,373 |  | 1,423 | 0,003 | 0 | 0,003 | 3,2 | 80 |
| NAPHTA34 |  | 1,42 | 0,002 |  | 0,001 |  | 0,001 |  | 1,42 |  | 1,42 |  | 1,375 |  | 1,377 |  | 1,416 | 0,001 | 0,001 | 0,002 | 2,53 | 150 |
| NAPHTA35 |  | 1,419 | 0,002 |  | 0 |  | 0,002 |  | 1,418 |  | 1,418 |  | 1,375 |  | 1,375 |  | 1,408 | 0,002 | 0 | 0,002 | 2,52 | 220 |
| NAPHTA36 |  | 1,419 | 0,003 |  | 0,001 |  | 0,001 |  | 1,417 |  | 1,414 |  | 1,374 |  | 1,369 |  | 1,412 | 0 | 0,002 | 0,002 | 2,81 | 295 |