Supporting Information
Fingerprint-Inspired Flexible Capacitive Sensor for Multi-Directional Tangential Force Sensing via Laser-Etched Geometry
[image: image1.png]



Figure S1. The optical microscope image of a sample without conductive silicone filling
[image: image2.emf]0 10 20 30 40 50 60

0.00

0.02

0.04

0.06

0.08

ΔC/C

0

Pressure/kPa

S

1

=0.00547

S

2

=0.00059


Figure S2. Different pressures were applied to a sensor with an electrode spacing of 400 μm
