Supplementary Information

Supplementary Figure 1. a, TEM images of aggregated TiO2 nanoparticles with 5-10 nm size. b, Ti column intensity variation in the HAADF images of the 5-10 nm TiO2 nanoparticles.

Supplementary Figure 2. HAADF images of STAO at TiO2 step with various density (from 0.005 to 4.5 wt%).

Supplementary Figure 3. a, b, XPS spectra of processing technique and STAO anchoring both induce Ti3+ formation. Reference sample is pristine TiO2 and treated TiO2 without STAO.

c, EPR signals change of photocatalyst with various STAO anchoring density. d, XPS of O1s in pristine TiO2, STAO/TiO2 and pristine STAO.

Supplementary Figure 4. X-ray diffraction patterns of pristine TiO2 substrate and photocatalysts with various STAO anchoring density.

Supplementary Figure 5. The HAADF image of 4.5 wt% STAO anchored on TiO2, the cluster (yellow circle) and the string of pearls (cyan circle) are shown.

Supplementary Figure 6. Stability of CH4-max STAO/TiO2 is investigated by 5 times cycling test.

Supplementary Figure 7. HAADF image and XPS spectra of STAO/TiO2 after 5 times cycling to exhibit the single site is not obviously changed in the CO2 reduction reaction.

Supplementary Figure 8. Blank test in photocatalytic CO2 reduction in the conditions of with no catalyst, no light, no CO2 or no added H2O (absorbed H2O molecule may be involved in the slight conversion of CO2).

Supplementary Figure 9. Time-resolved PL of catalysts with various STAO at step sites.

Supplementary Figure 10. PL suppression limit is achieved by STAO/TiO2. The PL signal of clustered tungsten oxide (4.5 wt%) is seen to increase.

Supplementary Figure 11. Temperature-programmed desorption of CO2 on pristine TiO2, CO-max catalyst and CH4-max catalyst with STAO at step sites.

Supplementary Figure 12. Amplified wavenumber 1350-1850 cm-1 DRIFTS signal of STAO/TiO2 and TiO2 during photocatalytic CO2 reduction in 60 mins.

Supplementary Figure 13. a, Possible pathways of intermediate on W5+ site, especially on CO and CH4 formation steps. b, CO formation on Ti3+ site. The CHO formation is thermodynamically difficult.

Supplementary Figure 14. a, Band diagram of catalysts with various STAO at step sites. b, c, UV-Vis and (αhν)2=A(hν-Eg) relations of various samples. d, UV-light photoelectronic spectra of pristine TiO2 and STAO/TiO2. e, Mott–Schottky plots of TiO2 and STAO/TiO2 samples obtained from semiconductor-electrolyte interface capacity values acquired by EIS at 400 Hz at different bias potentials.

Supplementary Figure 15. BET of catalysts with various STAO at step sites.

Supplementary Table 1. ICP-OES result of catalysts with various STAO at step sites.

| Samples | Tungsten Content（mg/kg） |
| --- | --- |
| TiO2 | 0 |
| 0.005 STAO/TiO2 | 67.8 |
| 0.05 STAO/TiO2 | 543.6 |
| 0.5 STAO/TiO2 | 4988.8 |
| 1 STAO/TiO2 | 9587.9 |
| 2 STAO/TiO2 | 21130.9 |
| 3 STAO/TiO2 | 29674.2 |
| 4.5 STAO/TiO2 | 43862.5 |

Supplementary Table 2. Time-resolved PL corresponding fitting results

| Samples | a1 | τ1 | a2 | τ2 | τav |
| --- | --- | --- | --- | --- | --- |
| TiO2 | 3774.70516 | 155.48648 | -831.31995 | 31.52561 | 161.2805 |
| 0.005 STAO/TiO2 | 3091.27964 | 534.33924 | 245.33996 | 4937.78716 | 2397.445 |
| 0.05 STAO/TiO2 | 2998.28915 | 551.92851 | 263.17384 | 4947.08337 | 2487.22048 |
| 0.5 STAO/TiO2 | 2837.41045 | 646.94305 | 351.63647 | 5382.21475 | 3050.73907 |
| 1 STAO/TiO2 | 3020.57315 | 751.29246 | 280.46687 | 7515.04542 | 4008.30104 |
| 2 STAO/TiO2 | 3050.65721 | 726.28435 | 269.76462 | 7868.43307 | 4220.78892 |
| 3 STAO/TiO2 | 2985.75371 | 784.38295 | 295.56222 | 8576.4513 | 4834.52229 |

Supplementary Table 3 Photocatalysts without sacrificial reagent or noble metal co-catalyst

Photocatalysts     Light Source       Products (µmol g-1 h-1)     Reference

STAO/TiO2     300W Xe Lamp      59.3 (CH4), 181.4 (CO)     This work

AM 1.5 Solar Simulator

CuIn5S8        300W Xe Lamp        8.7 (CH4)             Nat. Energy

λ＞420nm                             4, 690-699 (2019)

HCP-TiO2-FG   300W Xe Lamp     27.62 (CH4), 21.63 (CO)   Nat. Commun

λ＞420nm                               10, 676 (2019)

HCP-TiO2-FG   300W Xe Lamp     51.23 (CH4), 39.51 (CO)   Nat. Commun

UV                                  10, 676 (2019)

InVO4         300W Xe Lamp        18.28 (CO)          J. Am. Chem. Soc.

Solar Simulator                        141, 4209-4213 (2019)

Ti3C2          Xe Lamp        1.78 (CH4) 0.58 (CH3OH)    Adv. Funct. Mater.

/Bi2WO6                                              28, 1800136 (2018)

α‑Fe2O3        300W Xe Lamp          27.2 (CO)              Adv. Mater.

/g‑C3N4           λ＞420nm                           30, 1706108 (2018)

TiO2/Ni(OH)2    350W Xe Lamp        2.2 (CH4) 0.71(CO)   J. Mater. Chem. A

Simulated Sunlight       0.11 (CH3OH)      6,4729-4736 (2018)

0.15 (C2H5OH)

H-TiO2-x          300W Xe Lamp      16.2 (CH4) 4.2(CO)       ACS Catal.

AM 1.5              6.5(H2)        8, 1009−1017 (2018)

BiOIO3        300W Xe Lamp          5.42 (CO)         Adv. Funct. Mater.

28, 1804284 (2018)

carbon@TiO2                         4.22 (CH4)         J. Mater. Chem. A

9.11 (CH3OH)       5,5020-5029 (2017)

ZnIn2S4        300W Xe Lamp          33.2 (CO)        J. Am. Chem. Soc.

139, 7586-7594 (2017)

BiVO4        300W Xe Lamp        398.3 (CH3OH)       J. Am. Chem. Soc.

AM 1.5                           139, 3438−3445 (2017)

TiO2/g-C3N4     300W Xe Lamp    5.21 (CH4) 0.84(CO)  Appl. Catal. B: Environ.

λ＞400nm                         203,910-916 (2017)

TiO2/RGO      300W Xe Lamp         44.56 (CO)         Chem. Eng. J.

λ＞400nm                         316, 449-460 (2017)

m-CeO2/g-C3N4  300W Xe Lamp    0.69 (CH4) 0.51(CO)        Nano Energy

19,145-155 (2016)

N-GQDs/Vo-NaTaON 300W Xe Lamp    10 (CH4) 43(CO)      Nano Energy

λ＞400nm                           30,59-68 (2016)

CdS           300W Xe Lamp         1.02 (CH4)              Small

AM 1.5                           39, 5262-5271 (2015)

Bi2WO6        300W Xe Lamp      75 (CH3OH)             Angew.Chem.

AM 1.5                          54,13971-13974 (2015)

Cu3(BTC)2@TiO2 300W Xe Lamp       2.4 (CH4)               Adv. Mater.

λ＜400nm                      26, 4783-4788 (2014)

TiO2         300W Xe Lamp         1.35 (CH4)           J. Am. Chem. Soc.

136, 8839−8842 (2014)

Go/TiO2       300W Xe Lamp   10.1 (CH4) 16.8 (C2H4)     Adv. Funct. Mater.

23, 1743-1749 (2014)

Cu/TiO2       300W Xe Lamp   0.68 (CH4) 3.85 (CO)    Appl. Catal. B: Environ.

134-135, 349-358 (2014)