Supporting Information

Design of polyvinyl alcohol/bacterial cellulose/sodium alginate/MXene@Polydopamine hydrogel evaporator for fresh water acquisition

Lei Chen, Zhilong Lin, Yu Gao, Wenqin Wang *

* School of Materials Science and Chemical Engineering, Ningbo University, Ningbo 315211, PR China

Section S1 Evaporation performance testing

Indoor Solar Simulation Experiment (Environmental conditions: temperature 25 ± 1 °C, humidity 40 ± 5%): A xenon lamp equipped with an AM 1.5G filter served as the simulated sunlight source. The simulated light intensity was calibrated using a photometer (NBET-19011), while an infrared thermal imager (PI 400) monitored the evaporator surface temperature. An electronic balance connected to a computer recorded water mass changes every 30 seconds.

The formula for calculating the water evaporation rate (v) of an evaporator is as follows:

v= dmS·dt                                                       （1）

Here, m represents the change in mass of water during evaporation, S represents the surface area of the evaporator, and t represents the duration of the evaporation process.

The formula for calculating the light-to-heat conversion efficiency (η) is as follows:

η= △v·HvCopt·Q                                             （2）

Here, η represents the solar-to-thermal conversion efficiency, △v denotes the difference in water evaporation rates between simulated light and dark environments, Hv represents the enthalpy of water evaporation, Copt denotes optical density (1 kW·m⁻²), and Q denotes irradiance (1 kW·m⁻²).

Outdoor Evaporation Experiment: An outdoor solar-driven water evaporation setup was fabricated, with the P-BC-S/MXene@PDA hydrogel employed as the evaporation interface and polymethyl methacrylate (PMMA) utilized for fabricating the vapor collection module. Subsequently, outdoor water evaporation and collection tests were conducted under natural solar irradiation conditions.

Fig. S1. TEM image of MXene.

Fig. S2. XRD patterns of Ti₃AlC₂, MXene, and MXene@PDA.

Fig. S3. FTIR spectra of MXene and MXene@PDA.

Fig. S4. Comparison images of (a) MXene and (b) MXene@PDA before and after 1 day and 30 days of aging.

Fig. S5. (a) N 1s spectrum of the MXene@PDA; (b) Ti 2p spectrum of the MXene@PDA; (c) C 1s spectrum of the P-BC-S hydrogel; (d) C 1s spectrum of the P-BC-S/MXene@PDA hydrogel.

Fig. S6. Salt tolerance test.

Table S1. Performance comparison of the P-BC-S/MXene@PDA hydrogel evaporator with other reported evaporators in the literature.

| Evaporator | Light density （kW/m2) | Evaporation rate (kg·m-2·h-1) | Reference |
| --- | --- | --- | --- |

| CNT/PVA hydrogel | 1 | 1.10 | [33] |
| --- | --- | --- | --- |
| PVA/TA/GO gel copper foam | 1 | 1.88 | [2] |

| J-CNT/PVAs | 1 | 1.34 | [34] |
| --- | --- | --- | --- |
| APRC-PVA/PEG Hydrogel | 1 | 1.45 | [35] |
| PCBM/PNIPAm/PVA | 1 | 1.46 | [36] |
| PVA Sponge | 1 | 1.38 | [37] |
| NSCTP@SF | 1 | 1.96 | [38] |
| Fe3O4/PVA-wood | 1 | 1.30 | [39] |
| PPy/PVA-Wood | 1 | 1.62 | [40] |
| PBHs | 1 | 1.89 | [41] |
| P-BC-S/MXene@PDA hydrogel | 1 | 1.80 | This work |

Fig. S7. Digital photographs of the evaporator during 4 consecutive days of water evaporation testing